High Stability of Ti3C2Tx MXene in PDLC-Based Energy Efficient Smart-Windows

Sunil Kumar1, Hyun Min Park1, Van Huy Nguyen1, Minwook Kim1, Naila Nasir1, Manjeet Kumar2, Yongho Seo1*

1Department of Nanotechnology and Advanced Materials Engineering and HMC, Sejong University, Seoul 05006, South Korea

2Department of Electrical Engineering, Incheon National University, Incheon 406772, South Korea

*Corresponding author: yseo@sejong.ac.kr (Yongho Seo)

Figure S1. Actual photograph of MXene coated glass

Table S1. Electrical properties of MXene coated at glass substrate

| Parameter | Value |
| --- | --- |
| Carrier concentration (cm-3) | -1.620 x1022 |
| Sheet-resistance (Ω/sq.) | 5.12 x102 |
| Hall coefficient (cm3/C) | -3.853 x10-4 |
| Conductivity (S/cm) | 1.941 x103 |

Figure S2. Relative resistance change (R-R0/R0)%, (where R0 is the initial sheet resistance) of MXene films passivated with different NOA65 concentrations (1, 5, 10, and 50 %).

Figure S3. Relative resistance change (R-R0/R0)%, (R0 is the initial sheet resistance) of MXene films passivated with different polymers.

Figure S4. EDX spectra of MXene film on (a) day 1 and (b) day 30.

Table S2. EDX spectra of MXene film on day 1 and day 30.

| Element | Wt.% | Atomic % | Wt.% | Atomic % |
| --- | --- | --- | --- | --- |
|  | Day 1 |  | Day 30 |  |
| C | 33.25 | 39.17 | 30.40 | 33.73 |
| O | 16.27 | 16.95 | 24.59 | 24.45 |
| F | 15.51 | 13.81 | 10.95 | 13.55 |
| Al | 0.07 | 0.02 | 0.04 | 0.04 |
| Cl | 1.16 | 1.28 | 1.05 | 1.11 |
| Ti | 33.74 | 28.66 | 32.97 | 27.12 |
| Total: | 100.00 | 100.00 | 100.00 | 100.00 |

Figure S5. ON/OFF states of MXenes based PDLC smart window after 30 days.

Figure S6. UV-Vis. transmittance spectra of ITO based PDLC smart-window after (a) day 1 (b) 180 days.