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Figure S1. Actual photograph of MXene coated glass 

Table S1. Electrical properties of MXene coated at glass substrate 
	Parameter
	Value

	Carrier concentration (cm-3)
	-1.620 x1022

	Sheet-resistance (Ω/sq.)
	5.12 x102

	Hall coefficient (cm3/C)
	-3.853 x10-4

	Conductivity (S/cm)
	1.941 x103
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Figure S2. Relative resistance change (R-R0/R0)%, (where R0 is the initial sheet resistance) of MXene films passivated with different NOA65 concentrations (1, 5, 10, and 50 %).
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Figure S3. Relative resistance change (R-R0/R0)%, (R0 is the initial sheet resistance) of MXene films passivated with different polymers.
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Figure S4. EDX spectra of MXene film on (a) day 1 and (b) day 30.

Table S2. EDX spectra of MXene film on day 1 and day 30.
	Element
	Wt.%
	Atomic %
	Wt.%
	Atomic %

	
	Day 1
	Day 30

	C
	33.25
	39.17
	30.40
	33.73

	O
	16.27
	16.95
	24.59
	24.45

	F
	15.51
	13.81
	10.95
	13.55

	Al
	0.07
	0.02
	0.04
	0.04

	Cl
	1.16
	1.28
	1.05
	1.11

	Ti
	33.74
	28.66
	32.97
	27.12

	Total:
	100.00
	100.00
	100.00
	100.00
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Figure S5. ON/OFF states of MXenes based PDLC smart window after 30 days.
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Figure S6. UV-Vis. transmittance spectra of ITO based PDLC smart-window after (a) day 1 (b) 180 days.
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