Table 1 Synthesis of 3-benzylpyrano[3,2-c]chromene-2,5-diones 3a-ra,b

aReaction conditions: 1a (1.0 equiv.), 2a (1.0 equiv.), DBU  (4.0 equiv), bIsolated yields.

Table 2 Synthesis of 3-benzylpyrano[3,2-c]chromene-2,5-diones 3s-xa,b

aReaction conditions: 1a (1.0 equiv.), 2a (1.0 equiv.), DBU  (4.0 equiv), bIsolated yields.

Table-3. Photophysical, electrochemical, and band gap calculations of pyranochromene-dione derivatives 3a-x.

| Compound | λmax nm (log ɛ, M−1cm−1)a | λem nmb | τ, ns (A%)c | E0-0 (eV)d | Eox (V)e | Ered (V)e | HOMO (eV)f | LUMO (eV)f | Band gap (eV)g |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 3a | 276 (4.80) 346 (5.03) | 406 | 3.10 (100) | 3.200 | 1.77 | -1.64 | -6.429 | -2.303 | 4.126 |
| 3b | 275 (4.80) 347 (5.01) | 406 | 1.08(45) 6.50 (55) | 3.204 | 1.76 | -1.60 | -6.012 | -2.252 | 3.760 |
| 3c | 275 (4.66) 346 (4.92) | 371 485 | 0.89 (21) 2.74 (59) 9.59 (21) | 3.246 | 1.72 | -1.58 | -6.440 | -2.317 | 4.123 |
| 3d | 276 (4.92) 348 (5.18) | 376 477 | 2.12(61) 5.13 (39) | 3.258 | 1.78 | -1.59 | -6.189 | -2.854 | 3.335 |
| 3e | 274 (4.81) 347 (5.10) | 373 491 | 3.09 (45) 0.84 (25) 9.90 (30) | 3.241 | 1.78 | -1.60 | -6.4 | -2.276 | 4.124 |
| 3f | 273 (4.88) 349 (5.15) | 376 475 | 2.01 (76) 9.09 (24) | 3.247 | 1.77 | -1.61 | -6.402 | -2.278 | 4.124 |
| 3g | 276 (4.62) 346 (5.04) | 373 483 | 2.74 (83) 7.29 (17) | 3.254 | 1.79 | -1.54 | -6.498 | -2.373 | 4.125 |
| 3h | 277 (4.71) 343 (4.95) | 370 498 | 0.97 (17) 3.14 (62) 1.00 (21) | 3.246 | 1.75 | -1.56 | -6.501 | -2.37 | 4.131 |
| 3i | 276 (4.90) 347 (5.18) | 375 475 | 2.74 (83) 7.04 (17) | 3.252 | 1.78 | -1.58 | -6.464 | -2.33 | 4.137 |
| 3j | 277 (4.81) 348 (5.04) | 375 480 | 2.73 (79) 7.33 (21) | 3.248 | 1.77 | -1.54 | -6.441 | -2.309 | 4.132 |
| 3k | 276 (4.69) 347 (4.83) | 417 | 3.34 (100) | 3.201 | 1.80 | -1.53 | -6.501 | -2.38 | 4.121 |
| 3l | 273 (4.85) 348 (5.13) | 417 | 2.06 (55) 5.29 (45) | 3.200 | 1.80 | -1.55 | -6.517 | -2.385 | 4.132 |
| 3m | 275 (4.64) 347 (4.94) | 375 478 | 2.26 (64) 6.89 (36) | 3.250 | 1.78 | -1.56 | -6.568 | -2.434 | 4.138 |
| 3n | 276 (4.63) 348 (4.91) | 373 497 | 2.29 (65) 7.10 (35) | 3.249 | 1.79 | -1.51 | -6.643 | -2.509 | 4.134 |
| 3o | 271 (4.95) 347 (5.02) | 382 466 | 2.82 (76) 4.77 (24) | 3.245 | 1.78 | -1.55 | -6.568 | -2.434 | 4.134 |
| 3p | 274 (4.87) 347 (5.09) | 376 473 | 2.83 (85) 7.33 (15) | 3.247 | 1.78 | -1.49 | -8.965 | -0.988 | 7.977 |
| 3q | 274 (4.64) 347 (4.88) | 371 491 | 0.88 (20) 3.16 (58) 9.73 (22) | 3.243 | 1.80 | -1.45 | -6.643 | -2.508 | 4.135 |
| 3r | 277 (4.92) 351 (5.18) | 379 472 | 1.85 (86) 7.40 (14) | 3.254 | 1.01 | -1.66 | -6.367 | -2.262 | 4.105 |
| 3s | 274 (4.76) 343 (5.00) | 370 480 | 2.14 (74) 7.60 (26) | 3.251 | 1.80 | -1.65 | -6.445 | -2.307 | 4.138 |
| 3t | 275 (4.87) 345 (5.12) | 373 476 | 2.51 (84) 7.51 (16) | 3.252 | 1.78 | -1.65 | -6.436 | -2.3 | 4.136 |
| 3u | 276 (4.95) 345 (5.17) | 374 477 | 2.54 (82) 7.07 (18) | 3.249 | 1.78 | -1.64 | -6.424 | -2.354 | 4.07 |
| 3v | 276 (4.87) 346 (5.13) | 371 479 | 2.37 (78) 7.41 (22) | 3.246 | 1.79 | -1.63 | -6.437 | -2.339 | 4.098 |
| 3w | 276 (4.84) 346 (4.06) | 373 474 | 2.86 (100) | 3.245 | 1.80 | -1.63 | -6.437 | -2.339 | 4.098 |
| 3x | 276 (4.84) 345 (5.10) | 376 470 | 2.50 (85) 7.06 (15) | 3.246 | 1.80 | -1.62 | -6.436 | -2.338 | 4.097 |

aSolvent CH2Cl2. Error limits: λmax, ±1 nm; log ε, ±10%. bSolvent Error limits: λex, ±2 nm; λem, ±1 nm. cAll lifetimes are in nanoseconds (ns); Error limits of τ  ∼10%. Values in parentheses are relative amplitudes of the corresponding decay components. dSinglet state energies as estimated by the intersection between the absorption and the emission spectra; Error limits: ±0.05. eCH2Cl2, 0.1 M TBAP. Glassy carbon working electrode; standard calomel electrode is reference electrode, Pt electrode is auxiliary electrode. Error limits, E1/2 ± 0.03 V. fHOMO and LUMO energy level calculations using the Gaussian 09 package with a functional basis set of the B3LYP/6-31G (d, p). gBand gap values calculated from the optimized dye structures using EHOMO-ELUMO.