Supplementary Information

The non-volatile electrostatic doping effect in MoTe2 field-effect transistors controlled by hexagonal boron nitride and a metal gate

Muhammad Asghar Khan1#, Muhammad Farooq Khan2#, Shania Rehman2,3, Harshada Patil2,3, Ghulam Dastgeer1, Byung Min Ko1 and Jonghwa Eom1*

1Department of Physics & Astronomy and Graphene Research Institute-Texas Photonics Center International Research Center (GRI–TPC IRC), Sejong University, Seoul 05006, Korea

2Department of Electrical Engineering, Sejong University, Seoul 05006, Korea

3Department of Convergence Engineering for Intelligent Drone, Sejong University, Seoul 05006, Korea

#These authors contributed equally.

*Corresponding author: eom@sejong.ac.kr

Figure S1. Raman spectrum of the 2 nm-thick h-BN.

Figure S2. The transfer curve (Ids-Vg-Si) of the 0.8 nm-thick MoTe2 FET shows p-type behavior using Si as the back gate with sweeping from −60 to +60 V.

Figure S3. (a) AFM image of the MoTe2 FET on h-BN. (b) Height profile of MoTe2 along the blue line indicated in the AFM image (thickness ≈ 0.8 nm). (c) h-BN height profile, where the thickness is ~167 nm.

Figure S4. (a) AFM image of the MoTe2 FET on h-BN. (b) Height profile of MoTe2 along the blue line indicated in the AFM image (thickness ≈ 2.4 nm). (c) h-BN height profile, where the thickness is ~42 nm.

Figure S5. (a) Schematic diagram of the MoTe2 FET on a thin h-BN substrate after the photo-induced doping treatment, where donor-like defects are located around the upper side of the h-BN component. (b) Schematic diagram of the MoTe2 FET on a thick h-BN substrate after the photo-induced doping treatment, where the donor-like defects are distributed in the h-BN bulk.

Figure S6. (a) Capacitance as a function of the h-BN frequency as a dielectric material. (b) Capacitance as a function of the h-BN thickness.

(b)

(a)

Figure S7. (a) The transfer characteristics of n-MoTe2 demonstrate the stability of photo-induced doping. (b) Transfer characteristics of the MoTe2 (0.8 nm) FET on a 167 nm-thick h-BN substrate after photo-induced doping for 5 min with different writing voltages. The MoTe2 (0.8 nm) FET on h-BN (167 nm) was prepared by photo-induced doping with the writing voltage of -10 V before starting the experiment, so that MoTe2 (0.8 nm) FET became n-type.

Figure S8. Step-by-step fabrication process of the MoTe2 FET on the h-BN substrate for the generation of a floating-gate structure. (a) The lower isolated Cr/Au (1/10 nm) layer was patterned using e-beam lithography. (b) The h-BN substrate was transferred onto the top of the Cr/Au layer. (c) A MoTe2 flake was transferred onto the top of the h-BN layer. (d) The top Cr/Au (6/90 nm) electrodes were deposited using a thermal evaporator.

Figure S9. (a) N-type memory retention characteristics for program state (+25 V pulse) and erase state (-25 V pulse). (b) P-type memory retention characteristics for program state (-25 V pulse) and erase state (+25 V pulse).

Figure S10. Step-by-step fabrication process of the MoTe2 FET on the h-BN substrate for photo-induced doping. (a) The lower Cr/Au (3/13 nm) electrode was fabricated for use as the writing line voltage. (b) The h-BN substrate was transferred onto the top of the writing voltage electrode. (c) A MoTe2 flake was transferred onto the top of the h-BN substrate. (d) The source and drain Cr/Au (10/80 nm) electrodes were deposited using a thermal evaporator.