On-site colorimetric detection of Salmonella typhimurium based on peroxidase-like activity of aptamer-functionalized 3D covalent organic frameworks embedded with gold nanoparticles

Shengnan Wei, Zhenyue Su, Xiangong Bu, Xuening Shi, Bo Pang, Liang Zhang, Juan Li*, Chao Zhao*

School of Public Health, Jilin University, Changchun, Jilin, 130021, China

* E-mail: czhao0529@jlu.edu.cn; li_juan@jlu.edu.cn

CONTENT

- Instruments

- Bacterial Culture

- Optimization of Experimental Conditions

- Supplementary Figures and Tables

Figure.S1. a Wide-angle XRD pattern of COF-AuNPs, b FT-IR spectrum of COF (red line), COF-AuNPs (black line) and apt-COF-AuNPs (blue line).

Figure.S2. a UV-Vis absorption at 652 nm of TMB-H2O2 system catalyzed by apt-COF-AuNPs with different pH (at 37℃) and b different temperature (at pH = 4.0). Error bars represent the standard deviation of three replicates.

Figure.S3. Storage stability. UV-Vis absorption at 652 nm of TMB-H2O2 system catalyzed by apt-COF-AuNPs with storage for one to six months. Error bars represent the standard deviation of three replicates.

Figure.S4. The optimization results of several parameters: a incubation time of apt-COF-AuNPs and S. typhimurium, b coloration time of TMB-H2O2 system catalyzed by apt-COF-AuNPs + S. typhimurium or apt-COF-AuNPs. Error bars represent the standard deviation of three replicates.

Figure.S5. The calibration curve for S. typhimurium in spiked milk samples.

Figure.S6. Photographs of the colony-forming units on LB agar plates after treatment with real samples (milk of Mengniu Dairy, water of Nanhu Lake and Chaoyang Lake) for 12 h.

Table S1. Comparison of Km and vmax of COF-AuNPs, apt-COF-AuNPs and apt-COF-AuNPs + S. typhimurium for TMB and H2O2.

Table S2. A brief overview of recently reported methods for the determination of S. typhimurium

- Codes of the APP on Smartphone

- Supplementary References

- Instruments

The UV-vis absorption spectra were obtained by a spectrophotometer (TU-1810 DPC Persee, China). Transmission electron microscopy (TEM) images were performed on a JEOL JEM-2100F transmission electron microscope (JEOL, Japan). Fourier transform infrared (FTIR) spectra were recorded as KBr discs on a Nicolet 6700 FTIR spectrometer (Thermo Fisher Scientific, USA). X-ray diffraction (XRD) patterns were recorded on a D2 PHASER diffractometer (Bruker, German).

- Bacterial culture

Five foodborne pathogenic bacterial strains ((S. typhimurium (ATCC 14028) Staphylococcus aureus (S. aureus, ATCC 23213), Listeria monocytogenes (L. monocytogenes, ATCC 43251), Escherichia coli O157:H7 (E. coli O157:H7, ATCC 43888), and Vibrio parahaemolyticus (V. parahaemolyticus, ATCC 17802)) were from the Department of Hygienic Inspection, School of Public Health, Jilin University, China. All of them were grown on Luria-Bertani agar plates, except V. parahaemolyticus, which was on LB plates with 3% (w/v) NaCl. After 24 h of inoculation, a single colony of each strain was picked up and incubated in corresponding Luria-Bertani medium at 37 °C with a shaking at 180 rpm for 12 h. Then, the bacteria were inactivated by the 24 h-incubation of 4% formaldehyde at 4 °C. Lastly, the bacteria were washed three times using sterile PBS by centrifugation at 4000 rpm for 15 min.

- Optimization of Experimental Conditions

The main parameters of the assay procedure were performed to enhance the assay sensitivity and reliability and minimize the total analysis time, including the incubation time of apt-COF-AuNPs and S. typhimurium, reaction temperature, pH and reaction time of apt-COF-AuNPs and TMB-H2O2 system. First, different incubation time (15, 30, 45, 60, 75 min) were used to detect positive samples (1 × 107 CFU/mL S. typhimurium). It can be seen from Figure. S4a. that the value of absorbance at 652 nm was decreased to a plateau in 30 min. Then, a series of different coloration time (2, 3, 4, 5, 6, 7, 8 min) for TMB-H2O2 system was used to detect positive samples (1 × 107 CFU/mL S. typhimurium) and negative samples (staired PBS). It can be seen from Figure. S4b. that the value of absorbance at 652 nm between negative and positive was largest at 5 min. Based on the above results, the following experimental conditions were chosen to obtain the best assay results: (a) incubation time: 30 min. (b) coloration time: 5 min.

- Supplementary Figures and Tables.

Figure.S1. a Wide-angle XRD pattern of COF-AuNPs, b FT-IR spectrum of COF (red line), COF-AuNPs (black line) and apt-COF-AuNPs (blue line).

Figure.S2. a UV-Vis absorption at 652 nm of TMB-H2O2 system catalyzed by apt-COF-AuNPs with different pH (at 37℃) and b different temperature (at pH = 4.0). Error bars represent the standard deviation of three replicates.

Figure.S3. Storage stability. UV-Vis absorption at 652 nm of TMB-H2O2 system catalyzed by apt-COF-AuNPs with storage for one to six months. Error bars represent the standard deviation of three replicates.

Figure.S4. The optimization results of several parameters: a incubation time of apt-COF-AuNPs and S. typhimurium, b coloration time of TMB-H2O2 system catalyzed by apt-COF-AuNPs + S. typhimurium or apt-COF-AuNPs. Error bars represent the standard deviation of three replicates.

Figure.S5. The calibration curve for S. typhimurium in spiked milk samples (A652nm vs. the log scale of S. typhimurium concentration). Error bars represent the standard deviation of three replicates.

Figure.S6. Photographs of the colony-forming units on LB agar plates after treatment with real samples (milk of Mengniu Dairy, water of Nanhu Lake and Chaoyang Lake) for 12 h.

Table S1. Comparison of Km and vmax between COF-AuNPs, apt-COF-AuNPs and apt-COF-AuNPs + S. typhimurium for TMB and H2O2.

| Catalyst | Substance | Km (mM) | vmax (M·s-1) |
| --- | --- | --- | --- |
| COF-AuNPs | TMB | 0.1725 | 6.6094 × 10-8 |
| apt-COF-AuNPs | TMB | 0.1680 | 4.7059 × 10-8 |
| apt-COF-AuNPs + S. typhimurium | TMB | 0.2309 | 2.2815 × 10-8 |
| COF-AuNPs | H2O2 | 266.6667 | 4.9383 × 10-8 |
| apt-COF-AuNPs | H2O2 | 309.2894 | 5.5960 × 10-8 |
| apt-COF-AuNPs + S. typhimurium | H2O2 | 373.1430 | 2.2306 × 10-8 |

Table S2. A brief overview of recently reported methods for the determination of S. typhimurium

| Materials used | Detection method | Linear range (CFU/mL) | LOD (CFU/mL) | Detection time | Reference |
| --- | --- | --- | --- | --- | --- |
| Gold/silver nanodimer | SERS | 102-107 | 50 | 45 min | [1] |
| Alendronic acid @ upconversion nanoparticles and AuNPs | Fluorescence | 1.16 × 102 - 1.16 × 107 | 36 | 21 min | [2] |
| Antibody modified nickel nanowires | Electrochemical | 102-106 | 80 | 2 h | [3] |
| AuNPs magnetic particles | Colorimetric | 103-108 | 1000 | 3h | [4] |
| Aptamers@BSA-AuNC | Colorimetric | 101-106 | 1 | >1h | [5] |
| Aptamer-functionalized magnetic beads and AuNPs | Colorimetric | 102-106 | 240 | >3h | [6] |
| apt-COF-AuNPs | Colorimetric | 101-107 | 7 | 40 min | This work |

- Codes of the APP on Smartphone

- package com.color.identify;

- import android.content.Context;

- import android.graphics.Bitmap;

- import android.graphics.Canvas;

- import android.graphics.Color;

- import android.graphics.Paint;

- import android.util.AttributeSet;

- import android.util.Log;

- import android.view.Gravity;

- import android.view.LayoutInflater;

- import android.view.MotionEvent;

- import android.view.View;

- import android.widget.ImageView;

- import android.widget.TextView;

- import android.widget.Toast;

- import androidx.annotation.Nullable;

- import androidx.palette.graphics.Palette;

- public class RectImageView extends androidx.appcompat.widget.AppCompatImageView {

- private static final int WEIGHT = 100;

- private static final int HEIGHT = 100;

- int x = -1;

- int y;

- int xw;

- int yh;

- private static final String TAG = "RectImageView";

- public RectImageView(Context context) {

- super(context);

- }

- public RectImageView(Context context, AttributeSet attrs) {

- super(context, attrs);

- }

- public RectImageView(Context context, AttributeSet attrs, int defStyleAttr) {

- super(context, attrs, defStyleAttr);

- }

- @Override

- protected void onDraw(Canvas canvas) {

- super.onDraw(canvas);

- Paint paint = new Paint();

- paint.setAntiAlias(true);

- paint.setColor(Color.RED);

- paint.setStrokeWidth(5);

- paint.setStyle(Paint.Style.STROKE);

- if (x != -1) {

- canvas.drawRect(x, y, xw, yh, paint);

- }

- }

- @Override

- public boolean onTouchEvent(MotionEvent event) {

- //手指按下

- try {

- setDrawingCacheEnabled(true);

- Bitmap mPic = getDrawingCache();

- if (event.getAction() == MotionEvent.ACTION_DOWN && mPic != null) {

- Log.d(TAG, mPic.getWidth() + " " + mPic.getHeight() + " " + event.getX() + " " + event.getY());

- if (event.getX() < mPic.getWidth() && event.getY() < mPic.getHeight()) {

- x = (int) event.getX();

- y = (int) event.getY();

- xw = x + WEIGHT;

- yh = y + HEIGHT;

- Log.e(TAG, " " + x + " " + y + " " + xw + " " + yh);

- Bitmap selectPic = mPic.createBitmap(mPic, x, y, WEIGHT, HEIGHT);

- Palette palette = Palette.from(selectPic).generate();

- Palette.Swatch vibrant = palette.getVibrantSwatch();

- Palette.Swatch vibrant1 = palette.getDarkVibrantSwatch();

- Palette.Swatch vibrant2 = palette.getMutedSwatch();

- Palette.Swatch vibrant3 = palette.getLightVibrantSwatch();

- Palette.Swatch vibrant4 = palette.getDarkMutedSwatch();

- Palette.Swatch vibrant5 = palette.getLightMutedSwatch();

- int rgb1 = -2;

- if (vibrant != null) {

- rgb1 = vibrant.getRgb();

- } else if (vibrant1 != null) {

- rgb1 = vibrant1.getRgb();

- } else if (vibrant2 != null) {

- rgb1 = vibrant2.getRgb();

- } else if (vibrant3 != null) {

- rgb1 = vibrant3.getRgb();

- } else if (vibrant4 != null) {

- rgb1 = vibrant4.getRgb();

- } else if (vibrant5 != null) {

- rgb1 = vibrant5.getRgb();

- }

- Log.e("RectImageView ", "onTouch: rgb " + String.valueOf(rgb1));

- String rgb2;

- if (rgb1 == -2) {

- rgb2 = "Click area identification exception";

- Toast.makeText(getContext(), rgb2, Toast.LENGTH_SHORT).show();

- } else {

- int red2 = (rgb1 & 0xff0000) >> 16;

- int green2 = (rgb1 & 0x00ff00) >> 8;

- int blue2 = (rgb1 & 0x0000ff);

- rgb2 = "选中区域RGB： " + red2 + " " + green2 + " " + blue2;

- showToast(getFromR(red2));

- }

- //                    int pixel = mPic.getPixel((int) event.getX(), (int) event.getY());

- //                    Log.d(TAG, "pixel " + pixel);

- //                    int red = (pixel & 0xff0000) >> 16;

- //                    int green = (pixel & 0x00ff00) >> 8;

- //                    int blue = (pixel & 0x0000ff);

- //                    String rgb = red + " " + green + " " + blue;

- //                    Log.d(TAG, rgb);

- invalidate();

- return true;

- }

- } else {

- return false;

- }

- } catch (Exception e) {

- Log.e(TAG, "onTouchEvent: ", e);

- }

- return false;

- }

- private String getFromR(int b) {

- String a = "-1";

- if (b <= 140 && b >= 0) {

- a = "Safe";

- }else if (b <= 160 && b > 140) {

- a = "Danger";

- }else if (b <= 255 && b > 160) {

- a = "Extreme Danger";

- }

- if ( "-1".equals(a)) {

- return "The concentration is not within the national detection limit.";

- }

- return String.valueOf(a);

- }

- private void showToast(String message) {

- View view = LayoutInflater.from(getContext()).inflate(R.layout.toast_layout, null);

- TextView textView = view.findViewById(R.id.toast_text);

- textView.setText(message);

- if ("Safe".equals(message)) {

- textView.setTextColor(Color.GREEN);

- } else if ("Danger".equals(message)) {

- textView.setTextColor(Color.YELLOW);

- }else if ("Extreme Danger".equals(message)) {

- textView.setTextColor(Color.RED);

- }

- Toast toast = new Toast(getContext());

- toast.setView(view);

- toast.setDuration(Toast.LENGTH_SHORT);

- toast.setGravity(Gravity.CENTER,0,500);

- toast.show();

- }

- }

- Supplementary References

[1] X. Ma, X. Lin, X. Xu, Z. Wang, Fabrication of gold/silver nanodimer SERS probes for the simultaneous detection of Salmonella typhimurium and Staphylococcus aureus, Microchimica Acta 188(6) (2021) 202.

[2] M. Chen, L. Pan, K. Tu, A fluorescence biosensor for Salmonella typhimurium detection in food based on the nano-self-assembly of alendronic acid modified upconversion and gold nanoparticles, Anal Methods 13(21) (2021) 2415-2423.

[3] L. Wang, X. Huo, W. Qi, Z. Xia, Y. Li, J. Lin, Rapid and sensitive detection of Salmonella Typhimurium using nickel nanowire bridge for electrochemical impedance amplification, Talanta 211 (2020) 120715.

[4] W. Wu, J. Li, D. Pan, J. Li, S. Song, M. Rong, Z. Li, J. Gao, J. Lu, Gold nanoparticle-based enzyme-linked antibody-aptamer sandwich assay for detection of Salmonella Typhimurium, ACS Appl Mater Interfaces 6(19) (2014) 16974-81.

[5] Q. Chen, R. Gao, L. Jia, Enhancement of the peroxidase-like activity of aptamers modified gold nanoclusters by bacteria for colorimetric detection of Salmonella typhimurium, Talanta 221 (2021) 121476.

[6] S. Chen, X. Zong, J. Zheng, J. Zhang, M. Zhou, Q. Chen, C. Man, Y. Jiang, A Colorimetric Strategy Based on Aptamer-Catalyzed Hairpin Assembly for the On-Site Detection of Salmonella typhimurium in Milk, Foods 10(11) (2021) 2539.