Development of mechanical strengthened, UV-shielding and antibacterial hydroxyethyl cellulose-based composite films

Development of mechanical strengthened, UV-shielding and antibacterial hydroxyethyl cellulose-based composite films

Xueqin Zhang · Haoqi Guo · Wenhan Luo · Guojian Chen · Naiyu Xiao · Gengsheng Xiao · Chuanfu Liu

X. Zhang · H. Guo · W. Luo · G. Chen · N. Xiao () · G. Xiao ()

College of Light Industry and Food Technology, Zhongkai University of Agriculture and Engineering, Guangzhou 510225, China

Email: xiaony@163.com (N. Xiao); Gshxiao@aliyun.com (G. Xiao)

X. Zhang · W. Luo · G. Chen · N. Xiao · G. Xiao

Academy of Contemporary Agricultural Engineering Innovations, Zhongkai University of Agriculture and Engineering, Guangzhou 510225, China

X. Zhang · W. Luo · G. Chen · N. Xiao · G. Xiao

Guangdong Key Laboratory of Science and Technology of Lingnan Specialty Food, Zhongkai University of Agriculture and Engineering, Guangzhou 510225, China

X. Zhang · C. Liu ()

State Key Laboratory of Pulp and Paper Engineering, South China University of Technology, Guangzhou 510640, China

Email: chfliu@scut.edu.cn (C. Liu)

Table S1 The contents of PVA, ECH and ε-PL in the composite films, and the percentage of blocking from UV-A and UV-B, and UPF values of the composite films.

| Film | PVA (%) | ECH (%) | ε-PL (%) | T600 (%) | Percentage blocking |  | UPF value |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | UV-A | UV-B |  |
| H10P30L10E | 10 | 10 | 30 | 11.38 | 93.80 | 99.66 | 15.29 |
| H20P30L10E | 20 | 10 | 30 | 10.30 | 94.56 | 99.74 | 17.54 |
| H30P30L10E | 30 | 10 | 30 | 15.92 | 93.37 | 99.24 | 13.53 |
| H40P30L10E | 40 | 10 | 30 | 8.54 | 95.94 | 99.82 | 23.58 |
| H50P30L10E | 50 | 10 | 30 | 13.31 | 93.31 | 99.27 | 13.48 |
| H30P30L2.5E | 30 | 2.5 | 30 | 5.98 | 97.38 | 99.99 | 38.02 |
| H30P30L5E | 30 | 5 | 30 | 4.31 | 98.35 | 99.99 | 60.25 |
| H30P30L7.5E | 30 | 7.5 | 30 | 12.01 | 94.21 | 99.78 | 16.64 |
| H30P30L12.5E | 30 | 12.5 | 30 | 6.64 | 97.58 | 99.99 | 41.52 |
| H30P10L10E | 30 | 10 | 10 | 4.74 | 97.65 | 99.48 | 34.60 |
| H30P20L10E | 30 | 10 | 20 | 6.63 | 97.65 | 99.68 | 26.32 |
| H30P40L10E | 30 | 10 | 40 | 12.06 | 93.11 | 99.75 | 14.01 |
| H30P50L10E | 30 | 10 | 50 | 15.92 | 92.49 | 99.73 | 12.85 |

Table S2 Thermal characteristics of TGA/DTG studies for pure HEC film and the composite films reinforced with different content of PVA.

| Film | Moisture (%) | Tonset (℃) | T50% (℃) | Residue at 600 ℃ (%) | Tmax1 (℃) | Tmax2 (℃) |
| --- | --- | --- | --- | --- | --- | --- |
| H10P30L10E | 16.73 | 247.94 | 292.30 | 26.02 | 273.24 | 393.68 |
| H30P30L10E | 16.39 | 251.22 | 305.12 | 23.51 | 285.73 | 401.73 |
| H50P30L10E | 14.59 | 241.53 | 292.30 | 22.44 | 263.54 | 396.79 |
| Pure HEC film | 12.04 | 232.01 | 274.72 | 35.70 | 255.49 | -- |