Table 2. Oxidation reaction of various alcohols catalyzed by B-V-PIL/W a

| Entry | Substrate | Product | Time (min) | Yield (%)b |
| --- | --- | --- | --- | --- |
| 1 |  |  | 70 | 95 |
| 2 |  |  | 45 | 97 |
| 3 |  |  | 60 | 90 |
| 4 |  |  | 60 | 90 |
| 5 |  |  | 60 | 92 |
| 6 |  |  | 90 | 90 |
| 7 |  |  | 90 | 90 |
| 8 |  |  | 120 | 89 |
| 9 |  |  | 150 | 80 |
| 10 |  |  | 150 | 75 |
| 11 |  |  | 150 | 75 |
| 12 |  |  | 130 | 78 |
| 13 |  |  | 120 | 78 |
| 14 |  |  | 150 | 75 |
| 15 |  |  | 150 | 75 |

aReaction condition:  alcohol (1 mmol), H2O2 30% (1 mmol), malononitrile (1.2 mmol), B-V-PIL/W 40 mg in H2O/EtOH (2/1) at 70 °C, b Isolated yield.

Table 3. One-pot tandem oxidation /Knoevenagel condensation of alcohols with malononitrile catalyzed by B-V-PIL/Wa

| Entry | Substrate | Product | Time (min) | Yield (%)b |
| --- | --- | --- | --- | --- |
| 1 |  |  | 90 | 94 |
| 2 |  |  | 65 | 97 |
| 3 |  |  | 65 | 98 |
| 4 |  |  | 65 | 90 |
| 5 |  |  | 90 | 92 |
| 6 |  |  | 90 | 92 |
| 7 |  |  | 90 | 92 |
| 8 |  |  | 120 | 90 |
| 9 |  |  | 120 | 90 |
| 10 |  |  | 180 | 80 |
| 11 |  |  | 185 | 80 |
| 12 |  |  | 185 | 80 |
| 13 |  |  | 180 | 80 |
| 14 |  |  | 160 | 83 |
| 15 |  |  | 150 | 85 |
| 16 |  |  | 180 | 80 |
| 17 |  |  | 180 | 80 |

aReaction condition:  alcohol (1 mmol), H2O2 30% (1 mmol), B-V-PIL/W 40 mg in H2O/EtOH (2/1) at 70 °C, b Isolated yield.