Supplementary Material

Influence of the surface modification of granular activated carbon sintetized from macauba on heavy metals sorption

Regiane D. F. Rios,1 Patrícia J. B. Bueno, 1 Júlio C. S. Terra, 2 and

Flávia C. C. Moura,* 1

1Departamento de Química, ICEx, Universidade Federal de Minas Gerais, Av. Antônio Carlos, 6627. Belo Horizonte – MG -31270-901– Brazil.

2Centre for Green Chemistry and Catalysis, Department of Chemistry, McGill University, 801 Sherbrooke Street West, Montreal, QC, H3A 0B8, Canada.

*flaviamoura@ufmg.br

Table S1. Langmuir and Freundlich constants and correlation coefficients of the functionalized materials in adsorption of heavy metals.

|  | Langmuir |  |  | Freundlich |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | qmax (mg g-1) | B (L mg-1) | R2 | n | Kf (L mg-1) | R2 |
|  | Zn2+ |  |  |  |  |  |
| GAC | 5.26 | -0.027 | 0.943 | 1.769 | 0.253 | 0.897 |
| GAC-R60 | 14.09 | 0.462 | 0.996 | 3.049 | 3.767 | 0.914 |
| GAC-R180 | 58.82 | 0.083 | 0.999 | 2.066 | 4.764 | 0.900 |
| GAC/N | 344.83 | 0.116 | 0.996 | 3.702 | 68.502 | 0.922 |
| GAC-R180/N | 476.19 | 0.174 | 0.998 | 3.556 | 43.581 | 0.398 |
| GAC-CVD-ACN | 357.14 | 0.156 | 0.996 | 1.499 | 12.252 | 0.854 |
|  | Cd2+ |  |  |  |  |  |
| GAC | 30.30 | 0.000 | 0.020 | 1.022 | 0.009 | 0.972 |
| GAC-R60 | 14.92 | 4.188 | 0.999 | 2.809 | 3.767 | 0.658 |
| GAC-R180 | 83.33 | 0.194 | 0.998 | 2.309 | 10.023 | 0.808 |
| GAC/N | 625.00 | 0.009 | 0.9729 | 0.592 | 0.038 | 0.918 |
| GAC-R180/N | 769.23 | 0.028 | 0.9818 | 0.947 | 0.916 | 0.719 |
| GAC-CVD/ACN | 1428.57 | 0.001 | 0.2943 | 1.255 | 3.903 | 0.971 |
|  | Pb2+ |  |  |  |  |  |
| GAC | 6.423 | 0.030 | 0.945 | 1.880 | 0.398 | 0.657 |
| GAC-R60 | 200.00 | 0.019 | 0.911 | 1.200 | 6.223 | 0.994 |
| GAC-R180 | 500.00 | 0.004 | 0.184 | 1.072 | 3.228 | 0.982 |
| GAC/N | 27.47 | 0.023 | 0.937 | 1.937 | 1.242 | 0.585 |
| GAC-R180/N | 322.58 | 0.087 | 0.999 | 1.109 | 3.193 | 0.881 |
| GAC-CVD/ACN | 77.519 | 0.007 | 0.736 | 1.298 | 0.663 | 0.933 |

Table S2. Kinetic model parameters of Zn2+, Cd2+ and Pb2+ removal by different materials.

|  | Zn2+ |  |  |  |  | Cd2+ |  |  |  |  | Pb2+ |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Adsorbent | Pseudo-first-order |  | Pseudo-second-order |  |  | Pseudo-first-order |  | Pseudo-second-order |  |  | Pseudo-first-order |  | Pseudo-second-order |  |
| GAC | K1 | 0.0010 | K2 | -0.00512 |  | K1 | -0.0007 | K2 | -0.00540 |  | K1 | -0.00037 | K2 | -0.00083 |
|  | R2 | 0.05401 | R2 | 0.98829 |  | R2 | 0.01016 | R2 | 0.92256 |  | R2 | 0.13990 | R2 | 0.96847 |
| GAC-R60 | K1 | 0.00177 | K2 | 0.00040 |  | K1 | 0.00472 | K2 | 0.00023 |  | K1 | 0.00460 | K2 | 0.00008 |
|  | R2 | 0.81520 | R2 | 0.99439 |  | R2 | 0.87489 | R2 | 0.99847 |  | R2 | 0.87660 | R2 | 0.99624 |
| GAC-R180 | K1 | 0.00175 | K2 | 0.00056 |  | K1 | 0.00242 | K2 | 0.41926 |  | K1 | 0.00266 | K2 | 0.00005 |
|  | R2 | 0.49249 | R2 | 0.99570 |  | R2 | 0.41926 | R2 | 0.99359 |  | R2 | 0.72104 | R2 | 0.98493 |
| GAC/N | K1 | 0.00293 | K2 | 0.63191 |  | K1 | 0.00895 | K2 | 0.52970 |  | K1 | 0.00066 | K2 | 0.11640 |
|  | R2 | 0.00004 | R2 | 0.99352 |  | R2 | 0.00008 | R2 | 0.99617 |  | R2 | 0.00535 | R2 | 0.99465 |
| GAC-CVD/ACN | K1 | 0.03383 | K2 | 0.97626 |  | K1 | 0.00129 | K2 | 0.26659 |  | K1 | 0.00586 | K2 | 0.52007 |
|  | R2 | 0.00004 | R2 | 0.99481 |  | R2 | 0.00015 | R2 | 0.98958 |  | R2 | 0.00020 | R2 | 0.98743 |
| GAC-R180/N | K1 | 0.01147 | K2 | 0.89955 |  | K1 | 0.00242 | K2 | 0.41926 |  | K1 | 0.00968 | K2 | 0.78736 |
|  | R2 | 0.00002 | R2 | 0.99168 |  | R2 | 0.00022 | R2 | 0.99359 |  | R2 | 0.00003 | R2 | 0.98343 |

Figure S1. Reusability of functionalized activated carbons GAC-R60 (Blue), GAC-R180 (Red), GAC/N (Pink), GAC-CVD/ACN (Green) and GAC-R180/N (Dark blue) for adsorption of heavy metals (a) Zn2+ (b) Cd2+ and (c) Pb2+ at room temperature and pH 5.5.