Supplementary Information (SI)

Three-dimensional Network of Nitrogen-doped Carbon Matrix-encapsulated Si Nanoparticles/Carbon Nanofibers Hybrids for Lithium Ion Battery Anodes with Excellent Capability

Ruye Conga, Minsang Job, Angelica Martinoa, Hyun-Ho Parka, Hochun Leeb,

Chang-Seop Leea,*

aDepartment of Chemistry, Keimyung University, Daegu 42601, Korea

bDepartment of Energy Science and Engineering, DGIST, Daegu 42988, Korea

*Corresponding author: Chang-Seop Lee

Department of Chemistry, Keimyung University, Daegu 42601, Korea

Phone No: +82-53-580-5192; Fax No: +82-53-580-5056

E-mail: surfkm@kmu.ac.kr

Fig. S1. Proposed process for preparing the catalysts and synthesis of carbon nanofibers (CNFs).

Fig. S2. Schematic diagram of the chemical reaction process of the melamine formaldehyde resin (MFR) formed by the polymerization of formaldehyde and melamine.

Fig. S3. Representative Si 2p XPS spectra of (a) Si-OH, (b) Si-NH2, (c) GO/MFR@Si/CNF, and (d) NG/C@Si/CNF.

Fig. S4. (a) Cyclic voltammetry curves of the G@Si/CNF composite electrode in the initial five cycles. (b) The charge and discharge profiles of G@Si/CNF composite electrode. (c) The cycling performances of the synthesized G@Si/CNF composite electrode at a current density of 0.1 A·g−1.

Fig. S5. (a) Cyclic voltammetry curves of the NG/C@Si composite electrode in the initial five cycles. (b) The charge and discharge profiles of NG/C@Si composite electrode. (c) The cycling performances of the synthesized NG/C@Si composite electrode at a current density of 0.1 A·g−1.

Fig. S6. Representative SEM images from cross section view of the NG/C@Si/CNF, G@Si/CNF, and NG/C@Si electrodes (a, b, c) before the first cycle and (d, e, f) after 100 lithiation/delithiation cycles at a current density of 0.1 Ag−1.

Table S1. Raman spectroscopy results for the GO, rGO, CNFs, NG/C@Si/CNF, G@Si/CNF, and NG/C@Si samples (see Fig. 5b).

| Sample | ID/IG |
| --- | --- |
| GO | 1.05 |
| rGO | 0.99 |
| CNF | 0.99 |
| G@Si/CNF | 1.01 |
| NG/C@Si | 1.03 |
| NG/C@Si/CNF | 1.02 |

Table S2. Discharge capacity, Coulomb efficiency, and capacity retention rate of the NG/C@Si/CNF, G@Si/CNF, and NG/C@Si composite electrodes.

| Samples | Max. discharge capacity (mAh/g) | Discharge capacity (mAh/g) |  | Coulomb efficiency (%) |  | Capacity retention rate (%) |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | After 50 cycle | After 100 cycle | first cycle | 100 cycle | After 50 cycle | After 100 cycle |
| NG/C@Si/CNF | 2464.8 | 1388.4 | 1371.4 | 59.9 | 98.4 | 56.3 | 55.6 |
| G@Si/CNF | 2381.6 | 1027.8 | 1010.3 | 54.6 | 98.5 | 47.6 | 46.9 |
| NG/C@Si | 1768.6 | 894.7 | 868.3 | 48.1 | 97.8 | 50.5 | 49.1 |