Table 1 Composition and relative amount of elements in the vulcanized natural rubber sheets after treatment with Trichaptum abietinum and Trichaptum biforme for 3 months

Elements (% in weight)

Solid     Crystal form        C     O    Al    Si    S    K    Ca    Fe   Zn

A       Tetrahedron       35.6   42.1          0.6      21.3      0.5

B         Needle         30.2   52.6          0.2      17.0

C       Tetrahedron       29.3   57.2                 13.5

D         Needle         57.9   36.7       0.1   0.7      4.0      0.4

The data were obtained via scanning electron microscopy-energy dispersive X-ray spectroscopy analysis.

Table 2 Weight loss and physical characteristics of the vulcanized natural rubber sheets with and without fungal treatment for 3 months

Treatment          Weight loss         Hardness        Strength at breakage point

(%)           (relative value)              (MPa)

Control               0                67.3                   3.6

T. abietinum         3.00.6             74.5                   2.6

T. biforme           5.00.3             75.0                   2.6

Control refers to the treatment without fungi.

Table 3 Comparison of the relative proportions of three main components, volatile carbon, non-volatile carbon and ash in the vulcanized rubber sheets before and after fungal treatment.

Treatment        Period                        Proportions (% in weight)

(Month)          Volatile carbon    Non-volatile carbon    Ash

Control            0                 39.8              33.5            26.7

1                 40.3              33.0            26.7

T. abietinum        2                 40.1              33.0            26.9

3                 40.9              32.9            26.2

1                 41.1              32.9            26.0

T. biforme          2                 41.0              33.0            26.0

3                 44.7              31.7            23.6

The data were determined via thermogravimetric analysis. Control refers to the treatment without fungi.