Supplementary Information

Van der Waals interactions regulating the hydration of 2-methacryloyloxyethyl phosphorylcholine, the constructing monomer of biocompatible polymers

Masae Takahashi, Sifan Chen, Hiroshi Matsui, Nobuyuki Morimoto and Yuka Ikemoto

Contents

Table S1. Relative energies of 48 MPC conformers (in kcal/mol) calculated with different dielectric constant ()

Fig. S1. Number representing the 81 conformations, ABCD, of MPC.

Fig. S2. FIR spectra of conformers 1−6 in Fig.7 of the main text, calculated in a solvent with a dielectric constant  = 15.20 at the b3LYP/6-311++G(d,p) level with dispersion correction. The FWHM of the calculated spectra is set to the same value as that of the well-separated sharp peak observed at 423 cm−1 at 4 K in Fig. 2a of the main text (FWHM = 4.4 cm−1).

Table S1. Relative energies of 48 MPC conformers (in kcal/mol) calculated with different dielectric constant ()a

| conformersb | Solvent-free |  = 8.33 |  = 15.20 |
| --- | --- | --- | --- |
| 131Y (1) | 0.00 | 0.00 | 0.00 |
| 3112 (6) | 2.45 | 0.92 | 0.91 |
| 133X | 2.56 | 1.13 | − |
| 1332 (5) | 3.26 | 0.99 | 0.85 |
| 3X33 (4) | 3.62 | 0.96 | 0.73 |
| 1Y11 (2) | 4.26 | 0.99 | 0.64 |
| 1311 | 4.57 | 3.59 | 3.33 |
| 3311 | 4.60 | 2.78 | 2.49 |
| 3121 | 4.88 | 3.82 | 3.72 |
| 3131 (3) | 5.35 | 1.30 | 0.65 |
| 2311 | 5.37 | 4.20 | − |
| 1133 | 5.44 | 3.88 | 3.59 |
| 3323 | 5.71 | 4.30 | 4.23 |
| 1X32 | 6.35 | 4.32 | 4.14 |
| 1333 | 6.62 | 2.61 | 2.35 |
| 1212 | 6.65 | 3.47 | 3.17 |
| 1111 | 6.73 | 4.41 | 4.23 |
| 3313 | 6.73 | 4.14 | 3.54 |
| 3X32 | 6.74 | 2.77 | 2.31 |
| 2132 | 6.77 | 4.32 | − |
| 113X | 6.80 | 3.78 | 3.23 |
| 2312c | 6.98 | 5.00 | 4.24d |
| 3133 | 7.08 | − | 5.68 |
| Y111 | 7.11 | 3.87 | 3.57 |
| 2X32 | 7.23 | 4.71 | 4.51 |
| 1323 | 7.44 | 4.62 | 4.47 |
| 1112 | 7.49 | 4.62 | 4.33 |
| 2312c | 7.56 | − | 4.24d |
| 1131 | 7.56 | 5.12 | 4.61 |
| 2313 | 7.60 | 5.53 | − |
| 1322 | 7.66 | 5.16 | 5.05 |
| 1123 | 7.75 | 5.58 | 5.46 |
| 2333 | 7.83 | − | − |
| 1321 | 8.10 | 5.61 | 5.37 |
| 1121 | 8.12 | 5.84 | 3.59 |
| 3333 | 8.15 | 4.93 | 4.55 |
| 1122 | 8.26 | 5.76 | 5.54 |
| 1223 | 8.46 | − | 5.53 |
| 3332 | 8.59 | 5.04 | 4.56 |
| 1222 | 8.70 | − | − |
| 3321 | 9.03 | 5.96 | 5.65 |
| 3123 | 9.04 | − | − |
| 3232 | 9.06 | − | − |
| 1221 | 9.18 | 6.14 | 5.82 |
| 3322 | 9.24 | 6.08 | 5.69 |
| 3221 | 9.41 | 3.76 | − |
| 3222 | 9.80 | 6.16 | 5.72 |
| 3223 | 9.90 | 6.25 | 5.78 |

aResults at the B3KYP/6-311++G(d,p) level with dispersion correction. bSee Fig. S1 for conformational numbering. X and Y mean between 1 and 2, 2 and 3, respectively. The numbers in bold in parentheses are the molecule numbers in Fig. 7 of the main text. cTwo 2312 conformations with slight differences in the C(=O)C(CH2)CH3 moiety. dConformation is 3X12.

R1 = OCH2CH2N+(CH3)3, R2 = C(=O)C(CH2)CH3

Fig S1. Number representing the 81 conformations, ABCD, of MPC.

Fig. S2. FIR spectra of conformers 1−6 in Fig.7 of the main text, calculated in a solvent with a dielectric constant  = 15.20 at the b3LYP/6-311++G(d,p) level with dispersion correction. The FWHM of the calculated spectra is set to the same value as that of the well-separated sharp peak observed at 423 cm−1 at 4 K in Fig. 2a of the main text (FWHM = 4.4 cm−1).