Supplementary Information

Multiplexed DNA-functionalized graphene sensor with artificial intelligence discrimination performance of chemical vapor composition

Gilho Lee‡, Heejin Yu‡, Yun Ji Hwang‡, Jin Seong, Youngmo Jung, Jongeun Choi*, and Seong Chan Jun*

G. Lee, H. Yu, Y. J. Hwang, J. Seong, Y. Jung, J. Choi, S. C. Jun

School of Mechanical Engineering, Yonsei University, 50, Yonsei-ro, Seodaemun-gu, Seoul 03722, Republic of Korea

‡ These authors contributed equally.

*Corresponding author

Seong Chan Jun

Tel: +82-2-2123-5817; E-mail: scj@yonsei.ac.kr

Jongeun Choi

Tel: +82-2-2123-2813; E-mail: jongeunchoi@yonsei.ac.kr

Figure S1. Changes in Raman spectra of monolayer graphene before and after annealing.

Figure S2. TOF-SIMS image and peak of sensing channel in A6 DNA sequence.

Figure S3. TOF-SIMS image and peak of sensing channel in T6 DNA sequence.

Figure S4. TOF-SIMS image and peak of sensing channel in G6 DNA sequence.

Figure S5. TOF-SIMS image and peak of sensing channel in A6T6 DNA sequence.

Figure S6. TOF-SIMS image and peak of sensing channel in A6G6 DNA sequence.

Figure S7. TOF-SIMS image and peak of sensing channel in T6G6 DNA sequence.

Figure S8. Response of NH3 individual gas under low-humidity condition.

Figure S9. Response of NO2 individual gas under low-humidity condition.

Figure S10. Response of individual NO gas under low-humidity condition.

Figure S11. Response of NH3–NO2 mixed gases under low-humidity condition.

Figure S12. Response of NH3–NO mixed gases under low-humidity condition.

Figure S13. Response of NO2–NO mixed gases under low-humidity condition.

Figure S14. Response of NH3–H2S mixed gases under high-humidity condition.

Figure S15. Feature selection analysis using Boruta algorithm.

Table S1. Individual and mixture gases used for measurement.

|  | Individual gas |  |  |  | Mixture gas |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Species | NO2 | NO | NH3 | Species | NO2/NO | NO2/NH3 | NO/NH3 |
| Concentration [ppm] | 2, 5, 10 |  |  | Mixing Ratio | 5:5, 2.5:7.5, 7.5:2.5 |  |  |

Table S2. Feature description

| Feature | Description | Number of features |
| --- | --- | --- |
| Magnitude | Down-sampled values of the magnitude The maximum or minimum magnitude Down-sampled values of the normalized magnitude | 31 1 31 |
| Derivative | Down-sampled values of derivative D The maximum and minimum derivatives The maximum and minimum second derivative during both injection and purging stages | 31 2 4 |
| Difference | The difference (D) in magnitude | 5 |
| Time constant | The time when the reaction reaches 30%, 60%, 90%, and 100% of its maximum or minimum value (and 90%, 60%, and 30% of its maximum or minimum value during the purging stage) | 7 |
| Area | The area under the eight intervals of the curve, where the interval is divided by the time constant features | 8 |

Table S3. Accuracy of classification model with low humidity condition.

| Low Humidity Condition |  | Accuracy [%] |  |
| --- | --- | --- | --- |
| Chemical Vapor Composition | Mixing ratio | With feature selection | With 1D CNN |
| NH3–NO2 | 1:1 | 96 | 100 |
|  | 1:3 | 100 | 100 |
|  | 3:1 | 100 | 100 |
| NH3–NO | 1:1 | 100 | 100 |
|  | 1:3 | 100 | 100 |
|  | 3:1 | 100 | 100 |
| NO2–NO | 1:1 | 100 | 100 |
|  | 1:3 | 99.5 | 100 |
|  | 3:1 | 100 | 100 |

Table S4. Performance of classification model with low humidity condition.

|  | With feature selection |  |  |  | Using all features |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Chemical Vapor Composition | Precision [%] | Recall [%] | F1 score [%] | Compression ratio | Precision [%] | Recall [%] | F1 score [%] | Compression ratio |
| NO2–NH3 | 98.67 | 98.67 | 98.69 | 7.01 | 98.14 | 98.08 | 98.11 | 1 |
| NO–NH3 | 100 | 100 | 100 | 4.62 | 100 | 100 | 100 | 1 |
| NO–NO2 | 99.33 | 99.83 | 99.85 | 6.02 | 99.48 | 99.47 | 99.47 | 1 |

Table S5. Accuracy of classification model with high humidity condition.

| High Humidity Condition |  | Accuracy [%] |  |
| --- | --- | --- | --- |
| Chemical Vapor Composition | Mixing ratio | With feature selection | With 1D CNN |
| NH3–H2S | NH3 | 85 | 100 |
|  | H2S | 96.5 | 100 |
|  | 1:1 | 100 | 100 |
|  | 1:3 | 100 | 100 |
|  | 3:1 | 100 | 100 |
| NH3–NO | NH3 | 100 | 100 |
|  | NO | 99.83 | 100 |
|  | 1:1 | 100 | 100 |
|  | 1:3 | 100 | 100 |
|  | 3:1 | 96.83 | 100 |
| H2S–NO | H2S | 100 | 100 |
|  | NO | 99 | 100 |
|  | 1:1 | 100 | 100 |
|  | 1:3 | 100 | 100 |
|  | 3:1 | 100 | 100 |

Table S6. Performance of classification model with high humidity condition.

|  | Classification Accuracy [%] |  |
| --- | --- | --- |
| Chemical Vapor Composition | With feature selection | Using all features |
| NH3–H2S | 100 | 100 |
| NH3–NO | 98.94 | 97.23 |
| H2S–NO | 100 | 100 |