[image: ]Table 1. Deconvolution data of the neat CA membrane and the CA/lactic acid membranes at 0 and 8 bar (C=O)

Table 2. Deconvolution data of the pristine and the CA/lactic acid composites
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Peak (cm™) Neat CA CAl/lactic acid at 0 bar  CA/lactic acid at 8 bar

~1735-1737 79.19 86.82 78.95

~1754-1755 20.81 13.18 21.05
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Peak (cm™) Neat CA CA/lactic acid at 0 bar  CA/lactic acid at 8 bar

~1037-1038 81.54 79.24 81.68

~1072-1073 18.46 20.76 18.31





