Supplementary Material

Ce3+-induced fluorescence amplification of cooper nanoclusters based on aggregation-induced emission for specific sensing 2,6-pyridine dicarboxylic acid

Jingxiang Shen1,2, Zhefeng Fan1*

- School of Chemistry and Material Science, Shanxi Normal University, Taiyuan, 030006, People’s Republic of China

- Department of Chemistry, Changzhi University, Changzhi, 046011, People’s Republic of China

*Corresponding author: E-mail: zhefengfan@126.com

Instruments

Fig.S1 Comparison of fluorescence emission spectrum with Ce3+, Ce3+/GSH, GSH-CuNCs and Ce3+/GSH-CuNCs.

Fig.S2 Change of fluorescence intensity along with incubitation time.

Fig.S3 Effect of reaction time between DPA and Ce3+/GSH-CuNCs

Fig.S4 UV absorption spectrum of Ce3+, DPA and Ce3+-DPA complexes at pH=5.0 in HAc-NaAc buffer.

Table S1 Quantum yield calculation of GSH-CuNCs and Ce3+/GSH-CuNCs

Table S2 Comparison of our method with previously reported methods for sensing DPA

Experimental instruments

Fluorescent intensity were carried out by LS-55 fluorescence/phosphor spectrophotometer (Perkin-Elmer Company, USA). UV-vis absorbance measurements were performed by TU-1901 UV/Visible spectrophotometer (Beijing Purkinje General Instrument Co., Ltd, China). X-ray photoelectron spectroscopy (XPS) were measured using Thermo EscalAB 250Xi (Thermoelectric Corporation, USA). Fourier transform infrared (FTIR) spectra were obtained by Niocolet 380 spectrograph (Var-ian Instrument Co., Ltd, USA). Dynamic light scattering (DLS) and zeta potential were recorded by 90Plus PALS (NanoBrook, USA).

Fig. S1. Comparison of fluorescence emission spectrum with Ce3+, Ce3+/GSH, GSH-CuNCs and Ce3+/GSH-CuNCs

Fig. S2. Change of fluorescence intensity along with incubitation time

Fig. S3. Effect of reaction time between DPA and Ce3+/GSH-CuNCs

Fig. S4. UV absorption spectrum of Ce3+, DPA and Ce3+-DPA complexes at pH=5.0 in HAc-NaAc buffer.

Table S1. Quantum yield calculation of GSH-CuNCs and Ce3+/GSH-CuNCs

| Samples | Integrated area (F) | Absorbance (A) | Refractive index of solvent (η) | QY(Ø) |
| --- | --- | --- | --- | --- |
| Quinine sulfate | 76234.8 | 0.011 | 1 | 54% |
| GSH-CuNCs | 50.62 | 0.019 | 1 | 0.02% |
| Ce3+/GSH-CuNCs | 5436.1 | 0.025 | 1 | 1.7% |

Table S2. Comparison of our method with previously reported methods for sensing DPA

| Sensor materials | Linear range | LOD | refs |
| --- | --- | --- | --- |
| β-diketonate coordinated Eu(III)-complexes | 0–6 μM | 1.2μM | [1] |
| Cd6 Eu2 nanocluster | 30-60 μM | 8.7 μM | [2] |
| ZIF-8@AuNCs-Tb | 40-200 μM 200-100 μM | 1.8 μM | [3] |
| Cadmium sulfide quantum dots (CdSQDs) | 1-120 μM | 0.2 μM | [4] |
| Nanoscaled bimetallic lanthanoid MOF | 20-100 μM | 0.17 μM | [5] |
| Ce3+/GSH-CuNCs ensemble probe | 0.3-18 μM | 0.19 μM | This work |

1.	Abbas Z, Patra AK (2022) Luminescent β-diketonate coordinated europium(III) sensor for rapid and sensitive detection of Bacillus Anthracis biomarker. J Lumin 244:118726. https:// doi.org/10.1016/j.jlumin.2022.118726.

2.	Leng X, Shi D, Yang X, Zhang Z, Li H, Cheng Y, Ma Y, Schipper D (2022) Construction of a luminescent square-like Cd6Eu2 nanocluster for the quantitative detection of 2,6-dipicolinic acid as an anthrax biomarker. J Mater Chem C 10:510-516. https:// doi.org/10.1039/d1tc05929g.

3.	Shao K, Wen S, Zhang M, Wang J, Ye S, Pan Z(2021) A ratiometric fluorescent nanoprobe based on ZIF-8@AuNCs–Tb for visual detection of 2,6-pyridinedicarboxylic acid. J Rare Earths https:// doi.org/10.1016/j.jre.2021.08.005.

4.	Li X, Deng L, Ma F, Yang M (2020) A luminous off-on probe for the determination of 2,6-pyridinedicarboxylic acid as an anthrax biomarker based on water-soluble cadmium sulfide quantum dots. Microchim acta 187:287. https:// doi.org/10.1007/s00604-020-04272-0.

5.	Othong J, Boonmak J, Kielar F, Hadsadee S, Jungsuttiwong S, Youngme S (2020). Self-calibrating sensor with logic gate operation for anthrax biomarker based on nanoscaled bimetallic lanthanoid MOF. Sens Actuators B Chem 316:128156. https://doi.org/10.1016/ j.snb.2020.128156.