Supplementary Information†

Depicting polymorphism in eutectic mixtures

Pawanpreet Singh$*, Renu Chadhaф

$ Department of Food Science and Technology, I.K. Gujral Punjab Technical University, Kapurthala, Punjab, India.

ф University Institute of Pharmaceutical Sciences, Panjab University, Chandigarh-160014, India.

E-mail: pawanpreet.fst@ptu.ac.in

Phone: +919888646036

Figure S1 FTIR spectra of LZ form IV and heat treated eutectic polymorphs of linezolid after solubility study.

The FTIR spectra of LZ form IV and heat treated eutectic polymorphs after solubility study showed the complete transformation of LZ form IV into form II. Characteristic absorption peaks of LZ form II and respective coformers are present in case of all heat treated eutectic polymorphs of LZ.

Table S1: FTIR absorption frequencies (cm-1) of LZ form II, form IV, eutectic polymorphs and coformers used.

| Absorption bands | form II of LZ | form IV of LZ | LS(A) | LS(B) | LF(A) | LF(B) | LN(A) | LN(B) | SY | FA | INC |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Amide N-H stretch | 3363 (2o amide) | 3339 (2o amide) | 3363 | 3339 | 3362 | 3338 | N-H (sym) merged with 3363 N-H (asym) 3190 | N-H (sym) a peak shoulder at 3372 N-H (asym) 3188 | - | - | N-H (asym) 3370 N-H (sym) 3188 |
| Lactone C=O stretch | 1747 | 1742 | 1747 | 1742 | 1745 | 1741 | 1747 | 1742 | - | - | - |
| Amide C=O stretch | 1674 | 1662 | 1677 | 1663 | 1674 | 1664 | 1673 | 1665 | - | - | 1667 |
| Aliphatic C-H stretch | 2978 | 2967 | 2975 (broad) | 2970 | 2976 (broad) | 2969 (broad) | 2979 (broad) | 2973 (broad) | 2971 | 2996 | - |
| Acidic C=O stretch | - | - | 1697 | 1699 | Peak merge with Amide C=O stretch | Peak merge with Amide C=O stretch | - | - | 1699 | 1676 | - |
| Acidic O-H stretch | - | - | 3081 | 3080 | 3081 | 3081 | - | - | 3031 | 3082 | - |
| Phenolic O-H stretch | - | - | Peak merge with Amide N-H stretch | Peak merge with Amide N-H stretch | - | - | - | - | 3372 | - | - |

Table S2: 13C NMR chemical shifts (ppm) of LZ form II, form IV and different eutectic polymorphs. Doublet peaks are described as (d) in the parenthesis.

| Carbon number | formII/ IV of LZ | SY | FA | INC | LS(A) | LS(B) | LF(A) | LF(B) | LN(A) | LN(B) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C1 | 22.3 | - | - | - | 22.3 | 22.3 | 22.3 | 22.3 | 22.3 | 22.3 |
| C2 | 170.1 | - | - | - | 170.3 | 170.2 | 170.1 | 169.9 | 170.1 | 170.1 |
| C3 | 41.3 | - | - | - | 41.3 | 41.3 | 41.3 | 41.3 | 41.3 | 41.4 |
| C4 | 71.3 | - | - | - | 71.3 | 71.3 | 71.4 | 71.4 | 71.4 | 71.4 |
| C5 | 47.2 | - | - | - | 47.2 | 47.2 | 47.2 | 47.2 | 47.2 | 47.2 |
| C6 | 153.6 | - | - | - | 153.6 | 153.6 | 153.6 | 153.6 | 153.6 | 153.6 |
| C7 | 133.2 (d) | - | - | - | 133.2 (d) | 133.2 (d) | 133.3 (d) | 133.3 (d) | 133.3 (d) | 133.3 (d) |
| C8 | 106.6 (d) | - | - | - | 106.5 (d) | 106.5 (d) | 106.6 (d) | 106.6 (d) | 106.6 (d) | 106.6 (d) |
| C9 | 155.8 (d) | - | - | - | 155.8 (d) | 155.8 (d) | 155.7 (d) | 155.7 (d) | 155.8 (d) | 155.8 (d) |
| C10 | 135.4 (d) | - | - | - | 135.4 (d) | 135.4 (d) | 135.4 (d) | 135.4 (d) | 135.4 (d) | 135.4 (d) |
| C11 | 118.9 (d) | - | - | - | 118.7 (d) | 118.7 (d) | 118.9 (d) | 119.1 (d) | 118.8 (d) | 188.9 (d) |
| C12 | 113.5 (d) | - | - | - | 113.7 (d) | 113.6 (d) | 113.8 (d) | 113.9 (d) | 113.8 (d) | 113.8 (d) |
| C(13, 16) | 50.9 (d) | - | - | - | 50.5 (d) | 50.5 (d) | 50.6 (d) | 50.6 (d) | 50.6 (d) | 50.6 (d) |
| C(14, 15) | 66.1 | - | - | - | 66.1 | 66.1 | 66.1 | 66.1 | 66.1 | 66.1 |
| C(17,20) | - | - | 165.9 | - | - | - | 165.8 | 165.9 | - | - |
| C(18,19) | - | - | 133.8 | - | - | - | 133.8 | 133.9 | - | - |
| C21 | - | - | - | 166.4 | - | - | - | - | 166.3 | 166.3 |
| C22 | - | - | - | 141.2 | - | - | - | - | 141.1 | 141.1 |
| C(23,26) | - | - | - | 121.3 | - | - | - | - | 121.3 | 121.3 |
| C(24,25) | - | - | - | 150.1 | - | - | - | - | 149.9 | 149.9 |
| C27 | - | 140.1 | - | - | 140.0 | 140.0 | - | - | - | - |
| C(28,32) | - | 147.3 | - | - | 147.2 | 147.2 | - | - | - | - |
| C(29,31) | - | 106.8 | - | - | 106.7 | 106.7 | - | - | - | - |
| C30 | - | 120.3 | - | - | 120.3 | 120.4 | - | - | - | - |
| C(33,34) | - | 55.8 | - | - | 55.8 | 55.8 | - | - | - | - |
| C35 | - | 167.2 | - | - | 167.2 | 167.2 | - | - | - | - |

13C NMR spectra

Department of Food Science and Technology,

I.K. Gujral Punjab Technical University, Kapurthala, Punjab, India.

E-mail ID: pawanpreet.fst@ptu.ac.in

Phone: +919888646036