Supplementary Information

Azide-functionalized Ligand Enabling Organic–Inorganic Hybrid Dielectric for High-Performance Solution-Processed Oxide Transistors

Juhyeok Lee, Syed Zahid Hassan, Sangjun Lee, Hye Ryun Sim, Dae Sung Chung*

Department of Chemical Engineering, Pohang University of Science and Technology (POSTECH), Pohang 37673, Republic of Korea

*Correspondence: dchung@postech.ac.kr

Supplementary Fig. 1. FT-IR spectra of bis-FPA films before and after being crosslinked.

Supplementary Fig. 2. UV-visible absorption spectra of bis-FPA films before and after being crosslinked.

Supplementary Fig. 3. Breakdown voltage of hybrid dielectric with 5 wt% and 10 wt% of bis-FPA.

Supplementary Fig. 4. FT-IR spectra of a Hyb_1 and b Hyb_2 films before and after being crosslinked.

Supplementary Fig. 5. Capacitance and breakdown voltage as a function of ZrO2 fractions.

Supplementary Fig. 6. Contact angle images of a-d water and e-h DIM droplets on the surface of a,e crosslinked-PMMA, b,f Hyb_0, c,g Hyb_1, and d,h Hyb_2.

Supplementary Fig. 7. Mobility statistics of In2O3/ZnO heterojunction TFTs with Hyb_2 as a gate dielectric.

Supplementary Fig. 8. Temperature dependence of electron mobilities.

Supplementary Fig. 9. Carrier density characteristics of In2O3/ZnO heterojunction TFT with Hyb_2 as a gate dielectric. a Drain-source current (IDS) and electron mobility as a function of gate-source voltage (VGS). b Carrier densities (nfree and ntrap) as a function of Fermi energy level (EF) from the conduction band edge (Em).

Supplementary Fig. 10. Carrier density characteristics of In2O3/ZnO heterojunction TFT with SiO2 as a gate dielectric. a Drain-source current (IDS) and electron mobility as a function of gate-source voltage (VGS). b Carrier densities (nfree and ntrap) as a function of Fermi energy level (EF) from the conduction band edge (Em).

Supplementary Fig. 11. Synthetic procedure of ethane-1,2-diyl bis(4-azido-2,3,5,6-tetrafluorobenzoate).

Supplementary Fig. 12. 1H NMR data of 2-((4-(1-acetyl-2-hydroxy-1-propen-1-yl)benzoyl)oxy)ethyl 4-azido-2,3,5,6-tetrafluorobenzoate.

Supplementary Fig. 13. 13C NMR data of 2-((4-(1-acetyl-2-hydroxy-1-propen-1-yl)benzoyl)oxy)ethyl 4-azido-2,3,5,6-tetrafluorobenzoate.

Supplementary Fig. S14. 19F NMR data of 2-((4-(1-acetyl-2-hydroxy-1-propen-1-yl)benzoyl)oxy)ethyl 4-azido-2,3,5,6-tetrafluorobenzoate.

Supplementary Table 1. Summary of contact angles measured on various surfaces (crosslinked-PMMA, Hyb_0, Hyb_1, and Hyb_2) and surface energy values calculated on basis of them.

|  | θwater (o) | θDIM (o) | γ (mN/m) |
| --- | --- | --- | --- |
| Crosslinked-PMMA | 70.92 | 37.54 | 47.51 |
| Hyb_0 | 53.87 | 28.21 | 58.77 |
| Hyb_1 | 92.69 | 41.29 | 39.55 |
| Hyb_2 | 97.89 | 42.62 | 38.39 |

Supplementary Table 2. Comparison of dielectric properties and electrical characteristics for various n-MOS with different organic-inorganic hybrid gate dielectric materials.

| Dielectric material | Channel material | k | Mobility (cm2V-1s-1) | Ion/Ioff | VTH (V) | SS (V dec-1) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| PVP-co-PMMA-PMF-HfOx | IGTO | 8.84 | 25.9 | ~107 | -0.2 | 0.4 | 1 |
| PVP-co-PMMA-PMF-ZrO2 | IZO | 5.6 | 28.4 | ~107 | -2.0 | 0.7 | 2 |
| PMMA-GPTMS-Al2O3 | ZnO | 6.2 | 4.5 | ~107 | 0.7 | - | 3 |
| PMMA-GPTMS-ZrHfO2 | ZnO, IGZO | 9.4 | 12.8, 2.45 | ~103, ~107 | 2.5, 1.2 | 3, 0.68 | 4 |
| PMMA-TMSPM-ZrO2 | ZnO | 6.8 | 0.48 | ~105 | 3.3 | 0.47 | 5 |
| PMMA-GPTMS-HfO2 | ZnO | 11.3 | 15.5 | ~106 | 0.5 | 0.37 | 6 |
| PVP/Al2O3 | SIZO | - | 8.84 | ~105 | -1.5 | 1.09 | 7 |
| PVP/ZrO2:B | In2O3 | 8.5 | 0.44 | ~105 | 1.7 | - | 8 |
| PVP/Al2O3 | IGZO | - | 8.39 | ~105 | 7.03 | 0.68 | 9 |
| PVP-PMF-Al2O3 | IGZO | 6.1 | 5.13 | ~105 | 2.3 | 0.84 | 10 |
| PVP-PMF-HfO2 | In2O3 | 6.5 | 2.6 | ~105 | 0.1 | 0.33 | 11 |
| PVA-GO | IGZO | - | 42 | ~107 | 0.79 | 0.106 | 12 |
| GPTMS-HfO2 | IGZO | 11.4 | 4.74 | ~104 | 0.3 | - | 13 |
| PMMA-ZrO2 | In2O3/ZnO | 14.0 | 51.19 | ~107 | 0.46 | 0.108 | This work |

Supplementary Table 3. Comparison of bias-stress stability characteristics for various n-MOS with different gate dielectric materials.

| Dielectric material | Channel material | Stress time (s) | Gate stress (V) | τ (s) | β | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| SiO2 | In2O3/ZnO | 86,400 | 30 | 2.55x108 | 0.40 | 14 |
| SiO2 | In2O3/ZnO:Al | 86,400 | 30 | 6.03x103 | 1 |  |
| SiO2 | In2O3 | 13,200 | 10 | 3.64x104 | 0.53 | 15 |
| SiO2 | IGZO | 10,000 | 15 | 2.00x104 | 0.42 | 16 |
| SiO2 | In2O3 | 32,400 | 40 | 2.34x105 | 0.51 | 17 |
| SiO2 | ZnO | 32,400 | 40 | 2.32x105 | 0.50 |  |
| SiO2 | IGZO | 7,000 | 30 | 1.30x106 | 0.46 | 18 |
| Al2O3 | IGZO | 10,000 | 5 | - | - | 19 |
| ZrO2 | IZO | 1,000 | 20 | - | - | 20 |
| AlZrOx | SWCNT | 1,800 | -3 | 2.63x103 | - | 21 |
| HfOy/AlOx | ZTO | 3,600 | 3 | 1.13x107 | 0.20 | 22 |
| AlOx/HfOy | ZTO | 3,600 | 3 | 0.65x103 | 0.44 |  |
| ZrO2/HfO2 | IGZO | 3,600 | 5 | 8.31x106 | 0.79 | 23 |
| PMMA-ZrO2 | In2O3/ZnO | 43,200 | 10 | 4.06x105 | 0.64 | This work |

References

[1] Hur, J. S., Kim, J. O., Kim, H. A. & Jeong, J. K. Stretchable Polymer Gate Dielectric by Ultraviolet-Assisted Hafnium Oxide Doping at Low Temperature for High-Performance Indium Gallium Tin Oxide Transistors. ACS Appl. Mater. Interfaces 11, 21675-21685 (2019).

[2] Son, B.-G., Je, S. Y., Kim, H. J. & Jeong, J. K. Modification of a polymer gate insulator by zirconium oxide doping for low temperature, high performance indium zinc oxide transistors. RSC Adv. 4, 45742-45748 (2014).

[3] Meza-Arroyo, J., Syamala Rao, M. G., Mejia, I., Quevedo- López, M. A. & Ramírez-Bon, R. Low temperature processing of Al2O3-GPTMS-PMMA hybrid films with applications to high-performance ZnO thin-film transistors. Appl. Surf. Sci. 467-468, 456-461 (2019).

[4] Syamala Rao, M. G. et al. Low-temperature sol-gel ZrHfO2-PMMA hybrid dielectric thin-films for metal oxide TFTs. J. Non-Cryst. Solids 502, 152-158 (2018).

[5] Alvarado-Beltran, C. G., Almaral-Sanchez, J. L., Mejia, I., Quevedo-Lopez, M. A. & Ramirez-Bon, R. Sol-Gel PMMA-ZrO2 Hybrid Layers as Gate Dielectric for Low-Temperature ZnO-Based Thin-Film Transistors. ACS Omega 2, 6968-6974 (2017).

[6] Mullapudi, G. S. R., Velazquez-Nevarez, G. A., Avila-Avendano, C., Torres-Ochoa, J. A., Quevedo-López, M. A. & Ramírez-Bon, R. Low-Temperature Deposition of Inorganic–Organic HfO2–PMMA Hybrid Gate Dielectric Layers for High-Mobility ZnO Thin-Film Transistors. ACS Appl. Electron. Mater. 1, 1003-1011 (2019).

[7] Choi, J. Y., Kim, S., Hwang, B. U., Lee, N. E. & Lee, S. Y. Flexible SiInZnO thin film transistor with organic/inorganic hybrid gate dielectric processed at 150 °C. Semicond. Sci. Technol. 31, 125007 (2016).

[8] Park, J. H, Oh, J. Y, Han, S. W, Lee, T. I. & Baik, H. K. Low-temperature, solution-processed ZrO2:B thin film: a bifunctional inorganic/organic interfacial glue for flexible thin-film transistors. ACS Appl. Mater. Interfaces 7, 4494-4503 (2015).

[9] Hwang, B.-U. et al. Role of ultrathin Al2O3 layer in organic/inorganic hybrid gate dielectrics for flexibility improvement of InGaZnO thin film transistors. Org. Electron. 15, 1458-1464 (2014).

[10] Lai, H.-C., Pei, Z., Jian, J.-R. & Tzeng, B.-J. Alumina nanoparticle/polymer nanocomposite dielectric for flexible amorphous indium-gallium-zinc oxide thin film transistors on plastic substrate with superior stability. Appl. Phys. Lett. 105, 033510 (2014).

[11] Rao, M. G. S. et al. Tuning the electrical performance of solution-processed In2O3TFTs by low-temperature with HfO2-PVP hybrid dielectric. Mater. Today Commun. 26, 102120 (2021).

[12] Wang, X., Gao, Y., Liu, Z., Luo, J. & Wan, Q. Flexible Low-Voltage IGZO Thin-Film Transistors With Polymer Electret Gate Dielectrics on Paper Substrates. IEEE Electron Device Lett. 40, 224-227 (2019).

[13] Rao, M. G. S., Sánchez-Martinez, A., Gutiérrez-Heredia, G., Quevedo- López, M.A. & Ramírez-Bon, R. Sol-gel derived low temperature HfO2-GPTMS hybrid gate dielectric for a-IGZO thin-film transistors (TFTs). Ceram. Int. 44, 16428-16434 (2018).

[14] Lin, Y.-H. et al. Hybrid organic–metal oxide multilayer channel transistors with high operational stability. Nat. Electron. 2, 587-595 (2019).

[15] Abdullah, I. et al. Bias stability of solution-processed In2O3 thin film transistors. J. Phys. Mater. 4, 015003 (2020).

[16] Lee, J.-M., Cho, I.-T., Lee, J.-H. & Kwon, H.-I. Bias-stress-induced stretched-exponential time dependence of threshold voltage shift in InGaZnO thin film transistors. Appl. Phys. Lett. 93, 093504 (2008).

[17] Khim, D., Lin, Y. H. & Anthopoulos, T. D. Impact of Layer Configuration and Doping on Electron Transport and Bias Stability in Heterojunction and Superlattice Metal Oxide Transistors. Adv. Funct. Mater. 29, 1902591 (2019).

[18] Chowdhury, M. D. H., Ryu, S. H., Migliorato, P. & Jang, J. Effect of annealing time on bias stress and light-induced instabilities in amorphous indium–gallium–zinc-oxide thin-film transistors. J. Appl. Phys. 110, 114503 (2011).

[19] Kim, Y. H. et al. Flexible metal-oxide devices made by room-temperature photochemical activation of sol-gel films. Nature 489, 128-132 (2012).

[20] Park, J. H. et al. Low-temperature, high-performance solution-processed thin-film transistors with peroxo-zirconium oxide dielectric. ACS Appl. Mater. Interfaces 5, 410-417 (2013).

[21] Li, J., Huang, C.-X. & Zhang, J.-H. Tuning the electrical performance and bias stability of a semiconducting SWCNT thin film transistor with an atomic layer deposited AlZrOx composite. RSC Adv. 7, 52517-52523 (2017).

[22] Kim, Y. G., Avis, C. & Jang, J. Low Voltage Driven, Stable Solution-Processed Zinc-Tin-Oxide TFT with HfOy and AlOx Stack Gate Dielectric. ECS Solid State Lett. 1, Q23-Q25 (2012).

[23] Yang, J., Yang, X., Zhang, Y., Che, B., Ding, X. & Zhang, J. Improved gate bias stressing stability of IGZO thin film transistors using high-k compounded ZrO2/HfO2 nanolaminate as gate dielectric. Mol. Cryst. Liq. Cryst. 676, 65-71 (2019).