Figure captions

Fig.S1 Effect of flocculation time on removal of As(Ⅲ) and As(Ⅴ) by Fe(VI) (a), The residual Fe in water samples at different pH (b). (Initial concentration of As(Ⅲ) and As(Ⅴ) 250 μg/L, As(V) removal at Fe(VI) dosage 6 mg/L and As(III) removal at Fe(VI) dosage 4 mg/L).

Fig. S2 The size distribution of flocs formed in Fe(VI) and hydrolytic ferric iron oxides for arsenic removal (ferrate resultant particles self-decomposition (Fe(VI)), ferrate oxidation with arsenic particles (in-situ), mixture of 30 min hydrolytic ferric iron oxides particles with arsenic (ex-situ)).

Fig. S3 Curve fitting the XPS spectrum of F2p in Fig. 5(b).

Table captions

Table S1 Characteristics of water samples for the designed experiments

Table S2 The EDS elements of the particles formed in Fe(VI) and hydrolytic ferric iron oxides for arsenic removal (ferrate oxidation with arsenic particles (in-situ), mixture of 30 min hydrolytic ferric iron oxides particles with arsenic (ex-situ))

Fig.S1 Effect of flocculation time on removal of As(Ⅲ) and As(Ⅴ) by Fe(VI) (a), The residual Fe in water samples at different pH (b). (Initial concentration of As(Ⅲ) and As(Ⅴ) 250 μg/L, As(V) removal at Fe(VI) dosage 6 mg/L and As(III) removal at Fe(VI) dosage 4 mg/L).

Figure S2. The size distribution of flocs formed in Fe(VI) and hydrolytic ferric iron oxides for arsenic removal (ferrate resultant particles self-decomposition (Fe(VI)), ferrate oxidation with arsenic particles (in-situ), mixture of 30 min hydrolytic ferric iron oxides particles with arsenic (ex-situ)).

Figure S3. Curve fitting the XPS spectrum of F2p in Fig. 5(b).

Table S1 Characteristics of water samples for the designed experiments

| Characteristics | Units of measurement | Numerical value |
| --- | --- | --- |
| pH(25℃) | — | 7.70±0.05 |
| Turbidity | NTU | 0.40±0.10 |
| As(V)/As(Ⅲ) | μg/L | 250 |
| DOC | mg/L | 3.194 |
| Alkalinity | mg CaCO3/L | 90 |
| Hardness | mg CaCO3/L | 157.5 |
| P | mg/L | 0.012 |
| Al | mg/L | 0.076 |
| Fe | mg/L | 0.003 |
| SO42- | mg/L | 33.541 |
| Cl- | mg/L | 23.257 |

Table S2 The EDS elements of the particles formed in Fe(VI) and hydrolytic ferric iron oxides for arsenic removal (ferrate oxidation with arsenic particles (in-situ), mixture of 30 min hydrolytic ferric iron oxides particles with arsenic (ex-situ))

| Elements(%) | in-situ-As(V) |  | in-situ-As(III) |  | ex-situ-As(V) |  | ex-situ-As(III) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Weight | Atomic | Weight | Atomic | Weight | Atomic | Weight | Atomic |
| O | 93.76 | 98.15 | 96.42 | 98.99 | 90.69 | 97.21 | 93.21 | 97.95 |
| K | 0.16 | 0.08 | 0.03 | 0.01 | 0.02 | 0.01 | 0.09 | 0.04 |
| Fe | 5.52 | 1.65 | 2.91 | 0.86 | 8.42 | 2.58 | 6.59 | 1.98 |
| As | 0.56 | 0.12 | 0.63 | 0.14 | 0.86 | 0.2 | 0.11 | 0.03 |