Fig. S1. Effect of CZnO coating dosage and contact time on %RE of COD (at pH 2 and initial COD concentration of 200 mg/L)

Fig. S2. Effect of pH on %RE of COD (at 1.5 M CZnO coating dosage, 120 min contact time and initial COD concentration of 200 mg/L)

Fig. S3. Effect of initial COD concentration on %RE of COD (at 1.5 M CZnO coating dosage, 120 min contact time and pH 2)

Table S1. Effect of CZnO nanoadsorbent coating dosage and contact time on %RE of BOD (at pH 7 and initial BOD concentration of 100 mg/L)

| Contact time (min) | Coating dosage of CZnO (M) |  |  |  |
| --- | --- | --- | --- | --- |
|  | 0.5 | 1 | 1.5 | 2 |
| 20 | 40.14±0.30 (59.86) | 54.22±0.40 (45.78) | 60.14±0.45 (39.86) | 57.53±0.43 (42.47) |
| 40 | 48.46±0.36 (51.54) | 63.95±0.48 (36.05) | 75.46±0.56 (24.54) | 71.92±0.54 (28.08) |
| 60 | 55.94±0.42 (44.06) | 70.39±0.53 (29.61) | 83.94±0.63 (16.06) | 78.29±0.59 (21.71) |
| 80 | 61.54±0.46 (38.46) | 75.30±0.56 (24.70) | 91.54±0.69 (8.46) | 85.51±0.64 (14.49) |
| 100 | 69.24±0.52 (30.76) | 82.15±0.62 (17.85) | 93.24±0.70 (6.76) | 88.26±0.66 (11.74) |
| 120 | 75.22±0.56 (24.78) | 85.83±0.64 (14.17) | 95.22±0.71 (4.78) | 88.26±0.98 (11.74) |
| 140 | 75.22±0.32 (24.78) | 85.83±0.64 (14.17) | 95.22±0.78 (4.78) | 88.26±0.22 (11.74) |
| 160 | 75.22±0.28 (24.78) | 85.83±0.64 (14.17) | 95.22±0.18 (4.78) | 88.26±0.16 (11.74) |
| 180 | 75.22±0.21 (24.78) | 85.83±0.64 (14.17) | 95.22±0.36 (4.78) | 88.26±0.61 (11.74) |
|  | CD @ (1%) | SE(d)± | SE(m)± | p-value |
| Contact time (A) | 0.48 | 0.24 | 0.17 | 0.001 (s) |
| Coating dosage (B) | 0.32 | 0.16 | 0.11 |  |
| Interaction (A×B) | 0.97 | 0.48 | 0.34 |  |

Parenthesis value shows final concentration of BOD (mg/L)

Table S2. Effect of pH on %RE of BOD (at CZnO nanoadsorbent coating dosage of 1.5 M, contact time of 120 min and initial BOD concentration of 100 mg/L)

| pH | % RE of BOD |
| --- | --- |
| 2 | 57.24±0.26 (42.97) |
| 4 | 60.03±0.25 (39.76) |
| 6 | 90.03±0.39 (9.97) |
| 8 | 89.18±0.38 (10.82) |
| 10 | 87.21±0.38 (12.79) |
| 12 | 84.27±0.36 (15.73) |
| CD @ 1(%) | 1.07 |
| SE(m)± | 0.34 |
| SE(d)± | 0.48 |
| CV (%) | 0.76 |

Parenthesis value shows final concentration of BOD (mg/L)

Table S3. Effect of initial BOD concentration on %RE of BOD (at CZnO nanoadsorbent coating dosage of 1.5 M, contact time of 120 min and pH 6)

| Initial concentration (mg/L) | % RE of BOD |
| --- | --- |
| 50 | 94.44± 0.41 (2.78) |
| 100 | 94.39±0.41 (5.61) |
| 150 | 85.36±0.37 (21.95) |
| 200 | 76.19±0.33 (47.61) |
| 250 | 64.97±0.28 (87.56) |
| 300 | 64.89±0.28 (105.33) |
| CD @ 1(%) | 1.09 |
| SE(m)± | 0.35 |
| SE(d) ± | 0.49 |
| CV (%) | 0.76 |

Parenthesis value shows final concentration of BOD (mg/L)