Electronic Supplementary Information

Design and Synthesis of Magnetic Immobilized Pineapple Cellulose/EDTA for Removal of Copper(II) and Zinc(II) by Coordination

Journal of Inorganic and Organometallic Polymers and Materials

Hanan Sayahi, Simin Asadabadi*

Department of Applied Chemistry, Faculty of Chemistry, Bu–Ali Sina University, Hamedan 6517838695, Iran

*Corresponding author: (Dr. Simin Asadabadi), E-mail address: s.asadabadi@basu.ac.ir

Corresponding author’s ORCID ID: 0000-0001-8992-6894

Supplementary Figures and Tables

| (a) λmax = 600 nm | λmax = 620 nm (b) |
| --- | --- |

Fig. S1 UV-Vis absorption spectra of cation-bound Zincon (a) Cu2+-Zincon at concentration of 12.0 mg·L-1 in 10.0 ml phosphate buffer and (b) Zn2+-Zincon at concentration of 20.0 mg·L-1 in 10.0 ml phosphate buffer

Fig. S2 FE-SEM image of Fe3O4, Fe3O4@SiO2, Fe3O4@SiO2@NH2, EDTA, modified cellulose, and bionanocomposite

Fig. S3 Graph of ΔpH versus pHinitial

(a)

Table S1 Levels of factors used for design of experiments

| Factor | Level |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | -α | -1 | 0 | +1 | +α |
|  | Cu2+ |  |  |  |  |
| pH | 3.15 | 4.00 | 5.25 | 6.50 | 7.35 |
| T (°C) | 20.0 | 25.0 | 32.5 | 40.0 | 45.1 |
| CBNC (g·L1) | 0.06 | 0.12 | 1.30 | 2.00 | 2.48 |
|  | Zn2+ |  |  |  |  |
| pH | 3.97 | 5.25 | 7.12 | 9.00 | 10.28 |
| T (°C) | 20.0 | 25.0 | 32.5 | 40.0 | 45.1 |
| CBNC (g·L1) | 0.06 | 0.12 | 1.30 | 2.00 | 2.48 |

Table S2 Statistic used for testing the adequacy of model

| Formula |  |
| --- | --- |
| residual=Rexp,i-Rcal,i | Rexp,i: experimental response Rcal,i: calculated response |
| SSresidual=i=1n(Rexp,i-Rcal,i)2 | SSresidual: sum of squares of residual |
| SSmodel=SStotal-SSresidual | SSmodel: sum of squares of model |
| SStotal=i=1n(Rexp,i-R)2 | SStotal: sum of squares of total |
| PRESS=i=1n(Rexp,i-Rcal,i)2 | PRESS: prediction error sum of squares |
| R2=1-SSresidual(SSmodel+SSresidual) | R2: coefficient of determination |
| RAdj.2=1-SSresidual(n-p)(SSmodel+SSresidual)(n-1) | RAdj.2: adjusted coefficient of determination |
| RPred.2=1-PRESS(SSmodel+SSresidual)(n-1) | RPred.2: predicted coefficient of determination |
| SD=i=1n(Rexp,i-R)2n-1 | SD: standard deviation |
| C.V.%=sR×100% | C.V.%: coefficient of variation |
| A.P.=SignalNoise | A.P.: adequate precision |

Table S3 Kinetics model parameters, RAdj.2, AICc, χ2 and RMSE at optimum conditions and concentration of 30.0 mg·g-1

| Model | Cation | Parameter |  |  | Goodness of Fit |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PFO |  | qe (mg·g-1) | k1 | - | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | 13.47 | 2.86 |  | 0.9732 | 0.677 | 0.3232 | 0.6405 |
|  | Zn2+ | 13.52 | 0.08 |  | 0.9632 | 1.240 | 0.7403 | 0.8118 |
| PSO |  | qe (mg·g-1) | k2 | - | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | 14.00 | 0.43 |  | 0.9966 | -1.377 | 0.0449 | 0.2294 |
|  | Zn2+ | 16.77 | 0.004 |  | 0.9306 | 1.874 | 1.2672 | 1.1149 |
| Elovich |  | aE | bE | - | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | 5356234.77 | 1.32 |  | 0.9927 | -0.621 | 0.0878 | 0.3348 |
|  | Zn2+ | 1.70 | 0.25 |  | 0.8932 | 2.305 | 1.8445 | 1.3833 |
| MOE |  | qe (mg·g-1) | k1 | F2 | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | -0.05 | -14.38 | 0.00 | 0.9560 | 1.458 | 0.4555 | 0.8200 |
|  | Zn2+ | 12.72 | 0.16 | -6.63 | 0.9995 | -2.620 | 0.0108 | 0.0985 |
| PnO |  | qe (mg·g-1) | k1 | n | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | 14.61 | 0.08 | 2.88 | 0.9986 | -1.964 | 0.0163 | 0.1481 |
|  | Zn2+ | 13.34 | 0.09 | 0.80 | 0.9624 | 1.620 | 0.7252 | 0.8210 |
| MPnO |  | qe (mg·g-1) | k' | n | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | 13.98 | 7.75 | 0.04 | 0.9990 | -2.314 | 0.0110 | 0.1244 |
|  | Zn2+ | 12.81 | 0.39 | 0.31 | 0.9977 | -1.188 | 0.0446 | 0.2017 |
| FL-PFO |  | qe (mg·g-1) | k1' | a | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | 13.31 | 24.57 | 36.93 | 0.0823 | 4.496 | 48029879338 | 3.7456 |
|  | Zn2+ | 12.69 | 0.01 | 1.76 | 0.9993 | -2.373 | 0.0146 | 0.1115 |
| FL-PSO |  | qe (mg·g-1) | k2' | a | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | 14.49 | 0.32 | 0.65 | 0.9947 | -0.337 | 0.0148 | 0.3085 |
|  | Zn2+ | 13.07 | 0.00 | 2.68 | 0.9987 | -2.061 | 0.1018 | 0.1411 |

Table S4 Isotherm parameters, RAdj.2, AICc, χ2 and RMSE at optimum conditions

| Isotherm | Cation | Parameter |  |  | Goodness of Fit |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Langmuir |  | qm (mg·g-1) | KL | - | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | 151.0 | 0.738 |  | 0.9868 | 5.3078 | 66.6955 | 6.2071 |
|  | Zn2+ | 179.5 | 0.126 |  | 0.9508 | 6.6744 | 17.3114 | 12.2920 |
| Freundlich |  | KF | c | - | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | 73.4 | 0.181 |  | 0.8974 | 7.3581 | 34.1722 | 17.3020 |
|  | Zn2+ | 45.4 | 0.301 |  | 0.8106 | 8.0218 | 63.7484 | 24.1115 |
| Temkin |  | bT | KT | - | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | 131.9 | 54.49 |  | 0.9501 | 6.6371 | 18.8014 | 12.7969 |
|  | Zn2+ | 66.9 | 1.30 |  | 0.9075 | 7.3054 | 25.9123 | 17.8741 |
| Modified Langmuir |  | qm (mg·g-1) | KML | - | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | 151.0 | 2952213 |  | 0.9856 | 5.7549 | 66.6956 | 6.4883 |
|  | Zn2+ | 179.4 | 3803 |  | 0.9508 | 6.6744 | 17.3114 | 12.2920 |
| Redlich-Peterson |  | KRP | aRP | β | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | 11390440.3 | 155116.5 | 0.82 | 0.8846 | 7.8342 | 34.1697 | 18.3509 |
|  | Zn2+ | 11390440.3 | 250829.9 | 0.70 | 0.7870 | 8.4980 | 63.7483 | 25.5740 |
| Toth |  | qm (mg·g-1) | aT | c | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | 153.8 | 0.885 | 0.88 | 0.9857 | 5.7430 | 51.2939 | 6.4497 |
|  | Zn2+ | 152.2 | 0.077 | 3.94 | 0.9986 | 3.5069 | 0.3636 | 2.1086 |
| Extended Langmuir |  | qm (mg·g-1) | KEL | a | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | 155.1 | 0.840 | 0.17 | 0.9856 | 5.7549 | 55.1085 | 6.4883 |
|  | Zn2+ | 105.8 | 0.077 | -1.15 | 0.9954 | 4.6692 | 1.0832 | 3.7703 |
| Langmuir-Freundlich |  | qm (mg·g-1) | KLF | c | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | 155.4 | 0.707 | 0.85 | 0.9872 | 5.6392 | 27.7330 | 6.1238 |
|  | Zn2+ | 157.3 | 0.155 | 1.83 | 0.9915 | 5.2806 | 6.7317 | 5.1184 |
| Modified Langmuir-Freundlich |  | qm (mg·g-1) | KMLF | c | RAdj.2 | AICc | χ2 | RMSE |
|  | Cu2+ | 155.4 | 2830297 | 0.85 | 0.9872 | 5.6392 | 27.7332 | 6.1238 |
|  | Zn2+ | 157.3 | 4675 | 1.83 | 0.9915 | 5.2801 | 6.7283 | 5.1173 |