Table 1. Main types of bio-based products

| Biomaterials by category | Type of bio-based products | References |
| --- | --- | --- |
| Category 1 Binding materials, aggregates and/or additives for soil, cement and/or concrete | Sustainable cement Green, ecological and/or sustainable concrete Concrete blocks Hardened concrete Agro-concrete/cement Ordinary Portland cement (OPC) concrete Lightweight aggregate concrete Cement concrete Geopolymer concrete Clayey sand and soil Cement mortars Activated cement mortar Cement-based panels Wood-cement blocks Roofing tiles Clay and laterite soils | [7, 18, 54, 56, 63, 67–70, 72, 73, 76, 22, 82, 84, 87, 89–91, 93, 100, 23, 27, 36–38, 52, 53] |
| Category 2 Brick materials | Ceramic bricks Clay bricks Clay matrix bricks Fired clay bricks Agro bricks Earth bricks Light fired clay bricks Lightweight bricks Thermally efficient burnt clay bricks Eco-friendly clay bricks Eco-friendly porous ceramic bricks Unfired earth blocks/ bricks White brick fuel cell Building block for masonry wall | [6, 15, 77, 78, 80, 86, 97, 101–105, 26, 31, 38, 43, 55, 57, 59, 64] |
| Category 3 Materials/biocomposites for structural and/or reinforcement applications | Natural fiber/polymer composites (NFPCs) Polymer matrices for lightweight structural applications Reinforced polypropylene composites (wall panel) Bio-epoxy resin reinforced green composites Bio-based polymers Wallpaper Hybrid polypropylene composites False ceiling tiles Fiber-cement Concrete walls Cement-bonded particleboard Binderless fibre-board Reinforced polypropylene Reinforced composites Particleboard Fibreboards Unitary (or ‘‘monolithic”) structural components and assemblies Earth Plaster Composites Panels, door shutters, door frames, roofing sheets and dough molding compounds Roofing tiles, ceiling plates, thin sheets, wall panels Lightweight building components Structural sheathing materials Composite boards/panels | [30, 43, 106–113, 57, 58, 61, 79, 83, 96, 99, 100] |
| Category 4 Materials for thermal and/or acoustic insulation in buildings | Joints between walls, windows, floor, and roof Recycled waste panels Insulation panels Bio-based insulations Structural materials for low-energy buildings Thermal insulating plate Reinforced panels Particleboards Bio-Based Plastics | [14, 31–33, 62, 66, 98, 110, 114] |
| Category 5 Road construction materials | Sustainable bio-modified asphalt Asphaltic concrete Modified Asphalt Binders | [81, 95, 115, 116] |

Table 2. Main properties and parameters of the bio-based products

| Properties | Parameter | References |
| --- | --- | --- |
| Physical | Sorptivity Bulk density Microstructure Specific Gravity Drying shrinkage Apparent Porosity Water absorption | [6, 7, 55, 58, 61, 64, 65, 77, 78, 80, 81, 88, 14, 89, 91, 92, 95, 97, 98, 100, 102, 104, 105, 15, 106–110, 112, 114–116, 22, 25, 28, 32, 35, 53] |
| Mechanical | Durability Workability Flowability Flexural strength Tensile strength Impact strength Young’s modulus Thickness swelling Compressive strength | [6, 7, 32, 35, 36, 38, 53, 57, 58, 61–63, 14, 64, 68, 70–75, 82, 88, 15, 89, 91–94, 96, 97, 99, 100, 102, 18, 103–109, 111, 113, 114, 22, 116, 26–28, 31] |
| Chemical | Loss on ignition Chloride resistance Resistance to chloride Acid and sulphate resistance Heavy metals content/leaching toxicity | [7, 18, 22, 25, 28, 53, 55, 64, 78, 98] |
| Others | Mineralogical analysis Sound absorption Thermal conductivity High temperature resistance Thermogravimetric analysis | [6, 7, 59, 62, 64, 68, 73, 77, 78, 92, 98, 99, 14, 100, 102–107, 109–111, 26, 114, 31–33, 38, 55, 57] |

Table 3. Main types and properties of AWBs used by category

| Type of biomaterials | Main type and form of AWB | Main characteristics of the by-product | Effects on the properties of bio-based products | References |
| --- | --- | --- | --- | --- |
| Category 1 Binding materials, aggregates and/or additives for soil, cement and/or concrete | Rice Husk (Ash) Sugarcane bagasse (Ash) Coconut husks (Ash) | Rich in amorphous silica High pozzolanic activity Pore-forming additives Lower specific gravity Increases setting time lower thermal conductivity | Improved mechanical properties (Compressive, flexural, shear and tensile strength) Reduction of thermal conductivity Density reduction (lighter materials) Better resistance to acid attack Increased resistance to chloride penetration Lower water absorption Reduced permeability Improved durability Improved workability Improvement of the geotechnical properties of the soil | [6, 7, 35, 38, 52, 53, 56, 60, 63, 67–69, 15, 70–72, 74, 75, 82, 90, 92, 113, 18, 22–24, 28, 31, 34] |
| Category 2 Brick materials | Rice Husk (Ash) Cereal Straw (Ash –fibers) Sugarcane bagasse (Ash) |  | Increased ceramic strength Increase in amount and size of pores Reduction of bulk density Reduction of brick weight Reduction of the thermal conductivity coefficient Lower dead load Improved thermal insulation properties Improved static properties Reduced plasticity | [15, 26, 104, 105, 31, 55, 59, 64, 77, 78, 80, 102] |
| Category 3 Materials/biocomposites for structural and/or reinforcement applications | Cereal Straw (Fibers) Rice Husk (Ash) Coconut husks (Fibers - Ash) | Lower specific gravity High percentage of fibers Longer fibers Tubular internal structure, strong and efficient Low density High cellulose and hemicellulose content | Improvement of impact, tensile and flexural strength Better resistance to water and thickness swelling Low weight Good sound absorption Improved load transfer and crack arrest efficiency Improved thermal insulation/ thermal stability Better structural integrity and energy dissipation Good stiffness for civil infrastructural applications Control of shrinkagecracks Decreases erosion of materials Improveds shrinkage properties Better absorption of impact energy | [15, 30, 108–112, 114, 57, 58, 61, 83, 96, 99, 100, 106] |
| Category 4 Materials for thermal and/or acoustic insulation in buildings | Rice Husk (fibers) Cereal Straw (fibers) Sugarcane bagasse (fibers) |  | Better thermal and environmental performance Good thermal conductivity and resistivity Satisfactory results in mechanical and thermophysical performance High sound absorption coefficients Lower density | [14, 31–33, 66, 98, 114] |
| Category 5 Road construction materials | Rice Husk (Ash-fibers) Coconut Shell (Small aggregate) Sugarcane bagasse (Fibers) Palm shells (coarse aggregate) |  | Increased resistance to thermal cracking of the pavement at low temperatures Reduced permanent (plastic) deformation at high road surface temperatures under traffic loads Improvement of -the rutting factor Improved fatigue resistance of the asphalt binder Good range stability Marshall Improved mechanical properties | [81, 115, 116] |

Table 4. Limitations and improvement alternatives for bio-based products

| Limitations and/or disadvantages | Alternatives to reduce adverse effects | Reference |
| --- | --- | --- |
| Increase LOI Reduction of workability Lower strength activity index (SAI) Higher drying shrinkage High water absorption Susceptibility towards chemical attack Effect of moisture content on internal bonding Dimensional stability Lower durability Crack formation | Additional treatments Chemical and/or heat treatment of fibres Pre-treatment methods (screening, burning, drying, firing) Incorporation of nanomaterials nano silica, nano alumina Inclusion of bacteria in rice husk Addition of stone dust | [15, 18, 54, 58, 62, 91, 106, 107, 110–112, 114, 21, 22, 25, 29, 31, 32, 34, 35] |

Table 5. Main benefits by dimension

| Dimension | Description of main benefits or advantages | References |
| --- | --- | --- |
| Economic | New value chains New market opportunities Savings raw materials Reduction of material production costs Reduction of waste landfill fees Reduction of transportation costs Reduction in construction cost Reduction of road construction and maintenance in rural areas costs | [7, 15, 55, 58, 60, 64, 67, 70, 74, 82, 85, 86, 23, 91, 96, 97, 99–101, 105, 107, 115, 26, 28, 29, 31, 32, 37, 42] |
| Environmental | Carbon dioxide (CO2) emissions reduction Reducing global warming and climate change Increasing energy efficiency Reduction in consumption of thermal and electrical energy Landfill reduction Improving the management of the AWB Recycling and valorisation of AWB Values of leaching toxicity much lower Reduced consumption of natural clay reserves Reducing the exploitation of natural resources Reduction of AWB burning Reduction of water consumption Reduced consumption of virgin raw materials Reduction of soil erosion | [6, 7, 32–38, 42, 52, 54, 14, 55–58, 63, 64, 66–69, 15, 70, 72–78, 82, 83, 23, 85–87, 91, 94, 97–101, 24, 103, 105, 106, 108, 111, 114, 115, 26, 28, 29, 31] |
| Social | Creation of new jobs Enhancing the economic power of local communities. Low-cost building and/or infrastructure development in low-income regions Use of locally available materials for infrastructure works in developing countries Reduce social housing cost Functional, high quality, comfortable and affordable environments for building occupants Societal welfare Healthy indoor environment Population health benefits | [14, 31–33, 87, 91, 93, 100, 105, 115] |

Table 6. European Union projects

| Proyect name | Objetive | Type of AWB | Type of bio-based prodcuts | Project implementation date | R |
| --- | --- | --- | --- | --- | --- |
| Grant agreement ID: CR147691-BRE21154 | Development of new construction materials based on mineral binders derived from waste | Straw and husk | Mineral binder | May-July 1994 | [117] |
| ECO-PCCM | To introduce a new class of eco-friendly and cost-effective polymer composite construction material | Rice straw, hemp, kenaf, cotton, sisal, flax | Renewable eco-friendly composites for structural components | October 2004 - September 2007 | [118] |
| SYNPOL- Biopolymers from Syngas Fermentation | Establish a platform for integrating synthesis gas production and fermentation technologies for cost-effective commercial production of high value-added biopolymers. | Straw | Biopolymers | October 2012 - September 2016 | [119] |
| REHAP | Development of new materials for the construction sector from agricultural and forestry residues | Wheat straw | Thermoplastic PU Adhesive Wooden boards Cement | October 2016 - March 2021 | [123] |
| AgroCycle | To convert low-value agricultural waste into highly valuable products, achieving a 10% increase in waste recycling and valorisation by 2020. | Horticultural waste | High value-added biopolymers | June 2016 - May 2019 | [128] |
| Mycotaff | A renewable bio-based material that enables efficient, cost-effective production of high-quality insulation, packaging, dry-wall, and other building materials | Mushroom mycelia | Prefabrication walls material for insulation and other building applications | June - september 2018 | [129] |
| BARBARA | The development of novel bio-based engineering bioplastic materials to be validated as functional prototypes with advanced properties for the building and automotive sectors. | Lemon, carrot, pomegranate and almond shell | Polyester-Based Biocomposites Moulds for Resin Transfer Moulding and truss joint prototypes | May 2017- October 2020 | [130] |
| B-SMART | To develop new intelligent cementitious nanocomposites for multifunctional built infrastructure made by combining ordinary Portland cement (OPC) with cheap bio-nanomaterials synthesised from root vegetable waste such as carrot and beetroot waste streams produced by the food processing industry. | Carrot and beetroot waste | Intelligent cementitious nanocomposites for multifunctional built infrastructure | September 2018 - September 2020 | [131] |
| NoAW : No Agro-Waste | To generate innovative efficient approaches to convert growing agricultural waste issues into eco-efficient bio-based products opportunities with direct benefits for both environment, economy and EU consumer. | Maize silage grape stalks Vine shoots /wine pomace Fruit and vegetable wastes | Biocomposites/Biodegradable polymers - polyhydroxyalkanoates (PHAs). | October 2016 - January 2021 | [124] |

R: Reference