Supporting Information

Metal-nanoparticles/carbon nanosheets-derived from covalent organic frameworks for electrochemical sensing furazolidone, dopamine and uric acid

Jianhui Xiong, Yuxi Yang, Linyu Wang, Shouhui Chen*, Yan Du* and Yonghai Song

National Engineering Research Center for Carbohydrate Synthesis/Key Lab of Fluorine and Silicon  for Energy Materials and Chemistry of Ministry of Education, College of Chemistry and Chemical Engineering, Jiangxi Normal University, 99 Ziyang Avenue, Nanchang 330022, China.

Materials and reagents

1,3,5-Tris(4-aminophenyl)benzene (TAPB) and 2,6-dihydroxynaphthalene-1,5-diformaldehyde (DHNDA) were purchased from Jilin Chinese Academy of Sciences-Yanshen Technology Co., Ltd (Changchun, China). Dopamine (DA), uric acid (UA) and furazolidone (FZ), acetic acid (C2H4O2), 1,2-dichlorobenzene, 1-butanol, tetrahydrofuran, acetone, Cu(NO3)2·6H2O, Fe(NO3)3·9H2O, Co(NO3)2·6H2O and Ni(NO3)2·6H2O were purchased from Aladdin Co., LTD. (Shanghai, China). Na2HPO4·12H2O, NaH2PO4·2H2O, ethanol and other chemical substances were purchased from Beijing Chemical Reagent Factory (Beijing, China). A phosphate buffer (0.2 M PBS) was made from 0.2 M dibasic sodium phosphate solution and 0.2 M sodium dihydrogen phosphate solution. All reagents were analytically pure and were not further purified and used directly. All solution was prepared with ultrapure water, and the ultrapure water purification system is the Millipore - Q purified (ρ≥18.2 MΩ cm-1).

Instruments

JEM-2010 (HR) was used for obtaining transmission electron microscopy image (TEM). Fourier transform infrared spectroscopy (FTIR) was recorded on model Perkin-Elmer Spectrome 100 spectrometer (Perkin-Elmer Company, USA). N2 adsorption/desorption isotherm measurement was operated using a BELSORP-mini II instrument under the liquid nitrogen temperature (77 K). X-ray photoelectron spectroscopy was taken using the ESCA-LAB-MKII, with Al Kα as the excitation source, and C1s (284.6 eV) as the reference line. SDT 2960 was used for obtaining the instrument model of the thermogravimetric analysis (TGA), the heating rate was 10 °C min-1, and the test was performed under a nitrogen atmosphere. Powder X-ray diffraction (XRD) analysis was performed on a D/Max 2500 V/PC X-ray powder diffractometer using Cu Kα radiation range from 2° to 35° with scanning step controlled 1°/min. All electrochemical measurements were performed on a CHI 760D electrochemical workstation (Shanghai, China) with a conventional three-electrode system including COFTD/GCE, CN/GCE and MNPs/GCE (M=Cu, Fe, Co, Ni) modified electrode as the working electrodes, a platinum wire as the auxiliary electrode and a saturated calomel electrode (SCE, saturated KCl) as the reference electrode. Cyclic voltammetry (CVs) and electrochemical impedance spectroscopy (EIS) were performed in a 0.1 M KCl solution containing 5.0 mM Fe(CN)63-/4-, the frequency range is 0.01-100 KHz, and the voltage was the open circuit voltage. AC impedance was used to analyze the electron transmission rate and the interface state of ion transmission at various stages. The differential pulse voltammetry (DPV) test was performed in 0.2 M N2-statured PBS (pH=7).

Fig. S1. TEM image of CN.

Fig. S2. CVs of CuNPs/CN/GCE at different scan rates from 100 mV s−1 to 500 mV s−1 in 0.2 M N2-statured PBS (pH=7.0) to the detection of DA (A) and UA (C). Fitting curve between current density and the concentration of DA (B), UA (D)

Fig. S3. (A) The plot of peak current density versus Cu2+ concentrations. (B) The plot of peak current density versus different temperatures of carbonization. (C) The plot of peak current density versus different pH. (D) The plot of peak current density versus different concentrations of CuNPs/CN.

Fig. S4. (A) Stability of the CuNPs/CN/GCE for DA and UA detection. (B) Reproducibility of the CuNPs/CN/GCE for DA and UA detection. (C), (D) Selectivity of the CuNPs/CN/GCE for DA and UA detection.

Fig. S5. DPV of CuNPs/CN/GCE, CN/GCE, GCE, COFTD/GCE in 0.2 M PBS solution (pH=7) containing FZ.

Fig. S6. (A) CVs of CuNPs/CN/GCE at different scan rates from 50 mV s−1 to 500 mV s−1 in 0.2 M N2-statured PBS (pH=7.0) to the detection of FZ. (B) Fitting curve between current density and different scan rates.

Fig. S7. (A) Selectivity of the CuNPs/CN/GCE for FZ detection.

Fig. S8. (A) Stability of the CuNPs/CN/GCE for FZ detection. (B) Reproducibility of the CuNPs/CN/GCE for FZ detection.

Table S1. Compared to other DA and UA sensors.

| Electrode | Linear range (μM) | LOD(μM) | Reference |
| --- | --- | --- | --- |
| HNP-PtTi alloy | DA: 25-50 UA: 120-230 | 2.08 5.7 | [1] |
| Au-Cu2O/rGO | DA: 10-90 UA: 100-900 | 3.9 6.5 | [2] |
| pCu2O NS-rGO | DA:0.05-109.0 UA: 1.0-1380.0 | 0.015 0.122 | [3] |
| g-C3N4/Co | DA: 2-400 UA: 1-1000 | 0.4 0.4 | [4] |
| h-BN | DA: 10-300 UA: 10-500 | 5 4 | [5] |
| Au NPs@3D GR/ITO | DA: 0.1-5 DA: 5-60 | 0.1 - | [6] |
| NCCNPs800/GCE | DA:2-69.5 UA:5-192 | 0.34 0.98 | [7] |
| CuNPs/CN/GCE | DA:10-200 UA:100-1100 | 0.042 0.12 | This work |
| FeNPs/CN/GCE | DA:0.1-200 UA:0.5-900 | 0.035 0.145 | This work |
| CoNPs/CN/GCE | DA: 0.15-250 UA: 0.25-900 | 0.042 0.077 | This work |
| NiNPs/CN/GCE | DA: 0.15-250 UA: 0.4-800 | 0.052 0.125 | This work |

Table S2. Compared to other FZ sensors.

| Electrode | Linear range (μM) | LOD (nM) | Reference |
| --- | --- | --- | --- |
| COF@NH2-CNT | 0.2-100 | 77.5 | [8] |
| SnS2-SnO2/graphene/GCE | 0.015–190.5 | 1.42 | [9] |
| Gr/Au/GCE | 1-674 | 64.00 | [10] |
| PAR/GCE | 50-200 | 340 | [11] |
| NiFe2O4/rGO | 0.1-150 | 50 | [12] |
| h-BN/HNTs | 0.009-173.0 | 1 | [13] |
| CuNPs/CN/GCE | 0.06-200 | 20.1 | This work |

References

[1] Zhao DY, Yu GL, Tian KL, Xu CX. A highly sensitive and stable electrochemical sensor for simultaneous detection towards ascorbic acid, dopamine, and uric acid based on the hierarchical nanoporous PtTi alloy. Biosens. Bioelectron. 2016; 82: 119-126.

[2] Aparna TK, Sivasubramanian R, Dar MA. One-pot synthesis of Au-Cu2O/rGO nanocomposite based electrochemical sensor for selective and simultaneous detection of dopamine and uric acid. J. Alloy Compd. 2018; 741: 1130-1141.

[3] Mei L-P, Feng J-J, Wu L, Chen J-R, Shen LG, Xie YL, Wang A-J. A glassy carbon electrode modified with porous Cu2O nanospheres on reduced graphene oxide support for simultaneous sensing of uric acid and dopamine with high selectivity over ascorbic acid. Microchim Acta. 2016; 183(6): 2039-2046.

[4] Wang MM, Zhang MK, Zhu JL, Wang J, Hu LP, Sun TM, Wang M, Tang YF. G‐C3N4/Co nanohybrids for ultra‐sensitive simultaneous detection of uric acid and dopamine. ChemElectroChem. 2020; 7(6): 1373-1377.

[5] Bi Y-S, Liu B, Liu X-Y, Qin Y, Zou BX. A h-BCN for electrochemical sensor of dopamine and uric acid. J Nanomater. 2020; 2020: 1-9.

[6] Wang Z, Yue H Y, Huang S, Yu ZM, Gao X, Chen HT, Wang WQ, Song SS, Guan EH, Zhang HJ. Gold nanoparticles anchored onto three-dimensional graphene: simultaneous voltammetric determination of dopamine and uric acid. Mikrochim Acta. 2019; 186(8): 573.

[7] Guo H, Wang M, Zhao L, Youliwasi N, Liu CG. The effect of Co and N of porous carbon-based materials fabricated via sacrificial templates MOFs on improving DA and UA electrochemical detection. Microporous Mesoporous Mater. 2018; 263: 21-27.

[8] Sun YF, Waterhouse GIN, Xu LH, Qiao XG, Xu ZX. Three-dimensional electrochemical sensor with covalent organic framework decorated carbon nanotubes signal amplification for the detection of furazolidone. Sens. Actuators B. 2020; 321: 128501.

[9] Amalraj AJJ, Umesh NM, Wang SF. Synthesis of core-shell-like structure SnS2-SnO2 integrated with graphene nanosheets for the electrochemical detection of furazolidone drug in furoxone tablet. J Mol Liq. 2020; 313: 113554.

[10] He BS, Du GA. A simple and sensitive electrochemical detection of furazolidone based on an Au nanoparticle functionalized graphene modified electrode. Anal Methods. 2017; 9(30): 4341-4348.

[11] Chen CX, Chen W, Jiang JL, Qian L, Zhang X. Nitrofuran determination in aquaculture water by using poly-alizarin red-modified electrode. J Electrochem Soc. 2019; 166(10): H425-H432.

[12] Ensafi AA, Zandi-Atashbar N, Gorgabi-Khorzoughi M, Rezaei B. Nickel-ferrite oxide decorated on reduced graphene oxide, an efficient and selective electrochemical sensor for detection of furazolidone. IEEE Sens J. 2019; 19(14): 5396-5403.

[13] Kokulnathan T, Wang T-J, Thangapandian M, Alaswad SO. Synthesis and characterization of hexagonal boron nitride/halloysite nanotubes nanocomposite for electrochemical detection of furazolidone. Appl Clay Sci. 2020; 187: 105483.

Corresponding authors: Tel: +86 0791 88120861. E-mail: shouhuicchen@163.com (S. Chen) and yhsong@jxnu.edu.cn or yhsonggroup@hotmail.com (Y. Song).