Preparation and optimization of photocatalytic polyacrylic acid/guar gum/TiO2 hydrogels for absorption and removing of methylene blue under Visible and UV irradiation

Seyyed Masud Naserzadea, Mohsen Shahrousvanda*, Jamshid Mohammadi-Rovshandeha*, Hojjat Basatia

a Caspian Faculty of Engineering, College of Engineering, University of Tehran, P.O. Box 43841-119, Guilan, Rezvanshar, Iran

masud.naserzade@ut.ac.ir

m.shahrousvand@ut.ac.ir

roshandeh@ut.ac.ir

hojjat.basati@ut.ac.ir

Corresponding authors:

Mohsen Shahrousvanda, Caspian Faculty of Engineering, College of Engineering, University of Tehran, P.O. Box 43841-119, Guilan, Rezvanshar, Iran, Email: m.shahrousvand@ut.ac.ir

Jamshid Mohammadi-Rovshandeh, Caspian Faculty of Engineering, College of Engineering, University of Tehran, P.O. Box 43841-119, Guilan, Rezvanshar, Iran, Email: roshandeh@ut.ac.ir

Table 1S. Summary of full factorial design with four factors

| Variables | Units | Coded variables |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | -α | -1 | 0 | 1 | α |
| X1(BDOD) | % | 2 | 4 | 6 | 8 | 10 |
| X2 (GG) | % | 0.5 | 1 | 1.5 | 2 | 2.5 |
| X3 (TiO2) | % | 0 | 5 | 10 | 15 | 20 |
| X4 (pH) |  | 5 | 6 | 7 | 8 | 9 |

Fig. 1S. Images of synthesized hydrogels based on run number

Fig. 2S. Evaluation of swelling factors by design expert program

Fig. 3S. Evaluation of adsorption without UV (in visible light), factors by design expert program

Fig. 4S. Evaluation of adsorption with UV, factors by design expert program

Table 2S. Evaluation of swelling response by experimental design program

| Source | Sum of Squares | df | Mean Square | F-value | p-value |
| --- | --- | --- | --- | --- | --- |
| Model | 1.99E+05 | 14 | 14201.61 | 4.62 | 0.0035 |
| A-BDOD | 18014.4 | 1 | 18014.4 | 5.86 | 0.0296 |
| B-GG | 50508.38 | 1 | 50508.38 | 16.44 | 0.0012 |
| C-TiO2 | 66045.04 | 1 | 66045.04 | 21.5 | 0.0004 |
| D-pH | 7957.04 | 1 | 7957.04 | 2.59 | 0.1298 |
| AB | 689.06 | 1 | 689.06 | 0.2243 | 0.6431 |
| AC | 8695.56 | 1 | 8695.56 | 2.83 | 0.1146 |
| AD | 7612.56 | 1 | 7612.56 | 2.48 | 0.1378 |
| BC | 115.56 | 1 | 115.56 | 0.0376 | 0.849 |
| BD | 5439.06 | 1 | 5439.06 | 1.77 | 0.2046 |
| CD | 6683.06 | 1 | 6683.06 | 2.18 | 0.1624 |
| A² | 2055.11 | 1 | 2055.11 | 0.669 | 0.4271 |
| B² | 217.23 | 1 | 217.23 | 0.0707 | 0.7942 |
| C² | 12639.18 | 1 | 12639.18 | 4.11 | 0.062 |
| D² | 9775.01 | 1 | 9775.01 | 3.18 | 0.0961 |
| Residual | 43006.65 | 14 | 3071.9 |  |  |
| Lack of Fit | 43006.65 | 9 | 4778.52 |  |  |
| Pure Error | 0 | 5 | 0 |  |  |
| Cor Total | 2.42E+05 | 28 |  |  |  |

Table 3S. Evaluation of the adsorption response in Without UV (visible light) by Design Expert program

| Source | Sum of Squares | df | Mean Square | F-value | p-value |
| --- | --- | --- | --- | --- | --- |
| Model | 134.08 | 14 | 9.58 | 5.26 | 0.0019 |
| A-BDOD | 0.0791 | 1 | 0.0791 | 0.0434 | 0.8379 |
| B-GG | 11.65 | 1 | 11.65 | 6.4 | 0.0241 |
| C-TiO2 | 8.28 | 1 | 8.28 | 4.54 | 0.0513 |
| D-pH | 72.79 | 1 | 72.79 | 39.95 | < 0.0001 |
| AB | 2.96 | 1 | 2.96 | 1.63 | 0.223 |
| AC | 6.79 | 1 | 6.79 | 3.73 | 0.074 |
| AD | 0.0309 | 1 | 0.0309 | 0.017 | 0.8982 |
| BC | 1.21 | 1 | 1.21 | 0.6667 | 0.4279 |
| BD | 6.2 | 1 | 6.2 | 3.4 | 0.0864 |
| CD | 7.87 | 1 | 7.87 | 4.32 | 0.0565 |
| A² | 1.32 | 1 | 1.32 | 0.7271 | 0.4082 |
| B² | 5.22 | 1 | 5.22 | 2.87 | 0.1125 |
| C² | 9.41 | 1 | 9.41 | 5.17 | 0.0393 |
| D² | 0.0692 | 1 | 0.0692 | 0.038 | 0.8483 |
| Residual | 25.51 | 14 | 1.82 |  |  |
| Lack of Fit | 25.51 | 9 | 2.83 | 1.79E+10 | < 0.0001 |
| Pure Error | 7.92E-10 | 5 | 1.58E-10 |  |  |
| Cor Total | 159.59 | 28 |  |  |  |

Table 4S. Evaluation of adsorption with UV response by Design Expert program

| Source | Sum of Squares | df | Mean Square | F-value | p-value |
| --- | --- | --- | --- | --- | --- |
| Model | 1.99E+05 | 14 | 14201.61 | 4.62 | 0.0035 |
| A-BDOD | 18014.4 | 1 | 18014.4 | 5.86 | 0.0296 |
| B-GG | 50508.38 | 1 | 50508.38 | 16.44 | 0.0012 |
| C-TiO2 | 66045.04 | 1 | 66045.04 | 21.5 | 0.0004 |
| D-pH | 7957.04 | 1 | 7957.04 | 2.59 | 0.1298 |
| AB | 689.06 | 1 | 689.06 | 0.2243 | 0.6431 |
| AC | 8695.56 | 1 | 8695.56 | 2.83 | 0.1146 |
| AD | 7612.56 | 1 | 7612.56 | 2.48 | 0.1378 |
| BC | 115.56 | 1 | 115.56 | 0.0376 | 0.849 |
| BD | 5439.06 | 1 | 5439.06 | 1.77 | 0.2046 |
| CD | 6683.06 | 1 | 6683.06 | 2.18 | 0.1624 |
| A² | 2055.11 | 1 | 2055.11 | 0.669 | 0.4271 |
| B² | 217.23 | 1 | 217.23 | 0.0707 | 0.7942 |
| C² | 12639.18 | 1 | 12639.18 | 4.11 | 0.062 |
| D² | 9775.01 | 1 | 9775.01 | 3.18 | 0.0961 |
| Residual | 43006.65 | 14 | 3071.9 |  |  |
| Lack of Fit | 29.95 | 9 | 3.33 | 126.01 | < 0.0001 |
| Pure Error | 0 | 5 | 0 |  |  |
| Cor Total | 2.42E+05 | 28 |  |  |  |

Fig. 5S. MB calibration curve from 200 to 800 nm