Supporting Information

Record-High Gain Unipolar Barrier Solar Blind Avalanche Photodetector via Deliberate Lattice and Band Engineering

Qingyi Zhang,1 Ning Li,1 Tao Zhang,1 Dianmeng Dong,1 Yongtao Yang,1 Yuehui Wang,1 Zhengang Dong,1 Jiaying Shen,1 Tianhong Zhou,2 Yuanlin Liang,2 Weihua Tang,1 Yang Zhang,2, a) Zhenping Wu,1, a) Jianhua Hao3, a)

1 State Key Laboratory of Information Photonics and Optical Communications & School of Science, Beijing University of Posts and Telecommunications, Beijing 100876, P. R. China

2 Institute of Modern Optics & Tianjin Key Laboratory of Micro-Scale Optical Information Science and Technology, Nankai University, Tianjin 300071, P. R. China

3 Department of Applied Physics, The Hong Kong Polytechnic University, Hung Hom, Hong Kong, P. R. China

a) Corresponding author. Emails: yangzhang@nankai.edu.cn, zhenpingwu@bupt.edu.cn, and jh.hao@polyu.edu.hk.

Fig. S1. Schematic band diagram of Ga2O3 with other wide bandgap dielectrics.

Fig. S2. Surface topography acquired by atomic force microscopy (AFM).

Fig. S3. XPS measurements of Ga2O3/MgO/Nb:STO and Ga2O3/Nb:STO heterostructures. (a) Ga 2p core level and valence band spectra of Ga2O3 bulk. (b) Mg 2p core level and valence band spectra of MgO bulk. (c) Ti 2p core level and valence band spectra of Nb:STO bulk. (d) Ga 2p, Mg 2p, and Ti 2p core-level spectra of the ultrathin Ga2O3 (3 nm)/MgO (2 nm)/Nb:STO. (e) Ga 2p and Ti 2p core-level spectra of the ultrathin Ga2O3 (3 nm)/Nb:STO.

Fig. S4. Band diagram of Ga2O3/ Nb:STO heterostructure in equilibrium conditions (a) and in avalanche condition (b)

Fig. S5. Avalanche threshold voltage as a function of temperatures in dark.

Fig. S6. Reverse I-V characteristics of the isotype Ga2O3/Nb:STO APD in the dark and under various intensity 254 nm light illumination.

Fig. S7. The responsivity as functions of light intensities and applied bias of the isotype Ga2O3/Nb:STO APD.

Fig. S8. The detectivity as functions of light intensities and applied bias of the isotype Ga2O3/Nb:STO APD.

Supplementary Table 1. Comparison of the figure-of-merits among reported Ga2O3 APD, AlGaN APD and PMT.

| Device structures | Modes | Gain (a.u.) | R (A/W) | D* (Jones) | Bias (V) | Response speed | ref |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ZnO−Ga2O3 Core−Shell | n-n | 2.92×104 | 15.18×103 | 9.91×1014 | -10 | 20 μs/42 μs | [1] |
| β-Ga2O3/SnO2 | n-n | 2.5×105 | 6.3×103 | 1.7×1015 | -10 | 48 μs/102 μs | [2] |
| ITO/Ga2O3 | n-n | 6.8×104 | 5.9×104 | 1.8×1014 | -40 | - | [3] |
| α-Ga2O3/ZnO | n-n | 5224 | 1.1×104 | 2.3×1015 | -40 | 238 μs/3.04 ms | [4] |
| Ga2O3 | Schottky | 1.7×104 | 1.2×105 | 2×1016 | -40 | -/90 ms | [5] |
| AlGaN | p–i–n | 2×104 | 2.55×105 | 6.31×1014 | -140 | - | [6] |
| AlGaN | p–i–n | 2500 | 2.128 | 3.33×1010 | -62 | - | [7] |
| AlGaN | Schottky | 1560 | 666.67 | 1.4×1014 | -68 | - | [8] |
| AlGaN | Schottky | 4000 | 29.4 | 1.54×1012 | -177 | - | [9] |
| PMT | - | >5×105 | >1.4×104 | >5×1016 | -1500 | 4 ns/30 ns | [10] |
| Ga2O3/MgO/Nb:STO | nBn | 5.86×105 | 4.46×105 | 3.28×1017 | -78.1 | 12.4 ns/41.7 μs | This work |

Supplementary References

1	Zhao, B. et al. Solar-blind avalanche photodetector based on single ZnO-Ga2O3 core-shell microwire. Nano Lett 15, 3988-3993, (2015).

2	Mahmoud, W. E. Solar blind avalanche photodetector based on the cation exchange growth of β-Ga2O3/SnO2 bilayer heterostructure thin film. Sol. Energy Mater. Sol. Cells 152, 65-72, (2016).

3	Wang, Y. et al. Ultrahigh gain solar blind avalanche photodetector using an amorphous Ga2O3-based heterojunction. ACS Nano 15, 16654-16663, (2021).

4	Chen, X. et al. Solar-blind photodetector with high avalanche gains and bias-tunable detecting functionality based on metastable phase α-Ga2O3/ZnO isotype heterostructures. ACS Appl. Mater. Interfaces 9, 36997-37005, (2017).

5	Li, Z. et al. High-performance β-Ga2O3 solar-blind schottky barrier photodiode with record detectivity and ultrahigh gain via carrier multiplication process. IEEE Electron Device Lett. 41, 1794-1797, (2020).

6	Wu, H. et al. All AlGaN epitaxial structure solar-blind avalanche photodiodes with high efficiency and high gain. Appl. Phys. Express 9, 052103, (2016).

7	Sun, L., Chen, J., Li, J. & Jiang, H. AlGaN solar-blind avalanche photodiodes with high multiplication gain. Appl. Phys. Lett. 97, 191103, (2010).

8	Tut, T., Gokkavas, M., Inal, A. & Ozbay, E. AlxGa1−xN-based avalanche photodiodes with high reproducible avalanche gain. Appl. Phys. Lett. 90, 163506, (2007).

9	Huang, Z., Li, J., Zhang, W. & Jiang, H. AlGaN solar-blind avalanche photodiodes with enhanced multiplication gain using back-illuminated structure. Appl. Phys. Express 6, 054101, (2013).

10	Photomultiplier tube products from Hamamatsu Photonics, <www.hamamatsu.com/us/en/product/optical-sensors/pmt/pmt_tube-alone/head-on-type.html> (2022).