Supplementary Information for manuscript

Control of Monomeric Vo’s vs. Vo clusters in ZrO2-x for Solar-Light H2 Production from H2O at High-Yield [millimoles gr-1 h-1]

Yiannis Deligiannakis1,4*, Asterios Mantzanis1, Areti Zindrou1, Szymon Smykala3 and  Maria Solakidou1,2

1 Laboratory of Physical Chemistry of Materials & Environment, Department of Physics, University of Ioannina, Ioannina, Greece

2 Laboratory of Biomimetic Catalysis and Hybrid Materials, Department of Chemistry, University of Ioannina, GR45110 Ioannina, Greece

3Institute of Engineering Materials and Biomaterials, Silesian University of Technology, 18a Konarskiego St, 44-100 Gliwice, Poland

4 Institute of Environment & Sustainable Development, University Research Center of Ioannina, GR45110 Ioannina, Greece

* Corresponding author: Yiannis Deligiannakis (ideligia@uoi.gr)

Table S1. FSP-process conditions for the synthesis ZrO2/ZrO2-x materials.

| Materials | Dispersion O2 | Dispersion CH4 | P/D | Sheath O2(L/min) | Sheath N2(L/min) |
| --- | --- | --- | --- | --- | --- |
| [F.O.] | 3 | 0 | 3.0/3.0 | 10 | 0 |
| [3/0.1] | 3 | 0.1 | 3.0/3.1 | - | 10 |
| [3/0.2] | 3 | 0.2 | 3.0/3.2 | - | 10 |
| [2.3/0.7] | 2.3 | 0.7 | 3.0/3.0 | - | 10 |
| [1.3/1.7] | 1.3 | 1.7 | 3.0/3.0 | - | 10 |

Table S2. Structural characteristics of the present FSP-made ZrO2-X materials.

| Material | Calcination T/time (℃)/(Min) | Phase Comp.(%) |  | Crystallite size (nm) |  |  | SSA (m2g-1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | m-ZrO2 | t-ZrO2 | dXRD |  | dBET |  |
| [F.O] | - | 15 | 85 | 20 | 29 | 14 | 72 |
| [3/0.1] | - | 15 | 85 | 19 | 28 | 16 | 64 |
| [3/0.1]-60 | 400/60 | 30 | 70 | 18 | 26 | 17 | 58 |
| [3/0.1]-120 | 400/120 | 35 | 65 | 16 | 24 | 18 | 55 |
| [3/0.2] | - | 15 | 85 | 19 | 28 | 19 | 52 |
| [3/0.2]-30 | 400/30 | 25 | 75 | 19 | 27 | 20 | 50 |
| [3/0.2]-60 | 400/60 | 30 | 70 | 18 | 25 | 21 | 47 |
| [3/0.2]-90 | 400/90 | 30 | 70 | 17 | 24 | 22 | 45 |
| [2.3/0.7] | - | 15 | 85 | 18 | 24 | 23 | 44 |
| [2.3/0.7]-30 | 400/30 | 27 | 73 | 18 | 24 | 24 | 42 |
| [2.3/0.7]-60 | 400/60 | 30 | 70 | 17 | 23 | 25 | 40 |
| [2.3/0.7]-90 | 400/90 | 30 | 70 | 17 | 22 | 27 | 38 |
| [2.3/0.7]-120 | 400/120 | 33 | 67 | 16 | 22 | 27 | 37 |
| [1.3/1.7] | - | 15 | 85 | 17 | 25 | 29 | 34 |
| [1.3/1.7]-60 | 400/60 | 30 | 70 | 16 | 23 | 32 | 31 |

Figure S1. XRD patterns of (a) [3/0.1], (b) [3./0.2], (c) [2.3/0.7] and (d) [1.3/1.7] materials oxidized under ambient air at 4000C for the indicated time-periods (30,60,90,120 minutes).

Figure S2. Raman spectra of [3/0.1], [3/0.2], [2.3/0.7] and [1.3/1.7].

Figure S3. Raman spectra in the Carbon region, indicating the absence carbon-formation in the ΖrO2-x materials made by FSP.

Table S3. Raman bond vibrations for t-ZrO2 and m-ZrO2.

| Tetragonal Zirconia Modes |  | Monoclinic Zirconia Modes |  |  |
| --- | --- | --- | --- | --- |
| Assignment | R.Shift (cm-1) | Assignment | R.Shift (cm-1) | Bond Vibration* |
| Eg | 145 | Ag | 102 | O-O |
| A1g | 264 | Ag | 179 | Zr-Zr |
| B1g | 320 | Bg | 179 | Zr-Zr |
| Eg | 460 | Ag | 190 | Zr-Zr |
| B1g | 606 | Bg | 224 | Zr-O |
| Eg | 641 | Ag | 270 | Zr-Zr |
| - | - | Ag | 305 | Zr-O |
| - | - | Bg | 334 | Zr-O |
| - | - | Ag | 348 | O-O |
| - | - | Bg | 381 | O-O |
| - | - | Bg | 385 | O-O |
| - | - | Ag | 476 | O-O |
| - | - | Bg | 505 | O-O |
| - | - | Bg | 536 | O-O |
| - | - | Ag | 556 | O-O |
| - | - | Bg | 616 | O-O |
|  | - | Ag | 637 | O-O |

Table S4. Raman shifts of ZrO2-x materials.

| Material | Mode(cm-1) | Shift(cm-1) | Assignment |
| --- | --- | --- | --- |
| [3.0/0.1] | 264 | -3 | Zr-Zr |
|  | 320 | -6 | - |
|  | 641 | -9 | - |
| [3.0/0.2] | 476 | +4 | O-O |
| [2.3/0.7] | 320 | -5 | - |
|  | 476 | +3 | - |
|  | 641 | -6 | - |
| [1.3/1.7] | 102 | -7 | O-O |
|  | 145 | -1 | - |
|  | 179 | -5 | Zr-Zr |
|  | 264 | -8 | Zr-Zr |
|  | 381 | -10 | O-O |
|  | 476 | -2 | O-O |
|  | 554 | -5 | O-O |
|  | 641 | -21 | - |

Figure S4. XPS spectra of the Zr doublet of (a) [3/0.1], (b) [3.0/0.2], (c) [2.3/0.7] and (d) [1.3/1.7].

(b)bn

(a)bn

Figure S5. O1s XPS spectra of material [2.3/0.7] calcined for (a) 90 and (b) 120 min.

Figure S6. UV-Vis/DRS spectra of calcined (a) [3/0.1], (b) [3.0/0.2], (c) [2.3/0.7] and (d) [1.3/1.7] materials.

Table S5. EPR parameters for Vo signals in, ([3/0.1], [3/0.2], [2.3/0.7] and [1.3/1.7]).

| Material | Monomer |  |  | ΔH(±0.1G) | Cluster | ΔH(±0.1G) |
| --- | --- | --- | --- | --- | --- | --- |
|  | gzz | gyy | gxx |  | giso |  |
| 3/0.1 | 2.0072 | 2.0037 | 2.0011 | 5 | - | - |
| 400-60 | 2.0059 | 2.0042 | 2.0020 | 6 | - | - |
| 400-120 | 2.0060 | 2.0046 | 2.0034 | 5.2 | - | - |
| 3/0.2 | 2.0072 | 2.0037 | 2.0011 | 4.8 | 2.0028 | 6.5 |
| 400-60 | 2.0078 | 2.0041 | 2.0008 | 6.8 | - | - |
| 400-90 | 2.0076 | 2.0040 | 2.0007 | 8.6 | - | - |
| 400-120 | 2.0060 | 2.0043 | 2.0038 | 5.1 | - | - |
| 2.3/0.7 | 2.0072 | 2.0037 | 2.0011 | 4.8 | 2.0028 | 6.5 |
| 400-60 | 2.0072 | 2.0037 | 2.0011 | 4.8 | 2.0028 | 6.5 |
| 400-90 | 2.0078 | 2.0045 | 2.0020 | 5.8 | - |  |
| 400-120 | 2.0072 | 2.0041 | 1.9993 | 5.3 | - |  |
| 1.3/1.7 | 2.0072 | 2.0037 | 2.0011 | - | 2.0028 | 6.5 |
| 400-60 | 2.0072 | 2.0037 | 2.0011 | 4.8 | 2.0028 | 6.5 |
| 400-90 | 2.0072 | 2.0037 | 2.0011 | 4.8 | 2.0028 | 6.5 |
| 400-120 | 2.0072 | 2.0037 | 2.0011 | 4.8 | 2.0028 | 6.5 |

Figure S7. Experimental and fitted EPR spectra of [1.3/1.7] calcined at 400 ℃ for (a) 60 min and (b) 120 min.

Table S6. EPR Quantitation of VO centers in μmolg-1 of [3/0.1], [3/0.2], [2.3/0.7], [1.3/1.7] and calculation of VO / Zr atom ratio.

| Materials | μmolg-1 x103 (VO) | VO/Ζr-atom (x104) |
| --- | --- | --- |
| [3/0.1] | 21 | 22 |
| [3/0.2] | 24 | 25 |
| [2.3/0.7] | 32 | 35 |
| [1.3/1.7] | 148 | 159 |

Figure S8. (a) Catalytic Reuse experiments of material [2.3/0.7]-90, (b) X-Ray Diffraction patterns and (c) DRS-UV/Vis spectra after 4 catalytic cycles.

Theoretical DFT Calculations: Theoretical calculations were conducted for the t-ZrO2 phase, using DFT as implemented in the Quantum Espresso software1. The projector augmented-wave (PAW) method was used to describe the core pseudopotential and the generalized gradient approximation (GGA) as simplified by Perdew, Burke, and Ernzerhof (PBE) was used for exchange-correlation effects. Ultrasoft pseudopotentials containing 12 valence electrons were used for Zr ([Kr] 5s2 5p0 4d2) and 6 valence electrons for O ([He] 2s2 2p4). A plane-wave energy cutoff of 45.551 Ry was used. Using the B.F.G.S routine, the structure was relaxed until the forces acting on each atom were <10-3 meV/Å. For geometry optimization and electronic structure calculations, (1 × 1 × 2) and (2 × 2 × 5) Monkhorst-Pack k-point grids were used respectively. Considering the strong correlations in transition metal oxides, we used the DFT+U approximation in the approach of Cococcioni and de Gironcoli2 with a U-value of 4 eV applied on all structures.

Figure S9. Theoretical DFT calculated electron Density of States for (a) ZrO2, (b) ZrO2-(with one Vo per 9-unit cells) and (c) ZrO2-(with two Vo per 9-unit cells). The green-bar in (a) marks the Eg-value for pristine ZrO2. In (b), (c) is re-marked to facilitate the visualization of the band-gap narrowing and the creation of DOS tail in the CB-bottom. (Right panels) the 9-unit cell structures used to calculate the DOS by DFT.

References:

1.	Giannozzi, P. et al. QUANTUM ESPRESSO: a modular and open-source software project for quantum simulations of materials. J. Phys.: Condens. Matter 21, 395502 (2009).

2.	Cococcioni, M. & de Gironcoli, S. Linear response approach to the calculation of the effective interaction parameters in the LDA + U method. Phys. Rev. B 71, 035105 (2005).