SUPPORTING INFORMATION FILE

Assessing the time dependence of AOPs on the surface properties of Polylactic Acid

Charalampia Kalogirou a,b, Oliver Höfft c, Anna Gödde a, Pavlos K. Pandis b, 
Christos Argirusis a,b , and Georgia Sourkouni a,*

* Corresponding author: cogsa@tu-clausthal.de

a Clausthal Centre for Materials Technology (CZM), Clausthal University of Technology, Leibnizstr. 9, 38678 Clausthal-Zellerfeld, Germany

b School of Chemical Engineering, National Technical University of Athens, 9 Heroon Polytechneiou St., Zografou Campus, 15773 Athens, Greece

c Institute for Electrochemistry, Clausthal University of Technology, 38678 Clausthal-Zellerfeld, Germany

Figure S1: The XPS results showing different ratios of functional groups and elements for each sample treated at 20kHz Ultrasounds at different times.

Figure S2: The XPS results showing different ratios of functional groups and elements for each sample treated at 860kHz Ultrasounds at different times.

Figure S3: The XPS results showing different ratios of functional groups and elements for each sample treated with UVA irradiation at different times.

Figure S4: IR spectra comparison between the samples that have been treated with UVA irradiation and the Reference one.

Figure S5: IR spectra comparison between the samples that have been treated at 20kHz Ultrasounds and the Reference one.

Figure S6: IR spectra comparison between the samples that have been treated at 860kHz Ultrasounds and the Reference one.

Table S1: Results for the surface roughness of all treatment methods for 1, 3 and 6 hours by the characterization method CLSM

| Treatment | Reference | UVA irradiation |  |  | Ultrasounds at 20kHz |  |  | Ultrasounds at 860kHz |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Time |  | 1h | 3h | 6h | 1h | 3h | 6h | 1h | 3h | 6h |
| Ra (nm) | 9.102 | 9.290 | 8.792 | 11.925 | 8.634 | 8.029 | 6.082 | 11.052 | 7.463 | 8.628 |
| Rq (nm) | 11.736 | 11.689 | 11.130 | 15.264 | 11.061 | 10.238 | 7.723 | 13.375 | 9.479 | 11.040 |

Figure S7: CLSM 3D images for PLA Reference sample

Figure S8: CLSM 3D images for PLA sample treated at 20kHz Ultrasounds for 1 hour.

Figure S9: CLSM 3D images for PLA sample treated at 20kHz Ultrasounds for 3 hours.

Figure S10: CLSM 3D images for PLA sample treated at 20kHz Ultrasounds for 6 hours.

Figure S11: CLSM 3D images for PLA sample treated at 860kHz Ultrasounds for 1 hour.

Figure S12: CLSM 3D images for PLA sample treated at 860kHz Ultrasounds for 3 hours.

Figure S13: CLSM 3D images for PLA sample treated at 860kHz Ultrasounds for 6 hours.

Figure S14: CLSM 3D images for PLA samples treated with UVA irradiation for 1 hour.

Figure S15: CLSM 3D images for PLA samples treated with UVA irradiation for 3 hours.

Figure S16: CLSM 3D images for PLA samples treated with UVA irradiation for 6 hours.