# Photo-engineered optoelectronic properties of indium tin oxide via reactive laser annealing

James A. Hillier1, Panos Patsalas2, Dimitrios Karfaridis2, Sophie Camelio3, Wayne Cranton4, Alexei V. Nabok4, Christopher J. Mellor5, Demosthenes C. Koutsogeorgis1, and Nikolaos Kalfagiannis*1

1 Nottingham Trent University, School of Science and Technology, Nottingham, NG11 8NS, UK.

2 Aristotle University of Thessaloniki, Department of Physics, Thessaloniki, GR-54124, Greece.

3 Institut Pprime, UPR 3346 CNRS-Université de Poitiers, Poitiers, France.

4 Sheffield Hallam University, Materials and Engineering Research Institute, Sheffield, S1 1WB, UK.

5 The University of Nottingham, School of Physics and Astronomy, Nottingham, NG7 2RD, UK

* nikolaos.kalfagiannis@ntu.ac.uk

Contents

Section A: Thin Film Uniformity	2

Section B: Optical data	3

Parameterised Results	11

Section C: Ellipsometric modelling	14

Oscillator Functions	14

Justification of SE model	14

Section D: XRD data and analysis	15

XRD spectra for all ITO films	15

XRD analysis	16

Section E: XPS and EDX data and Analysis	17

XPS Data and fits	17

EDX data and analysis	18

References	19

Section A: Thin Film Uniformity

For the seed ITO films, some slight non-uniformity in the thickness and ρ4pp was present across the 4'' wafers. This non-uniformity introduces a problem for further LA experiments which require a set of laser-processed “spots” of ~1×1 cm across the full wafer. For example, deviations in the seed film may be mistaken for laser-induced modifications from the seed film to the annealed film. To account for this, we investigated into the non-uniformity of the film. After deposition of the ITO films, the wafers were cut into ~90, ~8×8 mm2 die. The die were cut along their long edge for each cut, into to reduce any stresses introduce to the film. The x and y position, relative to the sample centre, was noted and tracked for each die. Following this, we measured the visible reflectance, RVis, IR transmittance, TIR, for each die in order to determine the film thickness, dfilm, “optical” resistivity, ρopt, “optical” mean free time, τopt,and the optical constants, ε1 and ε2. The thickness, as determined from fitting of RVis, was used to calculate the collinear resistivity, ρ4pp, from four-point probe (4pp) measurements of the sheet resistance. Furthermore, dfilm, the UV oscillators, and the high-frequency permittivity, ε∞, were fixed during the fitting of IRT data. The properties of each die were plotted against their x and y position to produce a set of colour maps. The deviation is calculated as the percent difference of the die to the average value. We calculate of the “optical” carrier concentration, Nopt, and mobility, μopt, via Eq. 2 and Eq. 3, respectively, from which an understanding of the variations in the transport mechanisms (that are more fundamental properties than the resistivity) can be built. The absolute value of the effective mass (assumed to be to be 0.30 me)1 does not affect the resulting % deviation, but it is important to note that variations in Nopt and μopt may partially originate from variations in me*.

Figure S1a-d presents a colour map of the deviation in (a) dfilm, (b) ρopt, (c) Nopt, and (d) μopt, across the 4'' wafer. In Fig. A1a, we observe that the thickness range does not deviate more than 8 nm (7.2%) across the wafer and the standard deviation is only 2 nm (1.8%). It is well known that there exist a thickness dependence on the resistivity of ITO films2 Furthermore, the change in thickness across the wafer implies a change in the sputtering rate, which has been noted to drastically affect the resulting film properties.3,4 In Figure S1b, we observe a minor deviation in ρ4pp across the wafer, where the average resistivity is lower towards the center. From Figure S1c-d, it is found that the decrease in ρopt towards the centre of the wafer arises primarily from an increase in μopt from ~15 cm2/Vs to nearly twice the edge value of ~25 cm2/Vs at the centre. The carrier concentration remains near constant with a value of ~4.2 cm-3. It is apparent that the change in μopt gives rise to the decreasing resistivity with sputtering rate. As the film is amorphous across the entire wafer (Section D), structural alterations cannot be used to explain the change in μopt across the film. Instead, it is noted that for ITO films with N>~4×1020cm-3, the dominant scattering mechanism is ionized cluster scattering (ICS) that has a very large scattering coefficient for ITO films and thus the mobility is highly sensitive to N.5,6 Because of this observed disuniformity across the wafer, the die selected for further processing were limited to an area of the film where the deviation was minimal. In this area, two die were selected to cover the range of resistivity exhibited by this cluster.

Figure S1. Colour map of the percentile deviation from the average centre value in (a) the film thickness, dfilm, and the “optical” (b) resistivity, ρopt, (c) carrier concentration, Nopt, and (d) carrier mobility, μopt, of the ITO thin film coating across the 4'' Si wafer

Section B: Optical data

Figure S2. Fitting report for the “1st” seed ITO thin film with a resistivity at the upper end of the range exhibited by the seed films selected for further processing: (a) Ψ(E) (blue squares) and Δ(E) (red squares) at incident angles of 55° (darker shade), 60° (normal shade) and 65° (lighter shade). (b) The corresponding IR transmission, TIR(E), (blue squares) and visible reflection, RVIS(E), (red squares). In (a) and (b), the solid green lines indicate the fit to each collected data set. (c) The corresponding, as-fit, real and imaginary parts of the complex permittivity, εE=ε1E+iε2E, (solid red and blue lines, respectively). Note the logarithmic scale in the x-axis of (a), (b) and (c). The vertical dashed black line indicates the boundary between the IR and NIR-VIS-UV ranges covered by the two ellipsometers.

Figure S3. Fitting report for the “2nd” seed ITO thin film with a resistivity at the lower end of the range exhibited by the seed films selected for further processing: (a) Ψ(E) (blue squares) and Δ(E) (red squares) at incident angles of 55° (darker shade), 60° (normal shade) and 65° (lighter shade). (b) The corresponding IR transmission, TIR(E), (blue squares) and visible reflection, RVIS(E), (red squares). In (a) and (b), the solid green lines indicate the fit to each collected data set. (c) The corresponding, as-fit, real and imaginary parts of the complex permittivity, εE=ε1E+iε2E, (solid red and blue lines, respectively). Note the logarithmic scale in the x-axis of (a), (b) and (c). The vertical dashed black line indicates the boundary between the IR and NIR-VIS-UV ranges covered by the two ellipsometers.

Figure S4. Fitting report for the ITO thin film: subject to single-pulse ReLA at 25 mJcm-2 within a 100 psig pressured atmosphere of 5% H2 in N2: (a) Ψ(E) (blue squares) and Δ(E) (red squares) at incident angles of 55° (darker shade), 60° (normal shade) and 65° (lighter shade). (b) The corresponding IR transmission, TIR(E), (blue squares) and visible reflection, RVIS(E), (red squares). In (a) and (b), the solid green lines indicate the fit to each collected data set. (c) The corresponding, as-fit, real and imaginary parts of the complex permittivity, εE=ε1E+iε2E, (solid red and blue lines, respectively). Note the logarithmic scale in the x-axis of (a), (b) and (c). The vertical dashed black line indicates the boundary between the IR and NIR-VIS-UV ranges covered by the two ellipsometers.

Figure S5. Fitting report for the ITO thin film: subject to single-pulse ReLA at 25 mJcm-2 within a 100 psig pressured atmosphere of 100% O2: (a) Ψ(E) (blue squares) and Δ(E) (red squares) at incident angles of 55° (darker shade), 60° (normal shade) and 65° (lighter shade). (b) The corresponding IR transmission, TIR(E), (blue squares) and visible reflection, RVIS(E), (red squares). In (a) and (b), the solid green lines indicate the fit to each collected data set. (c) The corresponding, as-fit, real and imaginary parts of the complex permittivity, εE=ε1E+iε2E, (solid red and blue lines, respectively). Note the logarithmic scale in the x-axis of (a), (b) and (c). The vertical dashed black line indicates the boundary between the IR and NIR-VIS-UV ranges covered by the two ellipsometers.

Figure S6. Fitting report for the ITO thin film: subject to single-pulse ReLA at 50 mJcm-2 within a 100 psig pressured atmosphere of 5% H2 in N2: (a) Ψ(E) (blue squares) and Δ(E) (red squares) at incident angles of 55° (darker shade), 60° (normal shade) and 65° (lighter shade). (b) The corresponding IR transmission, TIR(E), (blue squares) and visible reflection, RVIS(E), (red squares). In (a) and (b), the solid green lines indicate the fit to each collected data set. (c) The corresponding, as-fit, real and imaginary parts of the complex permittivity, εE=ε1E+iε2E, (solid red and blue lines, respectively). Note the logarithmic scale in the x-axis of (a), (b) and (c). The vertical dashed black line indicates the boundary between the IR and NIR-VIS-UV ranges covered by the two ellipsometers.

Figure S7. Fitting report for the ITO thin film: subject to single-pulse ReLA at 50mJcm-2 within a 100 psig pressured atmosphere of 100% O2: (a) Ψ(E) (blue squares) and Δ(E) (red squares) at incident angles of 55° (darker shade), 60° (normal shade) and 65° (lighter shade). (b) The corresponding IR transmission, TIR(E), (blue squares) and visible reflection, RVIS(E), (red squares). In (a) and (b), the solid green lines indicate the fit to each collected data set. (c) The corresponding, as-fit, real and imaginary parts of the complex permittivity, εE=ε1E+iε2E, (solid red and blue lines, respectively). Note the logarithmic scale in the x-axis of (a), (b) and (c). The vertical dashed black line indicates the boundary between the IR and NIR-VIS-UV ranges covered by the two ellipsometers.

Figure S8. Fitting report for the ITO thin film: subject to single-pulse ReLA at 75 mJcm-2 within a 100 psig pressured atmosphere of 5% H2 in N2: (a) Ψ(E) (blue squares) and Δ(E) (red squares) at incident angles of 55° (darker shade), 60° (normal shade) and 65° (lighter shade). (b) The corresponding IR transmission, TIR(E), (blue squares) and visible reflection, RVIS(E), (red squares). In (a) and (b), the solid green lines indicate the fit to each collected data set. (c) The corresponding, as-fit, real and imaginary parts of the complex permittivity, εE=ε1E+iε2E, (solid red and blue lines, respectively). Note the logarithmic scale in the x-axis of (a), (b) and (c). The vertical dashed black line indicates the boundary between the IR and NIR-VIS-UV ranges covered by the two ellipsometers.

Figure S9. Fitting report for the ITO thin film: subject to single-pulse ReLA at 75 mJcm-2 within a 100 psig pressured atmosphere of 100% O2: (a) Ψ(E) (blue squares) and Δ(E) (red squares) at incident angles of 55° (darker shade), 60° (normal shade) and 65° (lighter shade). (b) The corresponding IR transmission, TIR(E), (blue squares) and visible reflection, RVIS(E), (red squares). In (a) and (b), the solid green lines indicate the fit to each collected data set. (c) The corresponding, as-fit, real and imaginary parts of the complex permittivity, εE=ε1E+iε2E, (solid red and blue lines, respectively). Note the logarithmic scale in the x-axis of (a), (b) and (c). The vertical dashed black line indicates the boundary between the IR and NIR-VIS-UV ranges covered by the two ellipsometers.

Figure S10. Fitting report for the ITO thin film: subject to single-pulse ReLA at 100 mJcm-2 within a 100 psig pressured atmosphere of 5% H2 in N2: (a) Ψ(E) (blue squares) and Δ(E) (red squares) at incident angles of 55° (darker shade), 60° (normal shade) and 65° (lighter shade). (b) The corresponding IR transmission, TIR(E), (blue squares) and visible reflection, RVIS(E), (red squares). In (a) and (b), the solid green lines indicate the fit to each collected data set. (c) The corresponding, as-fit, real and imaginary parts of the complex permittivity, εE=ε1E+iε2E, (solid red and blue lines, respectively). Note the logarithmic scale in the x-axis of (a), (b) and (c). The vertical dashed black line indicates the boundary between the IR and NIR-VIS-UV ranges covered by the two ellipsometers.

Figure S11. Fitting report for the ITO thin film: subject to single-pulse ReLA at 100 mJcm-2 within a 100 psig pressured atmosphere of 100% O2: (a) Ψ(E) (blue squares) and Δ(E) (red squares) at incident angles of 55° (darker shade), 60° (normal shade) and 65° (lighter shade). (b) The corresponding IR transmission, TIR(E), (blue squares) and visible reflection, RVIS(E), (red squares). In (a) and (b), the solid green lines indicate the fit to each collected data set. (c) The corresponding, as-fit, real and imaginary parts of the complex permittivity, εE=ε1E+iε2E, (solid red and blue lines, respectively). Note the logarithmic scale in the x-axis of (a), (b) and (c). The vertical dashed black line indicates the boundary between the IR and NIR-VIS-UV ranges covered by the two ellipsometers.

Figure S12. Fitting report for the ITO thin film: subject to single-pulse ReLA at 125 mJcm-2 within a 100 psig pressured atmosphere of 5% H2 in N2: (a) Ψ(E) (blue squares) and Δ(E) (red squares) at incident angles of 55° (darker shade), 60° (normal shade) and 65° (lighter shade). (b) The corresponding IR transmission, TIR(E), (blue squares) and visible reflection, RVIS(E), (red squares). In (a) and (b), the solid green lines indicate the fit to each collected data set. (c) The corresponding, as-fit, real and imaginary parts of the complex permittivity, εE=ε1E+iε2E, (solid red and blue lines, respectively). Note the logarithmic scale in the x-axis of (a), (b) and (c). The vertical dashed black line indicates the boundary between the IR and NIR-VIS-UV ranges covered by the two ellipsometers.

Figure S13. Fitting report for the ITO thin film: subject to single-pulse ReLA at 125 mJcm-2 within a 100 psig pressured atmosphere of 100% O2: (a) Ψ(E) (blue squares) and Δ(E) (red squares) at incident angles of 55° (darker shade), 60° (normal shade) and 65° (lighter shade). (b) The corresponding IR transmission, TIR(E), (blue squares) and visible reflection, RVIS(E), (red squares). In (a) and (b), the solid green lines indicate the fit to each collected data set. (c) The corresponding, as-fit, real and imaginary parts of the complex permittivity, εE=ε1E+iε2E, (solid red and blue lines, respectively). Note the logarithmic scale in the x-axis of (a), (b) and (c). The vertical dashed black line indicates the boundary between the IR and NIR-VIS-UV ranges covered by the two ellipsometers.

Figure S14. Fitting report for the ITO thin film: subject to single-pulse ReLA at 125 mJcm-2 within a 100 psig pressured atmosphere of 5% O2 in N2: (a) Ψ(E) (blue squares) and Δ(E) (red squares) at incident angles of 55° (darker shade), 60° (normal shade) and 65° (lighter shade). (b) The corresponding IR transmission, TIR(E), (blue squares) and visible reflection, RVIS(E), (red squares). In (a) and (b), the solid green lines indicate the fit to each collected data set. (c) The corresponding, as-fit, real and imaginary parts of the complex permittivity, εE=ε1E+iε2E, (solid red and blue lines, respectively). Note the logarithmic scale in the x-axis of (a), (b) and (c). The vertical dashed black line indicates the boundary between the IR and NIR-VIS-UV ranges covered by the two ellipsometers.

Figure S15. (a-c) Real and (d-f) imaginary parts of the complex permittivity, εE=ε1E+iε2E, report for the seed ITO thin films (black and grey lines) and those: subject to single-pulse ReLA at 25-125 mJcm-2 (red to blue lines in rainbow order) within a 100 psig pressured atmosphere of (a, d) 5% H2 in N2, (b, e) 5% O2 in N2, and (c, f) 100% O2, respectively. The inset in (a) and (b) present a close-up of the point where ε1E crosses the x-axis. The blue vertical lines indicate the plasma energy of the films annealed at 125 mJcm-2. Note the logarithmic scale in the x-axis of (a), (b) and (c).

Parameterised Results

Table S1. Numerical values for each parameter used to calculate the optical constants of the seed ITO films and the ITO film subject to LA at 125 mJcm-2 into an ambient environment of 5% O2 in N2.

| Environment |  | n/a – Seed ITO (Low ρopt) |  | n/a – Seed ITO (High ρopt) |  | 5% O2 in N2 |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Fluence | mJcm-2 |  |  |  |  | 124 | 2 |
| Ellipsometrically Determined Parameters |  |  |  |  |  |  |  |
| MSE |  | 8.139 |  | 8.303 |  | 9.959 |  |
| Parameter | Unit | Value | Error | Value | Error | Value | Error |
| Thickness | nm | 127.58 | 0.04 | 131.36 | 0.05 | 129.95 | 0.06 |
| Surface Roughness | nm | 5.09 | 0.07 | 5.32 | 0.08 | 5.35 | 0.07 |
| High-Frequency Permittivity |  | 3.365 | 0.003 | 3.287 | 0.003 | 3.293 | 0.004 |
| “Optical” Resistivity | ×10-4 Ωcm | 5.40 | 0.01 | 4.89 | 0.01 | 4.94 | 0.01 |
| “Optical” Mean Free Time | fs | 4.863 | 0.006 | 5.771 | 0.009 | 4.945 | 0.008 |
| Inhomogeneity | % | 10.9 | 0.2 | 12.5 | 0.2 | 11.2 | 0.3 |
| 1st Oscillator (Gaussian) |  |  |  |  |  |  |  |
| Parameter | Unit | Value | Error | Value | Error | Value | Error |
| Amplitude |  | 42 | 1 | 42 | 1 |  |  |
| Broadening | eV | 0.0352 | 0.0008 | 0.0294 | 0.0007 |  |  |
| Energy | eV | 0.045 | -- | 0.045 | -- | 0.045 | -- |
| 2nd Oscillator (Lorentz) |  |  |  |  |  |  |  |
| Parameter | Unit | Value | Error | Value | Error | Value | Error |
| Amplitude |  | 7.46 | 0.05 | 9.51 | 0.07 |  |  |
| Broadening | eV | 0.410 | 0.002 | 0.346 | 0.002 |  |  |
| Energy | eV | 4.229 | -- | 4.229 | -- | 4.229 | -- |
| Non-Optically Measured Parameters |  |  |  |  |  |  |  |
| Parameter | Unit | Value | Error | Value | Error | Value | Error |
| DC Resistivity (Van der Pauw) | ×10-4 Ωcm | 4.27 | 0.04 | 4.87 | 0.05 | 4.40 | 0.02 |
| DC Resistivity (4pp) | ×10-4 Ωcm | 4.2 | 0.1 | 5.0 | 0.3 | 4.2 | 0.3 |
| “Hall” Carrier Concentration | ×1020 cm-3 | 4.3 | 0.3 | 4.8 | 0.3 | 5.5 | 0.9 |
| Calculated Parameters |  |  |  |  |  |  |  |
| Parameter | Unit | Value | Error | Value | Error | Value | Error |
| Effective carrier mass ratio* |  | 0.355 | 0.007 | 0.348 | 0.007 | 0.37 | 0.02 |
| “Optical” Carrier Concentration | ×1020 cm-3 | 4.8 | 0.1 | 4.38 | 0.09 | 5.3 | 0.3 |
| “Optical” Carrier Mobility | cm2/Vs | 24.1 | 0.5 | 29.1 | 0.6 | 24 | 1 |
| “Hall” Carrier Mobility | cm2/Vs | 26.99 | 0.02 | 33.71 | 0.02 | 25.8 | 0.2 |
| Screened plasma energy | eV | 0.6655 | 0.0003 | 0.6484 | 0.0003 | 0.6972 | 0.0009 |

* The effective carrier mass ratio is calculated from the Hall carrier concentration by accounting for non-parabolicity in the conduction band.6

Table S2. Numerical values for each parameter used to calculate the optical constants of the ITO films subject to LA in 5% H2 in N2.

| Environment |  | 5% H2 in N2 |  |  |  | 5% H2 in N2 |  |  | 5% H2 in N2 |  |  |  | 5% H2 in N2 |  | 5% H2 in N2 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fluence | mJcm-2 | 25.1 | 0.3 |  | 49.7 |  |  | 0.8 | 75 | 1 |  | 100 |  | 2 | 124 | 2 |
| Ellipsometrically Determined Parameters |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| MSE |  | 14.91 |  |  |  | 9.09 |  |  | 9.35 |  |  |  | 9.30 |  | 14.66 |  |
| Parameter | Unit | Value |  | Error |  | Value | Error |  | Value |  | Error |  | Value | Error | Value | Error |
| Thickness | nm | 130.76 |  | 0.07 |  | 130.26 | 0.04 |  | 130.27 |  | 0.04 |  | 131.33 | 0.04 | 126.49 | 0.09 |
| Surface Roughness | nm | 4.1 |  | 0.1 |  | 5.19 | 0.07 |  | 5.00 |  | 0.07 |  | 5.16 | 0.07 | 6.0 | 0.1 |
| High-Frequency Permittivity |  | 3.404 |  | 0.005 |  | 3.319 | 0.003 |  | 3.336 |  | 0.003 |  | 3.311 | 0.003 | 3.368 | 0.007 |
| “Optical” Resistivity | ×10-4 Ωcm | 5.29 |  | 0.02 |  | 5.09 | 0.01 |  | 5.16 |  | 0.01 |  | 4.74 | 0.01 | 5.22 | 0.02 |
| “Optical” Mean Free Time | fs | 5.17 |  | 0.01 |  | 5.420 | 0.008 |  | 5.274 |  | 0.008 |  | 5.748 | 0.009 | 4.41 | 0.01 |
| Inhomogeneity | % | 2.9 |  | 0.3 |  | 11.0 | 0.2 |  | 9.9 |  | 0.2 |  | 8.7 | 0.2 | 9.5 | 0.5 |
| 1st Oscillator (Gaussian) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Parameter | Unit | Value |  | Error |  | Value | Error |  | Value |  | Error |  | Value | Error | Value | Error |
| Amplitude |  | 42 |  | 1 |  | 42 | 1 |  | 42 |  | 1 |  | 42 | 1 | 42 | 1 |
| Broadening | eV | 0.0294 |  | 0.0007 |  | 0.032 | 0.001 |  | 0.0303 |  | 0.0007 |  | 0.0314 | 0.0007 | 0.0307 | 0.0007 |
| Energy | eV | 0.045 |  | -- |  | 0.045 | -- |  | 0.045 |  | -- |  | 0.045 | -- | 0.045 | -- |
| 2nd Oscillator (Lorentz) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Parameter | Unit | Value |  | Error |  | Value | Error |  | Value |  | Error |  | Value | Error | Value | Error |
| Amplitude |  | 7.55 |  | 0.05 |  | 7.46 | 0.05 |  | 9.51 |  | 0.07 |  | 6.84 | 0.08 | 8.60 | 0.06 |
| Broadening | eV | 0.407 |  | 0.002 |  | 0.410 | 0.002 |  | 0.346 |  | 0.002 |  | 0.417 | 0.004 | 0.368 | 0.002 |
| Energy | eV | 4.229 |  | -- |  | 4.229 | -- |  | 4.229 |  | -- |  | 4.229 | -- | 4.229 | -- |
| Non-Optically Measured Parameters |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Parameter | Unit | Value |  | Error |  | Value | Error |  | Value |  | Error |  | Value | Error | Value | Error |
| DC Resistivity (Van der Pauw) | ×10-4 Ωcm | 4.69 |  | 0.02 |  | 4.42 | 0.07 |  | 4.59 |  | 0.07 |  | 4.15 | 0.07 | 4.4 | 0.2 |
| DC Resistivity (4pp) | ×10-4 Ωcm | 4.9 |  | 0.3 |  | 4.7 | 0.3 |  | 4.7 |  | 0.3 |  | 4.1 | 0.5 | 3.8 | 0.3 |
| “Hall” Carrier Concentration | ×1020 cm-3 | 4.8 |  | 0.3 |  | 4.4 | 0.2 |  | 4.6 |  | 0.2 |  | 4.4 | 0.3 | 5.7 | 0.7 |
| Calculated Parameters |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Parameter | Unit | Value |  | Error |  | Value | Error |  | Value |  | Error |  | Value | Error | Value | Error |
| Effective carrier mass ratio* |  | 0.356 |  | 0.009 |  | 0.349 | 0.005 |  | 0.353 |  | 0.005 |  | 0.349 | 0.007 | 0.37 | 0.02 |
| “Optical” Carrier Concentration | ×1020 cm-3 | 4.6 |  | 0.1 |  | 4.43 | 0.07 |  | 4.56 |  | 0.07 |  | 4.6 | 0.1 | 5.7 | 0.2 |
| “Optical” Carrier Mobility | cm2/Vs | 25.8 |  | 0.6 |  | 27.6 | 0.4 |  | 26.6 |  | 0.4 |  | 29.3 | 0.6 | 21.2 | 0.9 |
| “Hall” Carrier Mobility | cm2/Vs | 27.759 |  | 0.007 |  | 32.41 | 0.02 |  | 29.46 |  | 0.02 |  | 34.21 | 0.04 | 24.6 | 0.1 |
| Screened plasma energy | eV | 0.6592 |  | 0.0001 |  | 0.6573 | 0.0003 |  | 0.6614 |  | 0.0002 |  | 0.6636 | 0.0004 | 0.7178 | 0.0004 |

* The effective carrier mass ratio is calculated from the Hall carrier concentration by accounting for non-parabolicity in the conduction band.6

Table S3. Numerical values for each parameter used to calculate the optical constants of the ITO films subject to LA in 100% O2.

| Environment |  | 100% O2 |  | 100% O2 |  | 100% O2 |  | 100% O2 |  | 100% O2 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fluence | mJcm-2 | 25.1 | 0.3 | 49.7 | 0.8 | 75 | 1 | 100 | 2 | 124 | 2 |
| Ellipsometrically Determined Parameters |  |  |  |  |  |  |  |  |  |  |  |
| MSE |  | 14.91 |  | 9.09 |  | 9.35 |  | 9.30 |  | 14.66 |  |
| Parameter | Unit | Value | Error | Value | Error | Value | Error | Value | Error | Value | Error |
| Thickness | nm | 128.88 | 0.04 | 127.64 | 0.04 | 130.27 | 0.04 | 129.95 | 0.05 | 131.14 | 0.05 |
| Surface Roughness | nm | 5.05 | 0.07 | 5.15 | 0.07 | 5.00 | 0.07 | 4.33 | 0.08 | 4.21 | 0.09 |
| High-Frequency Permittivity |  | 3.358 | 0.003 | 3.357 | 0.003 | 3.336 | 0.003 | 3.372 | 0.003 | 3.362 | 0.003 |
| “Optical” Resistivity | ×10-4 Ωcm | 5.38 | 0.01 | 5.43 | 0.01 | 5.16 | 0.01 | 5.05 | 0.01 | 4.83 | 0.01 |
| “Optical” Mean Free Time | fs | 4.955 | 0.006 | 4.865 | 0.007 | 5.274 | 0.008 | 5.138 | 0.008 | 5.156 | 0.009 |
| Inhomogeneity | % | 10.1 | 0.2 | 11.1 | 0.2 | 9.9 | 0.2 | 7.0 | 0.2 | 3.4 | 0.2 |
| 1st Oscillator (Gaussian) |  |  |  |  |  |  |  |  |  |  |  |
| Parameter | Unit | Value | Error | Value | Error | Value | Error | Value | Error | Value | Error |
| Amplitude |  | 42 | 1 | 42 | 1 | 42 | 1 | 42 | 1 | 42 | 1 |
| Broadening | eV | 0.0339 | 0.0007 | 0.0331 | 0.0007 | 0.0314 | 0.0007 | 0.0339 | 0.0007 | 0.0351 | 0.0006 |
| Energy | eV | 0.045 | -- | 0.045 | -- | 0.045 | -- | 0.045 | -- | 0.045 | -- |
| 2nd Oscillator (Lorentz) |  |  |  |  |  |  |  |  |  |  |  |
| Parameter | Unit | Value | Error | Value | Error | Value | Error | Value | Error | Value | Error |
| Amplitude |  | 7.68 | 0.05 | 7.55 | 0.05 | 8.30 | 0.06 | 8.44 | 0.06 | 8.75 | 0.07 |
| Broadening | eV | 0.398 | 0.002 | 0.407 | 0.002 | 0.375 | 0.002 | 0.362 | 0.002 | 0.344 | 0.002 |
| Energy | eV | 4.229 | -- | 4.229 | -- | 4.229 | -- | 4.229 | -- | 4.229 | -- |
| Non-Optically Measured Parameters |  |  |  |  |  |  |  |  |  |  |  |
| Parameter | Unit | Value | Error | Value | Error | Value | Error | Value | Error | Value | Error |
| DC Resistivity (Van der Pauw) | ×10-4 Ωcm | 4.65 | 0.08 | 4.66 | 0.09 | 4.48 | 0.07 | 4.23 | 0.07 | 3.82 | 0.07 |
| DC Resistivity (4pp) | ×10-4 Ωcm | 5.2 | 0.3 | 5.3 | 0.3 | 4.9 | 0.3 | 4.7 | 0.2 | 4.0 | 0.2 |
| “Hall” Carrier Concentration | ×1020 cm-3 | 4.6 | 0.4 | 4.7 | 0.2 | 4.2 | 0.1 | 4.9 | 0.2 | 4.9 | 0.3 |
| Calculated Parameters |  |  |  |  |  |  |  |  |  |  |  |
| Parameter | Unit | Value | Error | Value | Error | Value | Error | Value | Error | Value | Error |
| Effective carrier mass ratio* |  | 0.353 | 0.009 | 0.354 | 0.005 | 0.346 | 0.004 | 0.358 | 0.005 | 0.357 | 0.007 |
| “Optical” Carrier Concentration | ×1020 cm-3 | 4.7 | 0.1 | 4.75 | 0.07 | 4.52 | 0.05 | 4.89 | 0.07 | 5.1 | 0.1 |
| “Optical” Carrier Mobility | cm2/Vs | 24.7 | 0.7 | 24.2 | 0.4 | 26.8 | 0.3 | 25.2 | 0.4 | 25.4 | 0.5 |
| “Hall” Carrier Mobility | cm2/Vs | 29.21 | 0.04 | 28.75 | 0.02 | 33.11 | 0.02 | 29.97 | 0.02 | 33.47 | 0.04 |
| Screened plasma energy | eV | 0.6655 | 0.0003 | 0.6673 | 0.0001 | 0.6614 | 0.0002 | 0.6766 | 0.0003 | 0.6987 | 0.0002 |

* The effective carrier mass ratio is calculated from the Hall carrier concentration by accounting for non-parabolicity in the conduction band.6

Section C: Ellipsometric modelling

Due to the nature of the “inverse problem” of SE, where the sample properties cannot be directly calculated from the measured ellipsometric quantities but the ellipsometry quantities can be calculated from any given sample properties, the precise nature of the fitting is highly dependent on the sample of interest.7

Oscillator Functions

Lorentz functions produced the best fit when utilised for UV absorption tail.8 They are described by Eq. (S1):

| εLorentzE=ALγE0E02-E2-iEγ | (S1) |
| --- | --- |

where AL is the oscillator amplitude, E0 is the centre energy and γ is the broadening of the oscillator. Gaussian functions produced the best fit when used for IR absorption centres.9 They are described by Eqs. (S2) and (S3).

| εGuassianE=ALΓE-E0σ+ΓE+E0σ+i⋅exp-E-E0σ2-exp-E+E0σ2 | (S2) |
| --- | --- |

where

| σ=γ2ln2 | (S3) |
| --- | --- |

and the function Γ is a convergence series used to ensure Kramers-Kronig consistency for the real permittivity.9 The other parameters are defined above.

Justification of SE model

This section outlines the process used to fit SE measurements across the entire IR and NIR-VIS spectral range (0.034-3.4 eV) to extract the complex permittivity, εE=ε1E+iε2E, and optoelectronic properties of the ITO films. A model that considers both the intra- and inter-band absorption is required to fit the optical properties of ITO. To achieve this, we require a “generalised oscillator” model that describes the permittivity of a material as a summation of various individual oscillators.7

To fit the measurement with a generalised oscillator model, a summation is made of one Drude and one Lorentz oscillator in order to describe both the absorption due to free carriers (intra-band absorption) and inter-band transitions, respectively, as has been suggested by Uprety et al. for ITO films.10 To improve the fit further, it was necessary to include an additional IR phonon absorption (described by a Gaussian oscillator) at ~0.045 eV. Due to amorphous structure of the ITO film and the screening of the peak by the free carrier absorption, the Sn-O, Sn-O-Sn, and In-O optical phonon modes cannot be individually resolved.11 The Gaussian oscillator at ~0.045 eV can be said to represent a convolution of the peaks. The final step to accurately fit the NIR-VIS SE data was to include a layer of “optical” surface roughness, described by an effective medium approximation consisting of 50% of the ITO layer below and 50% air.

It is important to note that any fit can be achieved, given enough oscillators. “Over-fitting” of the data in this way can complicate the ability to extract useful information from the generalised oscillator model. Potential over-fitting of the data can be investigated via the parameter correlation,7 a number between negative and positive unity assigned to each parameter pair where absolute values above 0.90 indicate that the variations in one parameter can be completely accounted for by variations in its correlated counterpart. The parameter correlation can be reduced, increasing the validity of the fit, by reducing the number of free parameters.1 A general rule is any added complexity in the model (i.e., introducing surface roughness or additional oscillators etc.) is valid if it produces a decrease in the mean-squared error (MSE), which defines how well the data is fit, by at least ~25%.7 Exceptions to this rule can be made if the parameter is thought to improve the “realness” of the model.

To guarantee confidence in the physical reality of the extracted optical constants and optoelectronic parameters, these principles were followed during the optical modelling: ensuring that the utilised model was as simple as possible while producing a good fit to data, with only few and largely uncorrelated fitting parameters, and had been constructed following the guidance of literature. Where possible, the parameters have been verified with independent techniques. For example, the carrier transport properties have been independently measured via Hall Effect. Fig. S16 compares the “Hall” (filled symbols) and “optical” (open symbols) (a) carrier concentration, NHall and Nopt respectively, and (b) mobility, μHall and μopt respectively, for the seed ITO films (grey stars) and those subject to reactive laser annealing in 5% H2 in N2 (red circles), 5% O2 in N2 (blue squares), and 100% O2 (green triangles) and between 25-125 mJcm-2 in steps of 25 mJcm-2. Further validation of the resistivity was achieved via four-point probe (Tables S1-S3) and the gradient in the carrier concentration was independently measured with depth-profile energy-dispersive X-ray spectroscopy (Fig. S20-Fig. S22).

Figure S16. “Hall” (filled symbols) and “optical” (open symbols) carrier concentration, NHall and Nopt respectively, seed ITO films (grey stars) and those subject to reactive laser annealing in 5% H2 in N2 (red circles), 5% O2 in N2 (blue squares), and 100% O2 (green triangles) and between 25-125 mJcm-2 in steps of 25 mJcm-2.

Section D: XRD data and analysis

XRD spectra for all ITO films

Figure S17. X-ray diffractograms for the seed ITO films (dark-light grey squares) and those subject to reactive laser annealing in (a) 100% O2 and (b) 5% H2 in N2 between 25-125 mJcm-2 in steps of 25 mJcm-2 (red-blue squares). The fitting of two pseudo-Voigt functions to the asymmetric peak of each film is shown with the solid lines. To facilitate the peak fitting, the (100) Si peak at 32.9⁰ - 33.1⁰ has been manually removed from all diffractograms.

XRD analysis

Figure S18. X-ray analysis results: (a) Grain size, (b) micro-strain, (c) stress, and (d) area ratio between the two pseudo-Voigt peaks for the seed ITO films (grey stars) and those subject to single-pulse reactive laser annealing in O2 (green triangles; dark green line) and 5% H2 in N2 (red circles; dark red line) at 25-125 mJcm-2 in steps of 25 mJcm-2.

Section E: XPS and EDX data and Analysis

XPS Data and fits

Figure S19. High resolution (a-b) Sn3d, (c-d) O1s and (e-f) In3d XPS spectra (black dots) for the seed ITO films before and after laser processing with a single pulse at 125 mJcm-2 into an ambient atmosphere of 5% H2 in N2, respectively. The blue, green, cyan, and pink solid lines present the deconvoluted peaks for each core-level and the red solid line presents the cumulative fit to the data.

EDX data and analysis

The EDX images for the (a) seed ITO film and laser processed with a single 125 mJcm-2 pulse in (b) 5% H2 in N2 and (c) O2 are presented in Fig. S20. Across the image, the average emitted X-ray intensity at the characteristic energy of each element within the sample is measured in order to build a depth profile of the relative elemental concentration across the film (Fig. S21).  To better compare the films, the intensity of each individual element is normalised to its peak value and the zero-point distance is set to the bottom of the film. This is done by setting the “bottom” of the film to the point where the normalised grey value intensity of In passes 0.2. This value is chosen as it gives a reasonable film bottom that allows each film to align. The normalised grey value intensities for (a) tin, (b) oxygen, (c) indium, (d) platinum and (e) silicon from the defined “bottom” of the seed (grey squares) ITO film and those subject to ReLA at 125 mJcm-2 pulse in 5% H2 in N2 (red squares) and (c) O2 (green squares) are  presented in Fig. S22.

Figure S20. Transmission Electron Microscopy bright-field cross-sectional images (greyscale) of the (a) seed ITO film and those subject to single-pulse reactive laser annealing at 125 mJcm-2 into a 100 psig pressurised environment of (b) 5% H2 in N2 and (c) 100% O2. The brightfield image is overlayed with images of the detected characteristic X-ray intensity of oxygen (red), indium (green), tin (blue), platinum (purple), and silicon (yellow), as measured via energy-dispersive X-Ray spectroscopy.

Figure S21. Depth-profiles of the energy-dispersive X-Ray spectroscopy intensity for the characteristic peaks of oxygen (pink), indium (orange), tin (yellow), platinum (blue), and silicon (purple) for the (a) seed ITO film and those subject to single-pulse reactive laser annealing at 125 mJcm-2 into a 100 psig pressurised environment of (b) 5% H2 in N2 and (c) 100% O2. The green squares present the depth profile of bright-field image greyscale intensity, for reference.

Figure S22. The normalised grey value intensities for (a) tin, (b) oxygen, (c) indium, (d) platinum and (e) silicon from the defined “bottom” of the seed (grey squares) ITO film and those subject to ReLA at 125 mJcm-2 pulse in 5% H2 in N2 (red squares) and (c) O2 (green squares). (f) Presents the depth profile of bright-field image greyscale intensity, for reference.

References

- Fujiwara, H. & Kondo, M. Effects of carrier concentration on the dielectric function of ZnO:Ga and In2O3:Sn studied by spectroscopic ellipsometry: Analysis of free-carrier and band-edge absorption. Physical Review B 71, 075109 (2005).

- Kim, H. et al. Electrical, optical, and structural properties of indium–tin–oxide thin films for organic light-emitting devices. Journal of Applied Physics 86, 6451–6461 (1999).

- Ellmer, K. & Mientus, R. Carrier transport in polycrystalline ITO and ZnO:Al II: The influence of grain barriers and boundaries. Thin Solid Films 516, 5829–5835 (2008).

- Ellmer, K. & Mientus, R. Carrier transport in polycrystalline transparent conductive oxides: A comparative study of zinc oxide and indium oxide. Thin Solid Films 516, 4620–4627 (2008).

- Masetti, G., Severi, M. & Solmi, S. Modeling of carrier mobility against carrier concentration in arsenic-, phosphorus-, and boron-doped silicon. IEEE Transactions on Electron Devices 30, 764–769 (1983).

- Hillier, J. A. et al. When ellipsometry works best: A case study with transparent conductive oxides. ACS Photonics 7, (2020).

- Hilfiker, J. N. & Tompkins, H. G. Spectroscopic Ellipsometry: Practical Application To Thin Film Characterization. (Momentum Press, 2015).

- Jellison, G. E. & Modine, F. A. Parameterization of the optical functions of amorphous materials in the interband region. Applied Physics Letters 69, 371–373 (1996).

- de Sousa Meneses, D., Malki, M. & Echegut, P. Structure and lattice dynamics of binary lead silicate glasses investigated by infrared spectroscopy. Journal of Non-Crystalline Solids 352, 769–776 (2006).

- Uprety, P., Junda, M. M., Salmon, H. & Podraza, N. J. Understanding near infrared absorption in tin doped indium oxide thin films. Journal of Physics D: Applied Physics 51, 295302 (2018).

- Gonçalves, G. et al. Influence of post-annealing temperature on the properties exhibited by ITO, IZO and GZO thin films. Thin Solid Films 515, 8562–8566 (2007).