# Solar-driven ultrafast lithium extraction from low-grade brine using microfluidics-mediated vortex in scalable electrochemical reactors

Xianyun Zhang,a† Zhen Li,b† Jiang Liu,c Fuzong Xu,c Leiliang Zheng,a Stefaan De Wolf,c Zhiping Lai,b * Xu Lua,c *

a Clean Combustion Research Center (CCRC), Division of Physical Science and Engineering, King Abdullah University of Science and Technology (KAUST), Thuwal, 23955-6900, Kingdom of Saudi Arabia.

b Chemical Engineering Program, Division of Physical Science and Engineering, King Abdullah University of Science and Technology (KAUST), Thuwal, 23955-6900, Kingdom of Saudi Arabia.

c KAUST Solar Center (KSC), Division of Physical Sciences and Engineering, King Abdullah University of Science and Technology (KAUST), Thuwal, 23955-6900, Kingdom of Saudi Arabia.

†	These authors contributed equally.

*	Corresponding authors: Xu Lu (xu.lu@kaust.edu.sa) and Zhiping Lai (zhiping.lai@kaust.edu.sa)

|  | Supplementary Table 1: Comparison of Li extraction performance in this study and the literature |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Active material |  |  | Reactor type | cLithium (ppm) | Mg/Li mass ratio in feed | Na/Li mass ratio in feed | Voltage (V) | Li/Mg selectivity | Li/Na selectivity | Current density (mA/cm2) | Extraction rate (mg/g/h) | Reference |
| LiFePO4/FePO4 |  |  | SMER | 308 | 66.00 | 182.89 | 0.70 | 391.06 | 191.47 | 2.50 | 21.96 | This study |
| LiTiO2 |  |  | Beaker | 400 | No Mg2+ | 19.96 | - | No Mg2+ in feed | 19.96 | - | 0.71 | 1 |
| Li1.36Mn1.63O4 |  |  | Beaker | 118 | 3.42 | 3.28 | - | 58556 | 5464 | - | 0.52 | 2 |
| Hydrogenated manganese oxide |  |  | H-shape reactor | 1460 | 6.53 | 5,163.26 | 1.0 – 3.5 | 10 | 26 | - | 0.093 | 3 |
| LiFePO4/FePO4 |  |  | H-shape reactor | 220 | 60 | 375.45 | 1.00 | 133.33 | - | - | 3.89 | 4 |
| Ag/FePO4 |  |  | Beaker | 347 | No Mg2+ | 100 | 0 – 0.50 | No Mg2+ in feed | 547.61 | 0.50 | - | 5 |
| Li(1−x)Ni0.33Co0.33Mn0.33O2/ Ag |  |  | Beaker | 234.8 | 5.15 | 10.93 | 0.3 – 0.75 | 130.80 | 156.10 | 0.25 | - | 6 |
| LiMn2O4/Li(1−x)Mn2O4 |  |  | H-shape reactor | 2050 | 58.8 | 0.40 | 0.65 | 399.46 | - | - | 3.14 | 7 |

cLithium denotes the Li concentration of the target brine.

Supplementary Table 2: Financial assumptions and cost analysis in the TEA model.

| Assumptions |  | Value | Units |
| --- | --- | --- | --- |
| Plant specifications | Plant scale | 100,000 | Reactor quantity |
|  | Plant capacity | 310.08a | Kilogram/year |
|  | Plant life | 10 | Year |
|  | Utilization rate | 90 | % |
|  | Working hour | 3,648b | Hour |
|  | Annual output | 279.07c | Kilogram/year |
|  | Starting year | 2022 | - |
|  | Development and construction period | 1 | Year |
| Financial specifications | Nominal hurdle IRRd | 9.24 | % |
|  | Cost of debt (after tax) | 2.40 | % |
|  | Gearing ratio | 3:7 | - |
|  | Debt tenor | 10 | Year |
|  | Inflation rate | 1.18 | % |
|  | Income tax rate | 20 | % |
|  | Depreciation method | Straight line | - |
|  | Depreciation life | 10 | Year |
|  | Salvage value | 0 | USD |

- Plant capacity = Unit reactor yield × Working hour × Reactor quantity; Unit reactor yield = 0.16 mg (Li+) per hour = 0.85 mg (Li2CO3) per hour;

- Working hour complies with the labor laws and public holidays in the Kingdom of Saudi Arabia;

- Annual output = Plant capacity × Utilization rate.

- IRR: Internal rate of return.

Supplementary Table 3: Initial and boundary assumptions and conditions for the COMSOL model.

| Position | Condition |
| --- | --- |
| Inlet | Constant inlet velocity |
| Outlet | Constant outlet pressure of 0 Zero-diffusive flux of species |
| Electrode | Chemical reaction |
| Wall | Non-flux boundaries Non-slip condition |
| Solution phase | Newtonian incompressible |

Supplementary Figure 1: Schematic of SMER during Li extraction.

Supplementary Figure 2: (a) Geometry of the SMER design and (b) cross-sectional view of the flow channel with dimensions, where L and W denote the length and width of the reactor, respectively; D is the channel diameter; rs is the spiral radius; Le and we represent the length and width of the electrode, respectively; wm is the membrane width; h is the channel height; and the pitch of the spiral is set to 2 mm.

Supplementary Figure 3: SEM images of (a) LiFePO4 and (b) FePO4 electrodes. The as-prepared LiFePO4 nanoparticles were irregularly shaped at diameters of 100 to 500 nm.

Supplementary Figure 4: CVs of FePO4 electrodes in different solutions containing (a) 308 ppm of LiCl; (b) 56,329 ppm of NaCl; (c) 474 ppm of KCl; (d) 20,324 ppm of MgCl2; and (e) 214 ppm of CaCl2. The first cycle was excluded because the impurity peaks of temporary side reactions disturb CV profiles.8 The scan rate was 1 mV/s. A Pt plate was used as the counter electrode. The Ag/AgCl electrode (saturated KCl, Pine Research) was employed as the reference electrode.

Supplementary Figure 5: Photographs of (a) LiCl, (b) NaCl, (c) KCl, (d) MgCl2 and (e) CaCl2 solutions after the CV tests on FePO4 electrodes in Supplementary Figure 4.

Supplementary Figure 4a presents the redox peaks at 0.423 and -0.136 V vs. Ag/AgCl, corresponding to the intercalation/release of Li+ to/from the electrode. The intensity and position of the redox peaks remained the same after four cycles, indicating good stability and cyclic performance of FePO4 in the LiCl solution. As a result, no precipitation was observed in the solution (Supplementary Figure 5a).

Supplementary Figure 4b demonstrates multiple redox peaks corresponding to the intercalation of Na+ as agreed by previous studies.8 The ionic radius of Na+ is 0.102 nm, larger than that of Li+ (0.076 nm).8 Intercalation of larger ions leads to the collapse of the FePO4 lattice structure, resulting in the yellow precipitate of Fe3+ salt in Supplementary Figure 5b.

K+ (ionic radius = 0.138 nm) is larger than Na+;9 thus, the intercalation of K+ into FePO4 is more difficult than that of Na+ and poses more serious damage to FePO4. This finding is validated by the reduced intensity of the redox peaks (Supplementary Figure 4c) and the orange precipitate of Fe3+ salt (Supplementary Figure 5c).

In contrast, the radius of Mg2+ is 0.072 nm,10 slightly smaller than that of Li+. The intercalation of Mg2+ would not deteriorate the lattice structure of FePO4 (Supplementary Figure 5d). However, due to its incompatible ionic charge, the intercalation of Mg2+ is harder than Li+, as reflected by the lower intensity of redox peaks in Supplementary Figure 4d.

Although the ionic radius of Ca2+ (0.100 nm)9 is similar than Na+, the ionic charge of Ca2+ is also incompatible with FePO4. Based on Supplementary Figure 4e, the intercalation of Ca2+ seems to be impossible over the scanned voltage range, and FePO4 was fully preserved after the CV test (Supplementary Figure 5e). Bubbles in Supplementary Figure 5e were gaseous hydrogen and oxygen from water electrolysis.

Supplementary Figure 6: SEM images of the LiFePO4 electrode (a) before and (b) after eight cycles of operation and the FePO4 electrode (c) before and (d) after eight cycles of operation. The LiFePO4/FePO4 electrodes had porous structures consisting of LiFePO4/FePO4 nanoparticles, carbon black particles and polymer binder (Supplementary Figures 3a, 3b, 6a, and 6c). These components adhered to each other, and the morphologies were well maintained after eight cycles of operation (Supplementary Figures 6b and 6d).

Supplementary Figure 7: XRD patterns of (a) LiFePO4 and (b) FePO4 electrodes before and after experiments in a single reactor and module. XRD patterns of the as-prepared LiFePO4 electrode fitted well with the standard pattern of olivine LiFePO4 (Crystalline PDF #40-1499), and these patterns were maintained after a series of experiments (Supplementary Figure 7a). The FePO4 electrode was prepared from the de-lithiation of olivine LiFePO4. The standard pattern of olivine FePO4 is unavailable; however, the pattern of olivine FePO4 in this study (Supplementary Figure 7b) fits well with that in the literature,11 indicating the full de-lithiation of LiFePO4. XRD patterns of FePO4 were also maintained after a series of experiments.

Supplementary Figure 8: Schematic of a traditional H-shape two-compartment reactor.

Supplementary Figure 9: Ratios of Li+ extraction rates in SMER to those in a traditional H-shape reactor based on ICP analyses and columbic calculations.

Supplementary Figure 10: (a) Integrated and (b) disassembled schematics for the SMER module consisting of four reactors in series and parallel.

Supplementary Figure 11: Output voltage profiles of the perovskite/silicon tandem solar cell when operating the SMER module.

# Financial Assumptions and Cost Analysis

The LCOP of the plant that operates the up-scaled SMER assembly was calculated using the carrying charge and the capital recovery factor by considering capital, operational, and financial costs. The LCOP reflects the net present cost of production for the plant over the project lifetime, which also equals the price at which the produced Li2CO3 should be sold to break even at the end of its lifetime.

The financial assumptions made in the calculation are listed in Supplementary Table 2. The plant was assumed to run at an annual capacity of 309 kg with a utilization rate of 90%. The plant lifetime was 10 years, which was the same for the depreciation and debt payback period. The project was financed with 30% debt at an after-tax cost of 2.4% and 70% equity at a real IRR of 8%. The straight-line depreciation method was used. The development and construction of the plant were completed in one year, and there would be no salvage value of the plant in the end. The inflation rate was set to 1.18%, and the tax rate was 20%, both based on the average value in the Kingdom of Saudi Arabia. The total capital cost includes 15% contingency, and the annual plant maintenance cost was assumed to be 10% of the capital expenditure. However, the sales and labor costs were not included in this analysis.

Figure 3h indicates that the CapEx of the plant only accounted for a small amount of the total cost, whereas the OPEX dominated. In particular, the electrode took 58.4% of the total cost, whereas the membrane ranked second at 13.7%. Reducing these costs can further lower the LCOP and enhance the cost-effectiveness of the project.

Supplementary Figure 12: Revenue and cost over the years of operation.

Supplementary Figure 13: Chronoamperograms for the electrochemical de-lithiation of LiFePO4.

# References

1	Li, X. et al. Taming wettability of lithium ion sieve via different TiO2 precursors for effective Li recovery from aqueous lithium resources. Chem. Eng. J. 392, 123731 (2020).

2	Zandevakili, S., Ranjbar, M. & Ehteshamzadeh, M. Improvement of lithium adsorption capacity by optimising the parameters affecting synthesised ion sieves. Micro Nano Lett. 10, 58-63 (2015).

3	Lee, D.-H. et al. Selective lithium recovery from aqueous solution using a modified membrane capacitive deionization system. Hydrometallurgy 173, 283-288 (2017).

4	Zhao, Z., Si, X., Liu, X., He, L. & Liang, X. Li extraction from high Mg/Li ratio brine with LiFePO4/FePO4 as electrode materials. Hydrometallurgy 133, 75-83 (2013).

5	Pasta, M., Battistel, A. & La Mantia, F. Batteries for lithium recovery from brines. Energy Environ. Sci. 5, 9487-9491 (2012).

6	Lawagon, C. P. et al. Li1−xNi0.33Co1/3Mn1/3O2/Ag for electrochemical lithium recovery from brine. Chem. Eng. J. 348, 1000-1011 (2018).

7	Xu, W., He, L. & Zhao, Z. Lithium extraction from high Mg/Li brine via electrochemical intercalation/de-intercalation system using LiMn2O4 materials. Desalination 503, 114935 (2021).

8	Liu, X., Chen, X., Zhao, Z. & Liang, X. Effect of Na+ on Li extraction from brine using LiFePO4/FePO4 electrodes. Hydrometallurgy 146, 24-28 (2014).

9	Li, X. et al. Synthesis and luminescent properties of CaMoO4: Tb3+, R+ (Li+, Na+, K+). Journal of alloys and compounds 478, 684-686 (2009).

10	Ying, J., Luo, M., Jin, Y. & Yu, J. Selective separation of lithium from high Mg/Li ratio brine using single-stage and multi-stage selective electrodialysis processes. Desalination 492, 114621 (2020).

11	Xiong, J., He, L., Liu, D., Xu, W. & Zhao, Z. Olivine-FePO4 preparation for lithium extraction from brines via electrochemical de-intercalation/intercalation method. Desalination 520, 115326 (2021).