Supplementary Information

A Digital Twin of Synchronized Circular Laser Array for Powder Bed Fusion Additive Manufacturing

Hamed Attariani¶,*,Shayna Renay Petitjean¶, Majid Dousti¶

*, ¶Department of Mechanical and Materials Engineering, Wright State University, Dayton, OH 45431, USA

Corresponding Author: hamed.attariani@wright.edu, Tell: (937) 775-8320, Fax: (419) 586-0320

| Table S1. Density, thermal conductivity, and specific heat of the Ti-6Al-4V [1]. |  |  |  |
| --- | --- | --- | --- |
| Temperature (K) | Density (kg/m3) | Thermal Conductivity (W/mꞏK) | Specific Heat (J/Kꞏkg) |
| 298 | 4420 | 7 | 546 |
| 373 | 4406 | 7.45 | 562 |
| 473 | 4395 | 8.75 | 584 |
| 573 | 4381 | 10.15 | 606 |
| 673 | 4366 | 11.35 | 629 |
| 773 | 4350 | 12.6 | 651 |
| 873 | 4336 | 14.2 | 673 |
| 973 | 4324 | 15.5 | 694 |
| 1073 | 4309 | 17.8 | 714 |
| 1173 | 4294 | 20.2 | 734 |
| 1273 | 4282 | 19.3 | 641 |
| 1373 | 4267 | 21 | 660 |
| 1473 | 4252 | 22.9 | 678 |
| 1573 | 4240 | 23.7 | 696 |
| 1673 | 4225 | 24.6 | 714 |
| 1773 | 4205 | 25.8 | 732 |
| 1873 | 4198 | 27 | - |

| Table S2. Equations and Boundary Conditions |  |
| --- | --- |
| Governing Equations |  |
| Anisotropic heat conduct model | cpρ∂T∂t= ∂∂xλxkx∂T∂x+∂∂yλyky∂T∂y+∂∂zλzkz∂T∂z-ρHf∂α∂t. |
| Melt volume fraction, 0<α<1 | α=0, &T<TS(T-TS)(TL-TS), &TS<T<TL1, &T>TL |
| Boundary Conditions |  |
| Gaussian Heat Flux | qx,y=2PAπro2exp⁡-2(x-vt2-y2ro2. |
| Radiation boundary conditions | q=hcT-T0+hrT4-T04 |
|  | q=qx,y+hcT-T0+hrT4-T04 |
| Solidification Map Equations |  |
| Thermal Gradient (G) | G=∂T∂x2+∂T∂y2+∂T∂z2 |
| Solidification Rate (R) | R=vGxG. |
| Equiaxed Criterion | G1.91R<1.04×106 K1.91cm2.91.s |
| Columnar Criterion | G1.91R>1.92×106 K1.91cm2.91.s |

Table S3. Variables List

| Variable | Symbol |
| --- | --- |
| Specific heat capacity | cp |
| Density | ρ |
| Thermal conductivity enhancement factors | λx, λy, λz |
| Thermal conductivity | kx, ky, kz |
| Absorption coefficient | A |
| Laser beam velocity | v |
| Laser power | P |
| Melting enthalpy | Hf |
| Solidus temperature | TS |
| Liquidus temperature | TL |
| Melting Temperature | Tm |
| Room temperature | T0 |
| Heat transfer convection coefficient | hc |
| Heat transfer radiation coefficient | hr |
| Laser spot radius | ro |

| b b a a | d d c c |
| --- | --- |
| Figure S1. The melt pool shape on the x-z and y-z planes for P=50W and v=100-1000 mm/s. a-b) v=100 mm/s, c-d) v=500 mm/s, e-f) v=1000 mm/s | e e f f |

| b b a a | d d c c |
| --- | --- |
| Figure S2. The melt pool shape on the x-z and y-z planes for P=300W and v=100-1000 mm/s. a-b) v=100 mm/s, c-d) v=500 mm/s, e-f) v=1000 mm/s | f f e e |

| b b a a | d d c c |
| --- | --- |
| Figure S3. The melt pool shape on the x-z and y-z planes for P=500W and v=100-1000 mm/s. a-b) v=100 mm/s, c-d) v=500 mm/s, e-f) v=1000 mm/s | f f e e |

[1]	K.C. Mills, Recommended values of thermophysical properties for selected commercial alloys , Woodhead Publishing, 2002.