Supplementary Materials for Ultrahigh-Q guided resonance in an all-dielectric metasurface

Lujun Huang1#*, Rong Jin2,3,4#, Chaobiao Zhou5#, Guanhai Li2,3,4*, Lei Xu6, Adam Overvig7,

Feng Deng1, Xiaoshuang Chen2,3,4, Wei Lu2,3,4, Andrea Alu7,8*, and Andrey E Miroshnichenko1*

1 School of Engineering and Information Technology, University of New South Wales, Canberra,

Northcott Drive, ACT, 2600, Australia

2State Key Laboratory of Infrared Physics, Shanghai Institute of Technical Physics, Chinese Academy of Sciences, 500 Yu Tian Road, Shanghai, 200083, China

3Hangzhou Institute for Advanced Study, University of Chinese Academy of Sciences, No.1 SubLane Xiangshan, Hangzhou, 310024, China

4Shanghai Research Center for Quantum Sciences, 99 Xiupu Road, Shanghai, 201315, China

5College of Mechanical and Electronic Engineering, Guizhou Minzu University, Guiyang, 550025, China

6Advanced Optics and Photonics Laboratory, Department of Engineering, School of Science Technology, Nottingham Trent University, Nottingham NG11 8NS, UK

7Photonics Initiative, Advanced Science Research Center, City University of New York, New York, NY
10031, United States of America
8Physics Program, Graduate Center, City University of New York, New York, NY 10016, United States of
America

# These authors contributed equally to this work

*ljhuang@mail.sitp.ac.cn, ghli0120@mail.sitp.ac.cn, aalu@gc.cuny.edu, andrey.miroshnichenko@unsw.edu.au

Section 1-Fabry-Perot leaky modes in a three-layer structure

We consider a three-layer structures shown in Fig.1a. The thickness of the middle layer is L. Such a structure could support a number of Fabry-Perot leaky modes. Detailed derivations of their eigenvalues are given below. Note exp(-it) is assumed during the following derivation process

Assume Ex—Hy and interface located at z=-L/2 and z=L/2

Solving the Maxwell equations, one can have the electric field as follows

Ex (z) =A exp(+in1k0z),  z>L/2                     (1a)

Ex (z) =B.exp(-in2k0z)+C.exp(+in2k0z), -L/2<z<L/2                (1b)

Ex (z) =D exp(-in3k0z),  z<-L/2                    (1c)

Also, the magnetic field H can be obtained by following equations

iµ0Hy=∂Ex∂z                               (2)

Substituting eq.(1) into eq.(2), we will have

Hy (z) =A.(n1µ0/c). exp(+in1k0z), z>L/2                 (3a)

Hy (z) =B.(-n2µ0/c). exp(-in2k0z) +C. (n2µ0/c).exp(+in2k0z), -L/2<z<L/2      (3b)

Hy (z) =D.(-n3µ0/c). exp(-in3k0z), z>L/2                  (3c)

By matching the continuity of boundary conditions at z=-L/2 and z=L/2,

A exp(in1k0L/2) = B.exp(-in2k0L/2) +C.exp(+in2k0L/2) (4a)

D exp(in3k0L/2) = B.exp(+in2k0L/2) +C.exp(-in2k0L/2) (4b)

A.(n1). exp(in1k0L/2)= B.(-n2).exp(-in2k0L/2)+C.n2.exp(+in2k0L/2) (4c)

D.(-n3). exp(in3k0L/2)= B.(-n2).exp(+in2k0L/2)+C.n2.exp(-in2k0L/2) (4d)

(4a)*n1-(4c): (n1+n2).exp(-in2k0L/2).B+(n1-n2). exp(+in2k0L/2).C=0 (5a)

(4b)*n3+(4c): (n3-n2).exp(+in2k0L/2).B+(n3+n2). exp(-in2k0L/2).C=0 (5b)

Or

(n1+n2). exp(-in2k0L/2). B=(n2-n1). exp(+in2k0L/2).C (6a)

(n2-n3). exp(+in2k0L/2). B=(n3+n2). exp(-in2k0L/2).C (6b)

(6a)/6(b) gives us

(n1+n2)(n2+n3)/(n2-n1)/(n2-n3)= exp(2in2k0L)                 (7)

For example, for air/Si/SiO2 with n1=1, n2=3.47 and n3=1.46, the eigenvalues are

N=n2k0L=m-0.7452i(m=1,2,3…)                  (8)

Section 2-Band structure for three-layer waveguide structure and GMs

We again consider a three-layer waveguide structure as shown in Fig.S1a, where a high-index layer n2 with thickness t is sandwiched between the super-substrate n1 and substrate n3. The waveguide dispersion for TE (E//y) and TM (H//y) have been derived in the textbook and are given as follows

TE: tan⁡(β2t)=β2(β1+β3)β22-β1β3                       (9)

TM: tan⁡(β2t)=n22β2(β1+n32β3)n32β22-n22β1β3                  (10)

Where β1=k2-n12k02, β2=n22k02-k2, β3=k2-n32k02, and k=kx2+ky2.

Also, it is necessary to mention that there is a cut-off frequency for different guided modes.

Ωcj=ctn22-n32(tan-1sn32-n12n22-n32+jπ)(j=0,1,2…)   (11)

Where s=1 for TE and s=n22, c is the speed of light in the vacuum.

To plot the band structure for such a waveguide system, we introduce an artificial but virtual periodic boundary condition. There are two ways of defining the periodic structure: 1D grating and 2D metasurface, as schematically shown in Fig.S2a-b. We first treat this waveguide system as a virtual grating with the period d. The band structure could be obtained by solving the transcendent equations (9) and (10). Fig.3 plots band structures of TE and TM modes for a real waveguide structure air/220nm-Si/SiO2. The refractive index of Si and SiO2 are set as n2=3.47 and n3=1.46, respectively. We are particularly interested in the guided modes at  point because they can be treated as pseudo bound states in the continuum (GMs). The GMs can be obtained by setting

k=2mπd                           (12)

Where m=1,2,3,….

Substituting Eq.(12) into Eqs. (9) and (10) gives us the eigenfrequency of GMs

Generally speaking, GMs could be designed at any wavelength by choosing the artificial period. As an example, the period is tuned to d=548nm to support 1st GM at 1550nm. Such a waveguide with d=548nm also supports many other GMs for both TE and TM modes at different wavelengths (See Fig.3 and Fig.S4). Moreover, due to the square lattice, there are degeneracy for GMs labelled in Fig.S3. For example, for 1D TE case, GM-1 includes TE21 and TE31, GM-2 includes TE22 and TE32, GM-3 includes TE41 and TE51. Their field profiles are shown in Fig.3a. For TM case, GM-4 include TM21 and TM31, GM-5 includes TM22 and TM32, GM-6 includes TE41 and TE51. Their field profiles are presented in Fig.S4

For 2D virtual metasurface with square lattice, the degeneracy number is 4. The degeneracy could be lifted and reduced to 2 by applying different lattice constants dx and dy along x and y axis, respectively. In fact, the virtual 1D grating can be treated as a special example of 2D metasurface by setting the lattice constant dy as infinity. Similarly, the GMs at  point can be obtained by setting

k=2πm2dx2+n2dy2                           (12)

Where m,n=0,1,2,3,….

For square lattice with dx=dy=d , it becomes

k=2πdm2+n2                           (12)

Where m,n=0,1,2,3,….

Section 3-Perturbation theory for GMs

In this section, we analyze the structural perturbation on the GMs. Again, we consider the three-layer waveguide structure shown in Fig.1a. For the sake of simplicity and without loss of generality, we treat this waveguide structure as a 1D virtual grating structure, its dielectric functions ε*(x,z) can be expressed as following forms

ε*x,z=ε*x+d,z=n12  z>t           (13a)

ε*x,z=ε*x+d,z=n22  0≤z≤t       (13b)

ε*x,z=ε*x+d,z=n32  z<0          (13c)

For the TE polarization case (E//y), Ey, also denoted as u, should satisfy the Helmholtz equation

∂2u∂x2+∂2u∂y2+k*2ε*=0                       (14)

Where k*=ω*/c,  is the eigenfrequency of the eigenmode and c is the speed of light.

Because we only consider the eigenmodes (also called as GMs in this work) at  point, its eigenfunction should satisfy

ux,z=u(x+d,z)                      (15)

Here, we assume that 0<k*<2π/d.

Then, we introduce the perturbation layer on top of layer 2 to this system

εx,y=ε*x,y+δF(x,y)                 (16)

Where δ is a small real parameter, F(x,y) is the perturbation profiles, which is Fx,y=1 ( t<z<t+t0, -w2<x<w/2) and Fx,y=0 for the else region.

After perturbation layer is added, GMs is converted into real leaky modes. Note that these leaky modes include symmetry protected BICs with anti-symmetric field profile and GMRs with symmetric field profile. Here, we focus on studying the perturbation layer effect on the Q-factor of GMRs. We are interested in complex eigenfrequency  and Q factor nearby GMs. They can be expanded as

u=u*+u1δ+u2δ2+u3δ3+…           (17a)

=*+1δ+2δ2+3δ3+…            (17b)

k=k*+k1δ+k2δ2+k3δ3+…             (17c)

Where kj=ωjc, j=1,2,3…

Substituting Eq.(17) into Helmholtz equation and comparing the coefficients of δ0, δ1, δ2 give us

Lu*=0                              (18a)

Lu1=-(2k*k1ε*+k*2F)u*                    (18b)

Lu2=-2k*k1ε*+k*2Fu1-(2k*k2ε*+k12ε*+2k*k1F)u*   (18c)

Where L=∂x2+∂x2+k*2ε*

Due to the nature of leaky modes, uj must satisfy the outgoing radiation condition when z. Also, uj is a periodic function. Note that Eq.(18b) is inhomogeneous and singular. It is easy to prove that there is no solution u1 unless the right side of Eq.(18b) is orthogonal to u*. We define the whole region  as x<d/2, -<z<. We then multiply the complex conjugate of u*on both sides and integrate on , we have

u*Lu1dxdz=0                           (19)

Then, we have

k1=ω1c=-k*Fu*2dxdz2ε*u*2dxdz                      (20)

Because F is real, k1 is also real.

For 0<k*<2π/d, u1 is mainly contributed by the zero-diffraction and contains only single radiation channel. Thus, we have

u1~b0±e±ik*x, x→±∞                         (21)

Where b0± are nonzero coefficients.

We also derive the imaginary part of k2 from the Eq. (18c),

Im(k2)=Im(ω2)c=-d(b0+2+b0-2)2ε*u*2dxdzδ2              (22)

Detailed derivation of above equation can be found in Ref. [3].

Then, the imaginary part of complex eigenfrequency becomes

Im(ω2)=-cd(b0+2+b0-2)2ε*u*2dxdzδ2                     (23)

And thus, we will have Q-factors

Q=k*ε*u*2dxdzd(b0+2+b0-2)δ-2                        (24)

Thus, the Q-factors of such GMRs are inverse proportionally to the perturbation δ-2.

Figure S1. Fabry-Perot leaky modes in multilayer structure. a, schematic drawing of three layer thin film structure. b, Ey distribution of mode TEM12. c, Ey distribution of mode TEM13.

Figure S2. Virtual periodic structure for a three-layer waveguide system. a, virtual 1D grating structure with lattice constant d along x axis. b, virtual 2D metasurface with different lattice constants dx and dy along x and y axis.

Figure S3. Dispersion relationship of TE and TM guided modes. a, Band structure of TE guided modes. b, Band structure of TM guided modes.

Figure S4. GMs for TM case. a, Hz distribution of GM TM21 mode. b, Hz distribution of GM TM31 mode. c, Hz distribution of GM TM22 mode. d, Hz distribution of GM TM32 mode. e, Hz distribution of GM TM41 mode. f Hz distribution of GM TM51 mode.

Figure S5. Band structure for a 1D perturbed meta-waveguide system. a, TE Band structure of a metagrating system. b, TM Band structure of a metagrating system. The thickness of top perturbation layer is chosen as 20nm. The period is 548nm and the width of grating is 200nm.

Figure S6. Band structure for a 3D perturbed meta-waveguide system. The periods along x and y axis are px=py=548nm. The top layer has thickness 20nm. The hole radius is 100nm.

Figure S7. Properties of GMR TE31. a, Reflection mapping as functions of top layer thickness and incident wavelength for metagrating with p=548nm and w=200nm. b, Q-factor of GMR TE31 as a function of top perturbation layer thickness. c, Resonant wavelength of GMR TE31 vs top layer thickness. d, Reflection mapping as functions of grating width and incident wavelength for metagrating with p=548nm and t=40nm. e, Q-factor of GMR TE31 as a function of grating width. f, Resonant wavelength of GMR TE21 vs grating width.

Figure S8. Properties of GMR TE21 and TE31 for metagrating with broken symmetry. a, Reflection mapping as functions of top layer thickness and incident wavelength. b, Q-factor of GMRs TE21 and TE31 as a function of perturbation layer thickness. c, Resonant wavelength of GMRs TE21 and TE31 vs top layer thickness. d, Reflection mapping as functions of gap center and incident wavelength. e, Q-factor of GMRs TE21 and TE31 as a function of gap center. f, Resonant wavelength of GMRs TE21 and TE31 vs gap center.

Figure S9. GMR in 3D metasurface. a, Electric field distribution for GMRs TE311 and TE131 mode. b, Resonant wavelength of modes TE311 and TE131 vs periods along y axis. c, Q-factors of modes TE311 and TE131 vs periods along y axis.

Figure S10. Properties of GMR in 3D metasurface. a, Electric field distribution of GMRs TE311 and TE131. b, Q-factors of GMRs TE311 and TE131 as a function of top layer thickness. c, Resonant wavelength of GMRs TE311 and TE131 as a function of top layer thickness

Figure S11. Schematic illustration of home-made measurement system.

Figure S12. Experimental measurement of GMRs in 3D metasurface. a, Schematic drawing of 3D metasurface. b, cross section of metasurface. c, Measured reflection spectra of metasurfaces with different periods along x axis. The period along y axis is fixed as 545nm. d, Retrieved resonant wavelength and calculated resonant wavelength for different periods. e, Measured Q-factor for mode TE311, where resonant wavelength is tuned by the varied px. f, Measured Q-factor for mode TE131 with stable resonant wavelengths.