Additional data for article

Captions

Table S1. ANOVA of the models.

Table S2. The wavelength assignments of the lignin, cellulose and hemicellulose related bands.

Table S3. The yields of xylose (X1) and XOS (X2-X6) from extracted xylan of sorghum pith, rind and whole stem.

Fig. S1. The correlation between the release of p-coumaric acid and the recovery of xylan.

Fig. S2. FTIR spectra of raw and pretreated pith (A), rind (B) and whole stem (C).

Fig. S3. SEM images of untreated and pretreated sorghum sample. Raw pith (A), raw rind (D), raw whole stem (G), NaOH-ethanol pretreated pith (B), NaOH-ethanol pretreated rind (E), NaOH-ethanol pretreated whole stem (H), NaOH pretreated pith (C), NaOH pretreated rind (F) and NaOH pretreated whole stem (I).

Fig. S4. X-ray diffractograms of untreated and pretreated sorghum samples.

Table S1. ANOVA of the models.

Pith:

| Source | Sum of Squares | DF | Mean Square | F-value | P-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| P-coumaric acid |  |  |  |  |  |  |
| Model | 12245.85 | 14 | 874.70 | 52.42 | < 0.0001 | significant |
| A-NaOH | 9049.72 | 1 | 9049.72 | 542.37 | < 0.0001 |  |
| B-Ethanol | 589.68 | 1 | 589.68 | 35.34 | < 0.0001 |  |
| C-Tempertature | 268.47 | 1 | 268.47 | 16.09 | 0.0013 |  |
| D-Time | 339.63 | 1 | 339.63 | 20.35 | 0.0005 |  |
| AB | 10.60 | 1 | 10.60 | 0.6350 | 0.4388 |  |
| AC | 72.93 | 1 | 72.93 | 4.37 | 0.0553 |  |
| AD | 29.43 | 1 | 29.43 | 1.76 | 0.2054 |  |
| BC | 11.53 | 1 | 11.53 | 0.6908 | 0.4198 |  |
| BD | 244.30 | 1 | 244.30 | 14.64 | 0.0019 |  |
| CD | 5.13 | 1 | 5.13 | 0.3075 | 0.5880 |  |
| A² | 1596.78 | 1 | 1596.78 | 95.70 | < 0.0001 |  |
| B² | 57.60 | 1 | 57.60 | 3.45 | 0.0843 |  |
| C² | 58.47 | 1 | 58.47 | 3.50 | 0.0823 |  |
| D² | 6.39 | 1 | 6.39 | 0.3828 | 0.5460 |  |
| Residual | 233.60 | 14 | 16.69 |  |  |  |
| Lack of Fit | 228.68 | 10 | 22.87 | 18.59 | 0.0063 | significant |
| Pure Error | 4.92 | 4 | 1.23 |  |  |  |
| R2 | 0.9813 |  |  |  |  |  |
| Adjusted R2 | 0.9626 |  |  |  |  |  |
| Predicted R2 | 0.8938 |  |  |  |  |  |
| Hemicellulose |  |  |  |  |  |  |
| Model | 1566.63 | 14 | 111.90 | 17.76 | < 0.0001 | significant |
| A-NaOH | 1170.98 | 1 | 1170.98 | 185.80 | < 0.0001 |  |
| B-Ethanol | 127.86 | 1 | 127.86 | 20.29 | 0.0005 |  |
| C-Tempertature | 1.47 | 1 | 1.47 | 0.2332 | 0.6366 |  |
| D-Time | 2.31 | 1 | 2.31 | 0.3672 | 0.5542 |  |
| AB | 1.17 | 1 | 1.17 | 0.1851 | 0.6736 |  |
| AC | 4.93 | 1 | 4.93 | 0.7820 | 0.3915 |  |
| AD | 3.61 | 1 | 3.61 | 0.5728 | 0.4617 |  |
| BC | 32.09 | 1 | 32.09 | 5.09 | 0.0405 |  |
| BD | 93.51 | 1 | 93.51 | 14.84 | 0.0018 |  |
| CD | 24.65 | 1 | 24.65 | 3.91 | 0.0680 |  |
| A² | 63.71 | 1 | 63.71 | 10.11 | 0.0067 |  |
| B² | 9.82 | 1 | 9.82 | 1.56 | 0.2325 |  |
| C² | 40.91 | 1 | 40.91 | 6.49 | 0.0232 |  |
| D² | 37.21 | 1 | 37.21 | 5.90 | 0.0291 |  |
| Residual | 88.23 | 14 | 6.30 |  |  |  |
| Lack of Fit | 87.13 | 10 | 8.71 | 31.61 | 0.0023 | significant |
| Pure Error | 1.10 | 4 | 0.2757 |  |  |  |
| Cor Total | 1654.87 | 28 |  |  |  |  |
| R2 | 0.9467 |  |  |  |  |  |
| Adjusted R2 | 0.8934 |  |  |  |  |  |
| Predicted R2 | 0.6957 |  |  |  |  |  |

Rind:

| Source | Sum of Squares | DF | Mean Square | F-value | P-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| P-coumaric acid |  |  |  |  |  |  |
| Model | 18566.46 | 14 | 1326.18 | 39.44 | < 0.0001 | significant |
| A-NaOH | 13563.65 | 1 | 13563.65 | 403.37 | < 0.0001 |  |
| B-Ethanol | 513.26 | 1 | 513.26 | 15.26 | 0.0016 |  |
| C-Temperature | 152.65 | 1 | 152.65 | 4.54 | 0.0513 |  |
| D-Time | 654.16 | 1 | 654.16 | 19.45 | 0.0006 |  |
| AB | 101.30 | 1 | 101.30 | 3.01 | 0.1046 |  |
| AC | 1.30 | 1 | 1.30 | 0.0386 | 0.8470 |  |
| AD | 6.43 | 1 | 6.43 | 0.1911 | 0.6687 |  |
| BC | 1.39 | 1 | 1.39 | 0.0414 | 0.8417 |  |
| BD | 251.06 | 1 | 251.06 | 7.47 | 0.0162 |  |
| CD | 13.40 | 1 | 13.40 | 0.3984 | 0.5381 |  |
| A² | 3277.73 | 1 | 3277.73 | 97.48 | < 0.0001 |  |
| B² | 171.32 | 1 | 171.32 | 5.09 | 0.0405 |  |
| C² | 115.61 | 1 | 115.61 | 3.44 | 0.0849 |  |
| D² | 40.52 | 1 | 40.52 | 1.20 | 0.2909 |  |
| Residual | 470.76 | 14 | 33.63 |  |  |  |
| Lack of Fit | 464.43 | 10 | 46.44 | 29.33 | 0.0026 | significant |
| Pure Error | 6.33 | 4 | 1.58 |  |  |  |
| Cor Total | 19037.22 | 28 |  |  |  |  |
| R2 | 0.9753 |  |  |  |  |  |
| Adjusted R2 | 0.9505 |  |  |  |  |  |
| Predicted R2 | 0.8590 |  |  |  |  |  |
| Hemicellulose |  |  |  |  |  |  |
| Model | 464.23 | 10 | 46.42 | 12.43 | < 0.0001 | significant |
| A-NaOH | 147.63 | 1 | 147.63 | 39.53 | < 0.0001 |  |
| B-Ethanol | 225.33 | 1 | 225.33 | 60.33 | < 0.0001 |  |
| C-Temperature | 3.55 | 1 | 3.55 | 0.9514 | 0.3423 |  |
| D-Time | 29.27 | 1 | 29.27 | 7.84 | 0.0119 |  |
| AB | 35.88 | 1 | 35.88 | 9.61 | 0.0062 |  |
| AC | 3.40 | 1 | 3.40 | 0.9115 | 0.3524 |  |
| AD | 0.0196 | 1 | 0.0196 | 0.0052 | 0.9430 |  |
| BC | 3.57 | 1 | 3.57 | 0.9565 | 0.3410 |  |
| BD | 14.90 | 1 | 14.90 | 3.99 | 0.0611 |  |
| CD | 0.6724 | 1 | 0.6724 | 0.1800 | 0.6764 |  |
| Residual | 67.23 | 18 | 3.73 |  |  |  |
| Lack of Fit | 66.45 | 14 | 4.75 | 24.54 | 0.0035 | significant |
| Pure Error | 0.7737 | 4 | 0.1934 |  |  |  |
| Cor Total | 531.46 | 28 |  |  |  |  |
| R2 | 0.8735 |  |  |  |  |  |
| Adjusted R2 | 0.8032 |  |  |  |  |  |
| Predicted R2 | 0.6212 |  |  |  |  |  |

Whole stem:

| Source | Sum of Squares | DF | Mean Square | F-value | P-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| P-coumaric acid |  |  |  |  |  |  |
| Model | 13421.69 | 14 | 958.69 | 39.35 | < 0.0001 | significant |
| A-NaOH | 10038.13 | 1 | 10038.13 | 412.01 | < 0.0001 |  |
| B-Ethanol | 534.40 | 1 | 534.40 | 21.93 | 0.0004 |  |
| C-Temperature | 275.33 | 1 | 275.33 | 11.30 | 0.0047 |  |
| D-Time | 355.67 | 1 | 355.67 | 14.60 | 0.0019 |  |
| AB | 34.28 | 1 | 34.28 | 1.41 | 0.2553 |  |
| AC | 75.26 | 1 | 75.26 | 3.09 | 0.1007 |  |
| AD | 5.00 | 1 | 5.00 | 0.2050 | 0.6576 |  |
| BC | 0.9506 | 1 | 0.9506 | 0.0390 | 0.8463 |  |
| BD | 222.01 | 1 | 222.01 | 9.11 | 0.0092 |  |
| CD | 3.46 | 1 | 3.46 | 0.1420 | 0.7120 |  |
| A² | 1847.33 | 1 | 1847.33 | 75.82 | < 0.0001 |  |
| B² | 77.75 | 1 | 77.75 | 3.19 | 0.0957 |  |
| C² | 38.85 | 1 | 38.85 | 1.59 | 0.2273 |  |
| D² | 9.95 | 1 | 9.95 | 0.4083 | 0.5331 |  |
| Residual | 341.09 | 14 | 24.36 |  |  |  |
| Lack of Fit | 335.26 | 10 | 33.53 | 23.01 | 0.0042 | significant |
| Pure Error | 5.83 | 4 | 1.46 |  |  |  |
| Cor Total | 13762.78 | 28 |  |  |  |  |
| R2 | 0.9752 |  |  |  |  |  |
| Adjusted R2 | 0.9504 |  |  |  |  |  |
| Predicted R2 | 0.8590 |  |  |  |  |  |
| Hemicellulose |  |  |  |  |  |  |
| Model | 1097.38 | 14 | 78.38 | 19.23 | < 0.0001 | significant |
| A-NaOH | 626.41 | 1 | 626.41 | 153.69 | < 0.0001 |  |
| B-Ethanol | 218.79 | 1 | 218.79 | 53.68 | < 0.0001 |  |
| C-Temperature | 0.3502 | 1 | 0.3502 | 0.0859 | 0.7737 |  |
| D-Time | 3.82 | 1 | 3.82 | 0.9371 | 0.3494 |  |
| AB | 15.44 | 1 | 15.44 | 3.79 | 0.0719 |  |
| AC | 10.82 | 1 | 10.82 | 2.66 | 0.1255 |  |
| AD | 0.4096 | 1 | 0.4096 | 0.1005 | 0.7559 |  |
| BC | 18.23 | 1 | 18.23 | 4.47 | 0.0528 |  |
| BD | 11.22 | 1 | 11.22 | 2.75 | 0.1193 |  |
| CD | 11.46 | 1 | 11.46 | 2.81 | 0.1158 |  |
| A² | 167.27 | 1 | 167.27 | 41.04 | < 0.0001 |  |
| B² | 9.27 | 1 | 9.27 | 2.27 | 0.1537 |  |
| C² | 0.6986 | 1 | 0.6986 | 0.1714 | 0.6851 |  |
| D² | 1.72 | 1 | 1.72 | 0.4210 | 0.5269 |  |
| Residual | 57.06 | 14 | 4.08 |  |  |  |
| Lack of Fit | 56.14 | 10 | 5.61 | 24.48 | 0.0037 | significant |
| Pure Error | 0.9175 | 4 | 0.2294 |  |  |  |
| Cor Total | 1154.44 | 28 |  |  |  |  |
| R2 | 0.9506 |  |  |  |  |  |
| Adjusted R2 | 0.9011 |  |  |  |  |  |
| Predicted R2 | 0.7186 |  |  |  |  |  |

Table S2. The wavelength assignments of the lignin, cellulose and hemicellulose related bands.

| Wavenumber (cm-1) | Wavelength Assignment |
| --- | --- |
| 3432 | O2-H2。。。O6 intramolecular stretching modes in cellulose |
| 1732 | C=O vibration of esters, ketones, aldehydes in hemicellulose and/or lignin |
| 1513 | Aromatic skeletal ring in lignin |
| 1399 | C-H deformation in cellulose and hemicellulose |
| 1254 | C-O stretch in lignin and C-O linkage in guaiacyl aromatic groups |
| 1162 | C-O-C vibrations in cellulose and hemicellulose |
| 1106 | Aromatic skeletal and C-O stretch in lignin |
| 1048 | C-O stretch in cellulose and hemicellulose |
| 896 | C-H deformation in cellulose |

Table S3. The yields of xylose (X1) and XOS (X2-X6) from extracted xylan of sorghum pith, rind and whole stem.

| Source | Xylanase | X1 (%) | XOS (%) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | X2 | X3 | X4 | X5 | X6 |
| Pith | EpXYN1 | 3.70 | 15.92 | 9.93 | 4.44 | 0.54 | 0.36 |
|  | EpXYN3 | 2.74 | 10.00 | 7.12 | 0.72 | 0.77 | 0.23 |
|  | XynII | 0.84 | 6.87 | 6.71 | n.d.a | 0.10 | 0.09 |
| Rind | EpXYN1 | 3.20 | 15.33 | 10.67 | 6.32 | 0.27 | 0.12 |
|  | EpXYN3 | 2.11 | 5.92 | 8.56 | n.d. | 0.86 | n.d. |
|  | XynII | 0.55 | 6.24 | 6.24 | n.d. | n.d. | 0.50 |
| Whole stem | EpXYN1 | 3.03 | 14.91 | 9.11 | 5.32 | 0.22 | 0.72 |
|  | EpXYN3 | 4.31 | 11.79 | 4.84 | 0.44 | 0.17 | 0.11 |
|  | XynII | 0.82 | 8.02 | 7.94 | n.d. | n.d. | n.d. |

a n.d., not detected.

Figure S1

Figure S2

Figure S3

Fig. S4