Methods

Hybrid molecular graphene transistor as an operando and optoelectronic platform

Jorge Trasobares1, Juan Carlos Martín-Romano1, Muhammad Waqas Khaliq2, Sandra Ruiz-Gómez2, Michael Foerster2, Miguel Ángel Niño2, Patricia Pedraz1, Yannick. J. Dappe3, Marina Calero de Ory4, Julia García-Pérez1, María Acebrón1, Manuel Rodríguez Osorio1, María Teresa Magaz3, Alicia Gomez3, Rodolfo Miranda4,5, Daniel Granados1

Theoretical methods	2

Electrochemical current	2

Molecular energy level:	2

Surface coverage	2

Coulombic interactions	3

Energy molecular junction alignment:	3

DFT calculations:	3

Dirac Point shift:	4

Graphene mobility	4

Photoconductance:	4

Fermi – Dirac distribution:	5

Exponential decay model:	5

Experimental methods	6

Experimental design:	6

Device fabrication:	7

Device characterization:	8

# Theoretical methods

Electrochemical current is modeled by the extended Laviron model 1:

iθ0=n2F2AυΓmaxRTθ0(θ-θ0)θθ2-2Gθ0ϕ(θ)(θ-θ0)							(1)

Where i(θ0 ) is the measured voltammetry current, A is the electrochemical working electrode area, υ is the potential scan rate (Vs-1), Γmax is the surface coverage (mol cm-2), n is the number of electrons exchange per molecule during a redox process, F is the Faraday constant, R is the Universal Gas constant, T is the temperature, θ0 the oxidized normalized surface coverage, ϕ(θ) a segregation factor, and G is a global constant of interaction.

Molecular energy level: in the junction is extracted from the electrochemical measurements2:

EHOMO= Eabs,NHE-eE12,NHE 								(2)

Eabs, NHE: absolute potential energy of the normal hydrogen electrode -4.5 eV.

e: elementary charge, 1.602 x 10-19 C.

E1/2, NHE: formal half-wave potential versus normal hydrogen electrode.

Ag/AgCl as reference electrode vs. NHE. 0.197 V

Surface coverage (ΓFc, mol/cm2) is calculated by equation 3, where the QFc is the total charge calculated by the integration of the redox waves, n is the number of electrons interchanged per molecule in the reaction, F is the Faraday constant and A the surface of the working electrode exposed to the electrolyte solution (0.2 cm2)

ΓFc=QFcnFA 										(3)

Coulombic interactions can be estimated from a simple model 3:

φ=e1-1+rad2-0.54πε0εrd									(4)

Considering e the elementary charge, ra the ion pairing distance, d intermolecular distance, ɛ0 the dielectric permittivity of vacuum and ɛr the relative permittivity of water respectively and φ an average value per molecule-molecule coulombic interaction.

Energy molecular junction alignment:

ΦAu> EH + V η> ΦGr+V								(5)

ΦAu<EH + V η< ΦGr+V								(6)

ΦAu: Gold work function, ΦGr: Graphene work function, EH: Molecular energy level,

V: Applied voltage, η: voltage drop

DFT calculations:

As a support to interpret the experimental results, we have modelled the junction to determine theoretically its electronic properties and its electronic transport characteristics, in particular its response to an applied bias. To this end, we have considered a model junction (as shown in Figure 4 a), namely a FcC11SH molecule sandwiched between a 35 gold atom pyramid acting as a gold electrode, and a 5x5 unit cell of graphene, which is repeated periodically in the xy plane, mimicking an infinite graphene plane, to act as the second electrode. This structure has been fully optimized, until the forces went below 0.1 eV/Å. We have used the very efficient localized-orbitals basis set DFT code Fireball 4. Basis sets of sp3d5 numerical orbitals for Au and Fe, sp3 for C and S, and s for H have been used for structural optimization and conductance calculation of the nanojunctions, with cutoff radii (in atomic units) s = 4.5, p = 4.9, d = 4.3 (Au), s = 4.8, p = 5.0, d = 5.2 (Fe), s = 4.5, p = 4.5 (C), s = 3.1, p = 3.9 (S), and s = 4.1 (H) 5. A formalism taking into account van der Waals interactions has also been considered to determine the molecule−graphene distance6. From the optimized configuration, we can determine the electronic structure of the system, and use it to determine the electronic conductance and the electronic current in the molecular junction. We use here a non-equilibrium Keldysh-Green formalism, which has been designed initially to calculate simulated STM images, but which can be used to calculate electronic current in a molecular junction since it takes into account multiple scattering 7. This formalism has been already applied successfully to several types of molecular junctions 8,9.

Dirac Point shift: Photoconductance versus time follows this model as the electric charge.

∆E=ℏυFπnVD2-VD1									(7)

ℏ: Planck constant in J s rad-1, υF: Fermi level velocity ﻿1.1x 106 m s −1, π: Mathematical constant, n: carrier density ﻿7.2 × 1010 cm −2 V −1, VD2: Change of neutrality point with respect the reference.

Graphene mobility (μ, cm2V-1s-1):

L = 10 µm (graphene length), w = 24 µm (graphene width), Cox = 115 µFm-2, VDS : Drain to source voltage, IDS : Drain to source current, VBG : Back gate voltage, gm : transconductance.

μ=LW1CoxVDSgm 										(8)

gm=∂IDS∂VG

Photoconductance:

GPhGDark≈∆nnDark											(9)

GPh = 10 µS (photoconductance), GDark = 2 mS (conductance at dark state), nDark = ﻿7.2 x 1010 cm-2V-1 (dark state number of carriers), ∆n = nLigh – nDark = 3 x 108 (increment in the number of carriers).

﻿From the linear dependence of conductivity, σ (VBG), elementary charge, e,  carrier mobility, µ, we can find the number of carriers, n 10.

σ=µ n e											(10)

Fermi – Dirac distribution: Photoconductance versus power and gate voltages is modeled by the logistic model. It determines the statistical distribution of fermions over the energy states of a system in thermal equilibrium.

ni=11+e(ei-µ)kbT=A1+e4µAλ-t+2								(11)

where kB is Boltzmann's constant, T is the absolute temperature, εi is the energy of the single-particle state i, and μ is the total chemical potential. Second term in the mathematical expression is a reparameterization logistic model used to fit the experimental data. A= 9.32, µ= 3.78, λ = 1.25 for fits in Figure 5d and A= 13.95, µ= 0.54, λ = 3.27 for fits in Figure 5e.

Exponential decay model: Photoconductance versus time follows this model as the electric charge. V0/R = 10 C/s and RC = 80 s for fits in Figure 5d.

I=V0Re-tRC											(12)

# Experimental methods

Experimental design:

We first explore the use of graphene as a high-performance top contact electrode on a single junction showing that: (1) electron transfer between the Fc group in the Au/SC11Fc SAM and the gold electrode is achieved by applying an electrochemical voltage and consequently generating the electrochemical double layer through a Gr monolayer that adjusts the energy level of the system; (2) surface spectroscopy shows that Gr encapsulates the molecules avoiding ambient Fc oxidation and (3) operando examination helps to discuss the transport mechanism in the molecular junction. On the m-GFET, (4) molecular decoration of electrodes shifts the graphene VDP to neutrality and (5) photodetection based on Au/SC11Fc //Gr electron transfer is realized on the electron conduction regime. Finally, (6) the heterogenous optical and electrical dual gate is operated as OR/AND logic functions. The archetype 11-(Ferrocenyl)undecanethiol (FcC11SH) is acquired from Sigmaaldrich and characterized with electrochemical and spectroscopic methods (XPS and XAS) once assembled on the surface. This redox couple allows to estimate the quality of the SAM by a surface coverage and introduce a redox function to access by the light when the molecule is mounted in the m-GFET. µSAMs are formed on the gold surfaces not covered by the HfO2.

Device fabrication:

W-Oxide Wafer 04/009 100mm. N PRIME CZ 100As 0.001-0.005 ohm.cm 525 +/-20um Single side polished Semi standard flat Oxide - AtOx, 290nm Double side coated.

Electrodes. The device consists of source and drain chromium/gold micrometer size electrodes. The distance between drain and source is 20 μm and the electrodes sit on top of a SiO2/Si substrate (290 nm of SiO2 and highly n++ doped silicon). The electrodes are passivated by a layer of hafnium oxide (HfO2) and the molecular junctions integrated in a micropore, both electrodes are contacted together thanks to a CVD graphene that is back gated. The micropores on the electrodes are etched by HF (1%) treatment during 5 min.

Preparation of SAMs. We follow the procedures described in literature 11. µSAMs are formed by immersing the surfaces in a freshly ethanolic solution of 3 mM of the ferrocenyl undecanethiol for 12h. The samples are then taken out from the solution, rinsed with ethanol, and dried under N2 stream.

CVD graphene Transfer. Homemade and commercially available from Graphenea, high-quality monolayer graphene (SLG) grown by CVD technique on copper foil (Cu), is transferred by standard PMMA transfer process onto 1 x 1 cm2 SiO2/Si substrates where the final devices are fabricated as explained above. First, a sacrificial PMMA layer (495, A4; 5000 rpm, 60 s; baked for 1 min at 180°C) is spin coated on SLG/Cu and the graphene on the Cu backside etched by oxygen plasma (100 W; 2 minutes; 150 ml/min O2). Then, the Cu layer is wet etched using an ammonium persulfate solution (APS), obtaining a PMMA/SLG film. The PMMA/SLG stack picked up from solution, using a glass slide, to a DI water bath to remove chemical residuals. After three DI water baths (10 minute each), the PMMA/SLG film is transferred on the final device with the corresponding molecular SAMs. Then, the stacked PMMA/SLG /substrate is dried in air for 30 minutes and stored in vacuum for at least 24 hours, to avoid the detachment of the graphene from the substrate. Finally, the PMMA layer is removed dipping the sample in acetone for 1 hour and in isopropyl alcohol for another hour.

Device characterization:

﻿Electrochemical Measurements are performed in a three-electrode, single chamber Teflon cell connected to a Autolab PGSTAT204 (Metrohm) Electrochemical Analyzer in 0.1M ﻿NaClO4 electrolyte using an Ag/AgCl reference electrode and a Pt wire as a counter electrode. Before the experimental measurements, the electrochemical cell was cleaned with ethanol and DI water. ‘Test’ sweeps between 0.1 and 0.6V with a highly doped silicon substrate are measured to confirm that there is no peak due to contamination.

AFM and CAFM are conducted in a Nanotec Cervantes AFM (Nanotec). ElectriMulti75-G AFM probes (Budget Sensors) are used with platinum overall coating and a nominal force of spring constant 3 N/m and nominal resonance frequency of 75 kHz. All AFM raw data are analyzed with WSxM software12.

XPS characterization is produced using Ultra High Vacuum (UHV) conditions with a photon energy of 1486.7 eV (Al Kα transition)

Spatially resolved X-ray absorption spectroscopy (XAS) was performed at the CIRCE beamline of the ALBA synchrotron. The PEEM endstation is equipped with an Elmitec LEEM/PEEM III microscope.  The microscope can be used as a regular LEEM microscope using electrons as illumination source or as a Photo-Emission Electron Microscope by illuminating the sample with X-rays. The spatial resolution is 20 nm and the beamline provides photon energies in the soft X-ray range, from 100 eV to 2000 eV with high intensity and resolution, and fully variable polarization. Low-energy secondary electrons are used to form images of the spatially dependent X-ray Absorption Spectrum.

Raman spectra are acquired with a Bruker Senterra confocal Raman microscope instrument equipped with a 532 nm excitation laser. Acquisition parameters are: 2 mW, 5s integration time, 10 co-additions, 1-15 cm-1 resolution.

Electrical characterization was carried out on a Keithley 4200-SCS probe station with four SMU.

Optoelectrical measurements use an incident light from a diode, Thorlabs Fiber-Coupled (LED) MCWHF2.

References

1.	Alévêque, O. et al. Electroactive self-assembled monolayers: Laviron’s interaction model extended to non-random distribution of redox centers. Electrochem. commun. 12, 1462–1466 (2010).

2.	Nijhuis, C. A., Reus, W. F. & Whitesides, G. M. Molecular rectification in metal-SAM-metal oxide-metal junctions. J. Am. Chem. Soc. 131, 17814–17827 (2009).

3.	Trasobares, J. et al. Estimation of π-π Electronic Couplings from Current Measurements. Nano Lett. 17, (2017).

4.	Lewis, J. P. et al. Advances and applications in the FIREBALL ab initio tight-binding molecular-dynamics formalism. Physica Status Solidi (B) Basic Research vol. 248 1989–2007 (2011).

5.	Basanta, M. A., Dappe, Y. J., Jelínek, P. & Ortega, J. Optimized atomic-like orbitals for first-principles tight-binding molecular dynamics. Comput. Mater. Sci. 39, 759–766 (2007).

6.	Dappe, Y. J., Ortega, J. & Flores, F. Intermolecular interaction in density functional theory: Application to carbon nanotubes and fullerenes. Phys. Rev. B - Condens. Matter Mater. Phys. 79, 165409 (2009).

7.	González, C., Abad, E., Dappe, Y. J. & Cuevas, J. C. Theoretical study of carbon-based tips for scanning tunnelling microscopy. Nanotechnology 27, 105201 (2016).

8.	Tao, S. et al. Graphene-Contacted Single Molecular Junctions with Conjugated Molecular Wires. (2018) doi:10.1021/acsanm.8b01379.

9.	Zhang, Q. et al. Graphene as a Promising Electrode for Low-Current Attenuation in Nonsymmetric Molecular Junctions. Nano Lett. 16, 6534–6540 (2016).

10.	Novoselov, K. S. et al. Two-dimensional gas of massless Dirac fermions in graphene. Nature 438, 197–200 (2005).

11.	Nerngchamnong, N. et al. The role of van der Waals forces in the performance of molecular diodes. Nat. Nanotechnol. 8, 113–118 (2013).

12.	Horcas, I. et al. WSXM: A software for scanning probe microscopy and a tool for nanotechnology. Rev. Sci. Instrum. 78, (2007).