Synthesis and Application of Fe3O4@Graphene Oxide-Thiobarbituric Acid Based Binary Composite for Selective Removal of Cd(II) from Industrial Wastewater

Aminul Islam*, Hina Javed

Analytical Research Laboratory, Department of Chemistry, Aligarh Muslim University, Aligarh, India 202 002

*Corresponding author: aminulislam.ch@amu.ac.in

Fig. S1 Far IR spectrum of Fe3O4@GO-Th

Fig. S2 A) XRD B) TGA of Fe3O4@GO-Th

Fig. S3 Effect of pH

C

B

A

Fig. S4 (A) Effect of contact time (B) pseudo first order (C) pseudo second order

B

A

Fig. S5 A) Thermodynamic plot of Ln K Vs 1/T (K) (B) effect of temperature on sorption capacity of Cd(II)

Table S1 Summary of Kinetic parameters

| Models | Parameters Values |  |
| --- | --- | --- |
| Pseudo-first-order lnQe-Qt=ln Qe-K1t | K1 (min-1) | 0.066 |
|  | aQe (cal) (mg g-1) | 4.10 |
|  | R2 | 0.597 |
| Pseudo-second-order tQt= 1K2Qe2+ tQe | K2 (g mg-1 min-1) | 0.02 |
|  | aQe (cal) (mg g-1) | 11.93 |
|  | R2 | 0.984 |
| Experimental data | aQe (exp) (mg g-1) | 10.11 |

Adsorbent dose 50 mg, Total volume 50 mL, pH = 5.6 Qe is Cd(II) adsorbed at equilibrium ; Qt: Cd(II) adsorbed at time t; K1: rate constant of pseudo-first order model, K2: rate constant for pseudo-second-order model

Table S2A Summary of different forms of non-linear Isotherm model equations

| Models | Nonlinear Forms | Parameters |  |  |
| --- | --- | --- | --- | --- |
| Langmuir | qe= qmL KLCe1+KLCe | KL | Langmuir isotherm constant (L mg-1) |
|  |  | qmL | maximum monolayer adsorption capacity predicted by Langmuir isotherm (mg g-1) |
| Freundlich | qe= KFCe1nF | KF | Freundlich isotherm constant ((mg g-1) (L mg-1)1/nF) |
|  |  | nF | Freundlich model exponent |
| Jovanovic | qe= qmJV{1-exp-KJVCe} | KJV | Jovanovic isotherm constant linked to the free energy of adsorption (L g-1) |
|  |  | qmJV | Maximum monolayer adsorption capacity predicted by Jovanovic isotherm (mg g-1) |
| Sips | qe= KsCeβs1+αsCeβs | KS | Sips isotherm constant related to affinity constant (L g-1) |  |
|  |  | βs | Sips model exponent |  |

Table S2B Statistical Error Analysis

| Error functions | Abbreviations | Definitions |
| --- | --- | --- |
| Hybrid fractional error function | HYBRID | 100n-pi=1nqe,exp-qe,cal2qe,expi |
| Average relative error | ARE | 100ni=1nqe,exp-qe,calqe,expi |
| Sum of absolute errors | EABS | i=1nqe,exp-qe,cali |
| Marquardt’s percent standard deviation | MPSD | 1001n-pi=1nqe,exp-qe,calqe,exp2i |
| Reduced chi square | Reduced χ2 | 1n-pi=1nqe,exp-qe,cal2 i |
| Residual root mean square Error | RMSE | 1n-2i=1nqe,exp-qe,cal2 |

Table S3 Thermodynamic studies

| Temperature (K) | ∆G (KJ mol-1) | ∆H (KJ mol-1) | ∆ S (J mol-1.K-1) |
| --- | --- | --- | --- |
| 293 K | -7.80 | 13.81 | 73.65 |
| 303 K | -8.40 |  |  |
| 313 K | -9.28 |  |  |

Adsorbent dose 50 mg, Total volume 50 mL, pH = 5.6