High mobility of isolated three-fold polar vertices by electric fields

Mingqiang Lia,b, Tiannan Yangc, Pan Chend, Yongjun Wange, Ruixue Zhua, Xiaomei Lia, Ruochen Shia, Heng-Jui Liuf, Yen-Lin Huange, Xiumei Maa, Jingmin Zhanga, Xuedong Baid,g,h, Long-Qing Chenc, Ying-Hao Chue,i, Peng Gaoa,j*

aElectron microscopy laboratory, and International Center for Quantum Materials, School of Physics, Peking University, Beijing 100871, China;

bDepartment of Materials Science and Engineering, University of Toronto, Toronto, ON M5S 3E4, Canada;

cDepartment of Materials Science and Engineering, The Pennsylvania State University, University Park, PA, 16802, United States;

dBeijing National Laboratory for Condensed Matter Physics, Institute of Physics, Chinese Academy of Sciences, Beijing 100190, China;

eDepartment of Materials Science and Engineering, National Yang Ming Chiao Tung University, Hsinchu, 30010, Taiwan, ROC;

fDepartment of Materials Science and Engineering, National Chung Hsing University, Taichung, 40227, Taiwan, ROC;

gSchool of Physical Sciences, University of Chinese Academy of Sciences, Beijing 100190, China.

hSongshan Lake Materials Laboratory, Dongguan, Guangdong 523808, China.

iInstitute of Physics, Academia Sinica, Taipei 11529, Taiwan, ROC;

jCollaborative Innovation Centre of Quantum Matter, Beijing 100871, China

*Peng Gao.

Email: p-gao@pku.edu.cn

Supplementary Information

Supplementary Figure. 1. Schematic diagrams of a 90° domain wall (a), three-fold vertex (b), and flux-closure polar structure (c) corresponding with their winding numbers.

Supplementary Figure 2. Atomic structure of three-fold vertices. Out-of-plane lattice parameters (a),in-plane (b) lattice parameters and lattice rotation (c) of the three-fold vertex. (d) Line profiles of lattice parameters across the three-fold vertex corresponding to marked regions in (a) and (b). (e) Line profile of c/a ratio from out-of-plane and in-plane lattice parameters. (f) Line profile of lattice rotation across the three-fold vertex corresponding to the marked area in (c).

Supplementary Figure 3. The distribution of electric field in PbTiO3 films under - 8 V modeled by Ansoft Maxwell software. The tip contact width is estimated to be 20 nm. Scale bar, 50 nm.

Supplementary Figure 4. Electric-field control of isolated three-fold vertices at PbTiO3/SrRuO3 interfaces. (a-g) Chronological TEM dark-field image series illustrates nucleation and lateral motion of two three-fold vertices under applied electric fields. (h) Plots of applied voltage (orange line) and distance between two isolated three-fold vertices (blue diamond) as functions of time. (i) Schematic diagrams of the electric-field-driven motion of three-fold vertices. White arrows indicate the direction of motion.

Supplementary Figure 5. Atomic structure of 180° domain wall at PbZrTiO3/SrTiO3 interfaces. (a) An annular bright field (ABF) image of PbZrTiO3/SrTiO3 interface with a 180° domain walls. Open arrows show the direction of polarization. The inset intensity profile indicated the location of PbZrTiO3/SrTiO3 interfaces. Quantitatively atomic structure analysis showing the distribution of out-of-plane lattice parameters (b), in-plane lattice parameters (c) and corresponding c/a ratio (d). Dashed lines indicate the location of PbZrTiO3/SrTiO3 interfaces.

Supplementary Movie 1. Electric-field-driven formation and motion of isolated three-fold vertices at PbTiO3/SrRuO3 interfaces.

Supplementary Movie 2. Repeated experiment of the formation and motion of isolated three-fold vertices.