Conjugated polymer-functionalized perovskite semiconductors for electrolyte-gated transistors

Supplementary Fig. 1| MAPbI3/P3HT structure. Cross-sectional SEM image of MAPbI3/P3HT film on glass substrate.

Supplementary Fig. 2| TOF-SIMS analysis. TOF-SIMS negative ion depth profiles for electrolyte/P3HT/MAPbI3/Si structure. From the S‒, C‒ and H‒ signals of the thiophene unit, the P3HT layer can be characteristically indicated in the electrolyte/P3HT/MAPbI3/Si structure. Particularly, the C‒ and H‒ signals showed double peaking behavior, indicting the P3HT/MAPbI3 bilayer structure. Noticeably, the existence of I‒ and PbI3‒ signals in the MAPbI3 perovskite beneath the P3HT layer can also be clearly identified. The above signals evidenced that three distinctive layers of electrolyte/P3HT/MAPbI3 were formed, as shown in a photographic image of Supplementary Fig. 4. Without the P3HT layer, the electrolyte solution will dissolve the MAPbI3 perovskite.

Supplementary Fig. 3| Transistor characteristics of the P3HT-capped MAPbI3 FETs with high capacitance electrolyte dielectric. a, ID0.5−VG plot for the neat P3HT and MAPbI3/P3HT FETs in the saturation regime. VG was swept at a rate of 85 mV s–1. b-d, Output characteristics of the pristine P3HT (b), MAPbI3 (0.2 M)-P3HT FETs (c) and MAPbI3 (0.3 M)-P3HT FETs (d).

Table 1| Summary of transistor parameters for the control P3HT and P3HT IFL-capped MAPbI3 transistors with high-capacitance electrolyte dielectric.a

| Polymer IFL | MAPbI3 Conc. (M) | µFET (Best) (cm2 V–1 s–1) | µFET(avg) (cm2 V–1 s–1) | VT (V) | Ion/off |
| --- | --- | --- | --- | --- | --- |
| P3HT | - | 8.89 | 6.22 ± 1.87 | –0.98 ± 0.05 | >103 |
|  | 0.1 | 13.51 | 10.65 ± 0.84 | –0.90 ± 0.04 | ~103 |
|  | 0.2 | 6.16 | 5.09 ± 0.48 | –0.90 ± 0.04 | >102 |
|  | 0.3 | 3.74 | 2.01 ± 0.74 | –0.79 ± 0.07 | >102 |

- a Average values were obtained from at least 10 devices.

Supplementary Fig. 4| Perovskite/electrolyte dielectric contact. a-c, Photographic images of the pristine MAPbI3 spin-coated from 0.3 M concentration (a), MAPbI3 film after the deposition of electrolyte dielectric (b), and MAPbI3/P3HT/electrolyte dielectric showing perovskite protection capability (c) on a 15 mm × 15 mm substrates.

Supplementary Fig. 5| Surface morphology of the MAPbI3 films depending on the concentration of precursor solution. a, SEM images of the pristine MAPbI3 films on the glass substrates prepared with different precursor concentrations (0.1, 0.2, and 0.3 M). b, AFM images of the pristine MAPbI3 films on glass substrates prepared with different precursor concentrations. c, AFM images of the MAPbI3/P3HT films on glass substrates with different MAPbI3 concentrations. σRMS is root mean square surface roughness.

Supplementary Fig. 6| Energy level analysis of the MAPbI3 film. Ultraviolet photoelectron spectroscopy plots of the MAPbI3 prepared with different precursor concentrations on Au films (left) and its magnification of the region close to valence band edge of MAPbI3 (right). Bare Au film was used as a reference.

Supplementary Fig. 7| Transistor characteristics of the P3HT-capped MAPbI3 FETs with PMMA and P(VDF-HFP) dielectrics. a, Transfer curves of the neat P3HT and MAPbI3/P3HT transistors with low-κ PMMA dielectric. b,c, Output curves of the neat P3HT (b) and MAPbI3/P3HT (c) transistors with low-κ PMMA dielectric. d, Transfer curves of the neat P3HT and MAPbI3/P3HT transistors with high-κ P(VDF-HFP) dielectric. e,f, Output curves of the neat P3HT (e) and MAPbI3/P3HT (f) transistors with high-κ P(VDF-HFP) dielectric.

Table 2| Summary of metal halide perovskite FETs with top-gate structure.

| Perovskitea | Structureb | Dielectric | µh (cm2 V–1 s–1) | µe (cm2 V–1 s–1) | Year | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| MAPbI3-xClx | TGBC | Cytop | 1.3 | 1 | 2015 | 1 |
| (PEA)2SnI4 | TGTC | Cytop | 15 |  | 2016 | 2 |
| Csx(MA0.17FA0.83)1-xPb(Br0.17I0.83)3 | TGBC | PMMA | 2.1 | 2.5 | 2017 | 3 |
| (PEA)2SnI4 | TGTC | Cytop | 26 | 4.6 | 2017 | 4 |
| CsPbBr3 | TGBC | PMMA | 0.26 |  | 2017 | 5 |
| FAMAPbBr3 | TGBC | Cytop | 0.02 |  | 2020 | 6 |
| MAPbI3 | TGBC | Cytop | 1.8 | 3 | 2020 | 7 |
| Csx(MA0.17FA0.83)1-x Pb(Br0.17I0.83)3 (with DPP) | TGBC | PMMA/Y2O3 | 4.02 | 3.35 | 2020 | 8 |
| MAPbI3/Py1 | TGBC | Electrolyte | 30.87 |  | 2022 | This work |

a PEA = phenethylamine; MA = methylammonium; FA = formamidinium.

b TGBC = top gate bottom contact; TGTC = top gate top contact.

Supplementary Fig. 8| Defects passivation of the perovskite films after capping with IFLs. a-d, Pb 4f XPS plots of the MAPbI3/PTB7 (a), MAPbI3/Py0 (b), MAPbI3/Py2 (c) and MAPbI3/Py3 (d) films. e-f, I 3d XPS plots of the MAPbI3/PTB7 (e), MAPbI3/Py0 (f), MAPbI3/Py2 (g) and MAPbI3/Py3 (h) films. Diluted IFL solutions (1 mg mL–1 in chlorobenzene) were used for XPS analysis.

References

- Mei, Y., Zhang, C., Vardeny, Z. & Jurchescu, O. Electrostatic gating of hybrid halide perovskite field-effect transistors: balanced ambipolar transport at room-temperature. MRS Commun. 5, 297–301 (2015).

- Matsushima, T. et al. Solution-processed organic–inorganic perovskite field-effect transistors with high hole Mobilities. Adv. Mater. 28, 10275–10281 (2016).

- Yusoff, A. R. b, M. et al. Ambipolar triple cation perovskite field effect transistors and inverters. Adv. Mater. 29, 1602940 (2017).

- Matsushima, T. et al. Intrinsic carrier transport properties of solution-processed organic–inorganic perovskite films. Appl. Phys. Express 10, 024103 (2017).

- Hu, X. et al. Direct vapor growth of perovskite CsPbBr3 nanoplate electroluminescence devices. ACS Nano 11, 9869–9876 (2017).

- Senanayak, S. P. et al. A general approach for hysteresis-free, operationally stable metal halide perovskite field-effect transistors. Sci. Adv. 6, eaaz4948 (2020).

- She, X.-J. et al. A solvent-based surface cleaning and passivation technique for suppressing ionic defects in high-mobility perovskite field-effect transistors. Nat. Electron. 3, 694–703 (2020).

- Kim, H. P. et al. A hysteresis-free perovskite transistor with exceptional stability through molecular crosslinking and amine-based surface passivation. Nanoscale 12, 7641–7650 (2020).