Supporting Information

Impacts of residual 3D printing metal powders on immunological response and bone regeneration: An in vivo study

J.C. Tanga, Z. Sangb,*, X.K. Zhangb, C.H. Songc, W. Tangd, X.P. Luoe, M. Yana,*

aDepartment of Materials Science and Engineering, Southern University of Science and Technology, Shenzhen, 518055, China

bThe Eighth Affiliated Hospital, Sun Yat- sen University, Shenzhen, 518033, China

cDepartment of Mechanical and Automotive Engineering, South China University of Technology, Guangzhou 510641, China

dShenzhen Institutes of Advanced Technology, Chinese Academy of Sciences, Shenzhen, 518055, China

eNanjing Stomatological Hospital Medical School of Nanjing University, Nanjing 210008, China

*Corresponding authors, E-mail addresses: yanm@sustech.edu.cn; sangzhuohao@163.com

Fig. S1 (a) SEM micrograph of SLM-printed Ti-15Mo lattice. (b) Enlarged image of the red square area form (a), where partially-melted powders (white arrows) and loose powders (red arrows) on the surface of the implants can be observed.

Table S1 SLM processing parameters of all implants.

| Implants | Power (W) | Scanning speed (mm/s) | Layer thickness (μm) | Hatching space (μm) | Energy density (J/mm3) |
| --- | --- | --- | --- | --- | --- |
| 316L | 200 | 800 | 30 | 120 | 69.44 |
| CoCrMo | 360 | 500 | 50 | 175 | 82.29 |
| CP-Ti | 176 | 650 | 30 | 100 | 90.26 |
| Ti64 | 176 | 650 | 30 | 100 | 90.26 |

Table S2 Particle size distributions of all powders analyzed by Image J software.

| Powders | D10 (μm) | D50 (μm) | D90 (μm) |
| --- | --- | --- | --- |
| 316L-S | 9.7 | 15.5 | 22.2 |
| 316L-M | 29.3 | 39.6 | 46.1 |
| CoCrMo-S | 10.8 | 20.3 | 28.5 |
| CoCrMo-M | 31.7 | 37.2 | 49.2 |
| CP-Ti-S | 9.9 | 15.3 | 26.8 |
| CP-Ti-M | 24.1 | 31.4 | 44.6 |
| Ti64-S | 12.3 | 19.8 | 26.9 |
| Ti64-M | 31.8 | 41.7 | 47.3 |

Fig. S2 (a-c) High-magnification staining images of bone tissue around the Ti64 implant. (d-f) Enlarged images of the red square area from the staining images, where more small-sized powder particles (black arrows) can be observed.

Fig. S3 (a) SEM image of the CoCrMo-S powder. (b,c) Enlarged images of single powder particles corresponding to areas Ⅰ and Ⅱ in (a), repectively.

Fig. S4 (a) XPS survey spectrum and (b) detailed XPS spectra of Cr on the surface of the CoCrMo powders. (C) Schematic of the surface structure of the 316L-S powder.