One-dimensional nanostructured vanadium oxides with single-crystalline structure synthesized by cellulose nanocrystal-template-assisted hydrothermal method for Li-ion battery cathodes

Chulmin Youna,c, Wonsuk Kob, Ayoung Joc, Joonbong Leec, Sang Young Yeoa, Yongho Seoc, Jonghun leee,f, Byoung-Sun Leed*, Jongsoon Kimb*, Taekjib Choic*

aAdvanced Textile R&D Department, Korea Institute of Industrial Technology, 143 Hanggaul-ro, Sangnok-gu, Ansan-si, Gyeonggi-do, 15588, Republic of Korea

bDepartment of Energy Science, Sungkyunkwan University, 2066 Seobu-ro, Jangan-gu, Suwon-si, Gyeonggi-do, 16419, Republic of Korea

cHybrid Materials Research Center, Department of Nanotechnology and Advanced Materials Engineering, Sejong University, 209 Neungdong-ro, Gwangjin-gu, Seoul, 05006, Republic of Korea

dSchool of Polymer System/Department of Fiber Convergence Material Engineering, College of Engineering, Dankook University, 152 Jukjeon-ro, Suji-gu, Yongin-si, Gyeonggi-do, 16890, Republic of Korea

eDivision of Automotive Technology, Daegu Gyeongbuk Institute of Science and Technology, 333 Techno Jungang-daero, Hyeonpung-eup, Dalseong-gun, Daegu, 42988, Republic of Korea

fDepartment of interdisciplinary Engineering, Graduate School, Daegu Gyeongbuk Institute of Science and Technology, 333 Techno Jungang-daero, Hyeonpung-eup, Dalseong-gun, Daegu, 42988, Republic of Korea

*Corresponding authors:

E-mail: tjchoi@sejong.ac.kr (T. choi)

jongsoonkim@skku.edu (J. Kim)

sp6002@snu.ac.kr (B.-S. Lee)

This supporting information contains the following sections:

Fig. S1. TEM image of TEMPO-oxidized cellulose nanocrystal.

Fig. S2. Hydrothermal synthesis process for polycrystalline VO2(B) NPs without TCNC and various vanadium oxide with TCNC.

Fig. S3. Schematic diagram explaining step-by-step processes of nuclei formation, one-dimensional nanostructure formation, and one-dimensional nanostructure VO2(B) formation during the hydrothermal synthesis process.

Fig. S4. FESEM image showing the diameters of V2O5nH2O and VO2(B) NBs.

Fig. S5. XPS spectra of a) V2O5nH2O and b) VO2(B) NBs (C1s in the range of 281–291 eV).

Fig. S1 TEM image of TEMPO-oxidized cellulose nanocrystal.

Fig. S2 Hydrothermal synthesis process for polycrystalline VO2(B) NPs without TCNC and various vanadium oxide with TCNC.

Fig S3 Schematic diagram explaining step-by-step processes of nuclei formation, one-dimensional nanostructure formation, and one-dimensional nanostructure VO2(B) formation during the hydrothermal synthesis process.

Fig. S4 FESEM image showing the diameters of V2O5nH2O and single crystalline VO2(B) NBs.

Fig. S5 XPS spectra of a) V2O5nH2O and b) single crystalline VO2(B) NBs (C1s in the range of 281–291 eV).