Supporting Information on

Efficient separation and recovery of Re (VII) from Re/U bearing acidic solutions using aminotriazole modified cellulose microsphere adsorbents

Di Wen1,2#, Rong Hua1#, Zhen Dong1, Kangjun Xie1,2, Wei Qi1,2,Long Zhao1*

1State Key Laboratory of Advanced Electromagnetic Engineering and Technology, School of Electrical and Electronic Engineering, Huazhong University of Science and Technology, Wuhan 430074, China

2 School of Chemistry and Chemical Engineering, Huazhong University of Science and Technology, Wuhan 430074, China

3School of Nuclear Science and Engineering, East China Institute of Technology, 330013, Nanchang, China

- Kinetic Model Fitting

The pseudo-first-order, pseudo-second-order kinetic models are given as following Eqs. (S1, 2) (Ho and McKay 1998):

Inqe-qt=Inqe+K1t      (S1)

tqt=1K2qe2+tqe             (S2)

The intraparticle diffusion model is shown in Eq. (3) (W.J. Weber 1963):

qe=kintt0.5+c    (S3)

The Boyd liquid film diffusion model is shown in Eqs. (S4, 5) (Boyd et al. 1947; Reichenberg and McCauley 1955)

-0.4977-ln1-F=kbtF<0.85     (S4)

(π-π-π2F3)2=kbtF>0.85      (S5)

Where k1 (h-1) and k2 (g∙mg-1∙h-1) refer to the rate constants of pseudo-first-order and pseudo-second-order kinetic models, respectively. kint (mg⋅g-1 h-1/2) and kb (h−1) are the intra-particle diffusion and Boyd film diffusion rate constants, respectively. C (mg⋅g-1) shows the thickness of adsorption layer. F (F=qt/qe) is the fractional attainment of equilibrium at different time t. qe and qt are the amounts of Re(VII) adsorbed (mg∙g-1) at equilibrium and at time t(h), respectively.

- Isotherm Model Fitting

The equilibrium data were fitted using the following models: Langmuir model, Freundlich model and Temkin model.

Generally, the Langmuir model, Freundlich model can be expressed as Eq. (S6, S7) (Freundlich 1906; Langmuir 1917)

Ceqe=Ceqm+1KFqm     (S6)

qe=KFCe1n       (S7)

Where qe is the adsorption amount at equilibrium (mg∙g-1) and Ce is the equilibrium concentration (mg∙L-1), qm is the theoretical maximum adsorption amount (mg∙g-1), KL (L∙mg-1) and KF [(mg⋅g−1) (L mg−1) (1/n)] are the Langmuir and empirical constants, respectively; n represents the adsorption intensity or surface heterogeneity of the sample. KDR is a constant related to sorption energy (mol2⋅kJ−2).

S3 FTIR analysis and SEM analysis

Fig S1. FTIR image of MCC, MCC-g-GMA, 3-ATAR (A);SEM image of (a) MCC; (b) MCC-g-GMA; (c) 3-ATAR(B)

The FTIR spectra of MCC, MCC-g-GMA and 3-ATAR are shown in Fig. 2. The characteristic absorption band of epoxide group at 906 cm-1 and 843 cm-1 and carbonyl group (C=O) at 1720 cm-1 indicated that the GMA was successful grafted onto the MCC. The absorption bands of N-H at 1567 cm−1 and the band of the –C–N– in the triazole rings at 1110 cm-1 in 3-ATAR (Vashchenko et al. 2016). Meanwhile, C-O-C stretching vibration in epoxide ring decreased. Furthermore, the increase in intensity of the band around 3405 cm–1 in the spectrum of 3-ATAR can attribute to the combination and overlap of -OH and NH (in the triazole ring) (Wrzosek and Bukowska 2007; Moghaddam et al. 2019). The microstructure of sample was observed by SEM and shown in Fig. 5, it can be clearly seen that all exhibits sphere-like shape but various surface morphology, and some larger gaps and the bigger microsphere after opening reaction were appeared on the fracture surface (Fig 2B, b, c). 3-ATAR exhibited a spherical shape with a diameter about 300 μm.

Table S1. Kinetic parameter of Re(VII) adsorption onto 3-ATAR

| Parameter | 3-ATAR |
| --- | --- |
| qe,exp / (mg·g-1) | 16.83 |
| te / (min) | 45 |
| Langmuir Model |  |
| qe,est / (mg·g-1) | 16.45 |
| k1 / (g·mg-1·h-1) | 0.1671 |
| R2 | 0.9405 |
| Freundlich Model |  |
| qe,est / (mg·g-1) | 17.22 |
| k2 / (g·mg-1·min-1) | 0.01949 |
| R2 | 0.9999 |
| Intraparticle diffusion Model |  |
| Stage 1 |  |
| kint (mg·g−1·min−0.5) | 1.778 |
| C (mg·g−1) | 6.3826 |
| R2 | 0.9536 |
| Stage 2 |  |
| kint (mg·g−1 min−0.5) | 0.1024 |
| C (mg·g−1) | 15.72 |
| R2 | 0.9996 |
| Stage 3 |  |
| kint (mg·g−1 min−0.5) | 0.02853 |
| C (mg·g−1) | 16.24 |
| R2 | 0.9996 |
|  | Boyd film Model |
| Kb (min-1) | 0.04306 |
| Intercept | 1.207 |
| R2 | 0.9662 |

qe,est: equilibrium adsorption capacities obtained from kinetic models

qe,exp: experimental adsorption capacities at equilibrium

k1 and k2: Adsorption kinetic rate constants of Pseudo-first order and Pseudo-second order models, respectively;

R2: Correlation coefficient;

kint: Intraparticle diffusion rate constant;

Kb: Boyd film diffusion rate constant;

C: Constant related to the boundary layer thickness;

Table S2 Isotherm parameters for the adsorption Re (VII) on 3-ATAR in U/Re binary system

|  | Langmuir model |  |  | Freundlich model |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | qe(mg g-1) | k1(L mg-1) | R2 | k2 / (mg/g)/(mg/l)1/n) | n | R2 |
| 3-ATAR | 146.4 | 0.025 | 0.9870 | 12.71 | 2.425 | 0.9942 |

Reference

Boyd GE, Adamson AW, Myers LS (1947) The Exchange Adsorption of Ions from Aqueous Solutions by Organic Zeolites. II. Kinetics. J Am Chem Soc 69:2836–2848. https://doi.org/10.1021/ja01203a066

Freundlich HMF (1906) Over the adsorption in solution. J Phys Chem 57:1100–1107

Ho YS, McKay G (1998) A Comparison of chemisorption kinetic models applied to pollutant removal on various sorbents. Process Saf Environ Prot 76:332–340. https://doi.org/10.1205/095758298529696

Langmuir I (1917) The Adsorption of Gases on Plane Surfaces of Glass, Mica and Platinum. J Am Chem Soc 40:. https://doi.org/10.1021/ja02242a004

Moghaddam RH, Dadfarnia S, Shabani AMH, Tavakol M (2019) Synthesis of composite hydrogel of glutamic acid, gum tragacanth, and anionic polyacrylamide by electron beam irradiation for uranium (VI) removal from aqueous samples: Equilibrium, kinetics, and thermodynamic studies. Carbohydr Polym 206:352–361. https://doi.org/10.1016/j.carbpol.2018.10.030

Reichenberg D, McCauley D (1955) Properties of ion-exchange resins in relation to their structure. Part VII. Cation-exchange equilibria on sulphonated polystyrene resins of varying degrees of cross-linking. J Chem Soc 3:. https://doi.org/10.1039/jr9550002741

Vashchenko O V., Khomenko DM, Doroshchuk RO, et al (2016) Structure and Fluorescence Properties of Uranyl Ion Complexes with 3-(2-Hydroxyphenyl)-5-(2-Pyridyl)-1,2,4-Triazole Derivatives. Theor Exp Chem 52:38–43. https://doi.org/10.1007/s11237-016-9448-8

W.J. Weber JCM (1963) Kinetics of Adsorption on Carbon from Solution. J Sanit Eng Div 89:31–40

Wrzosek B, Bukowska J (2007) Molecular structure of 3-amino-5-mercapto-1,2,4-triazole self-assembled monolayers on Ag and Au surfaces. J Phys Chem C 111:17397–17403. https://doi.org/10.1021/jp075442c