Highlights

- PANi/ZnO nanohybrid has been successfully synthesized by one-step pyrolysis and characterized by XRD, FT-IR, SEM, and UV-visible.

- The PANi/ZnO nanohybrid was used for removing methylene orange dye.

- PANi/ZnO nanohybrids potentially performs as an efficacious adsorbent material for dye pollutants removal.

- Adsorption of MO dye onto adsorbent is fitted well to Pseudo-second-order model.

- Maximum removal efficiencies at optimum conditions were higher than 97% at pH 11, concentration of dye:10 mg/l, time equal to 40 min and dose 0.1 g of PANi/ZnO.

- The adsorption of dye molecules based on the rate of chemical adsorption, and so the adsorption rate depends on the capacity of the adsorption over the adsorbate concentration