Table 1. Constants for adsorption kinetic models from Cr(VI) adsorption by EFD&C (Corresponding to Fig. 5).

| Kinetic model | Kinetic parameters |  |
| --- | --- | --- |
| Pseudo-first-order model in Fig. 5(a) | qe1 (mg/g) | 27.8920 |
|  | k1 (1/min) | 0.0970 |
|  | R2 | 0.9555 |
| Pseudo-second-order model in Fig. 5(b) | qe2(mg/g) | 65.9100 |
|  | k2 (g/(mg·min)) | 0.0170 |
|  | R2 | 0.9968 |
| Eloovich model in Fig. 5(c) | α (g/(mg·min2)) | 76.4084 |
|  | β (mg/(g·min)) | 0.1299 |
|  | R2 | 0.9815 |
| Intraparticle diffusion model in Fig. 5(d) | Ki,1 (mg/(g·min1/2)) | 6.5807 |
|  | C1(mg/g) | 16.2810 |
|  | R12 | 0.9815 |
|  | Ki,2(mg/(g·min1/2)) | 0.7105 |
|  | C2(mg/g) | 48.4856 |
|  | R22 | 0.9603 |

Table 2. Constants for equilibrium adsorption isotherms curve from Cr(VI) adsorption by EFD&C (Corresponding to Fig. 6).

|  | Results from experiments | Langmuir model |  |  | Freundlich model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| T (oC) | qm,exp(mg/g) | qm(mg/g) | KL (L/mg) | R2 | KF [(mg/g)(mg/L)-n] | n | R2 |
| 25 | 91.55 | 97.0887 | 0.0580 | 0.9971 | 40.1775 | 0.1522 | 0.9905 |
| 35 | 96.96 | 101.7811 | 0.0680 | 0.9972 | 44.4185 | 0.1453 | 0.9582 |
| 45 | 111.94 | 116.5328 | 0.0760 | 0.9970 | 39.9228 | 0.1928 | 0.9763 |

Table 3. Thermodynamic parameters from Cr (VI) adsorption by EFD&C at different temperatures.

| ΔS0 (KJ/(mol·K) | ΔH0 (KJ/mol) | ΔG0 (KJ/mol) |  |  | R2 |
| --- | --- | --- | --- | --- | --- |
|  |  | 25 oC | 35 oC | 45 oC |  |
| 0.0488 | 12.8759 | -1.9197 | -2.3554 | -2.8975 | 0.9945 |