[Supplementary material]

Highly bright silica-coated InP/ZnS quantum dot-embedded silica nanoparticles as biocompatible nanoprobes

Kyeong-Min Hama,†, Minhee Kima,†, Sungje Bocka, Jaehi Kima, Wooyeon Kima, Heung Su Jungb, Jaehyun Ana,c, Hobeom Songc, Jung-Won Kimc, Hyung-Mo Kima,d, Won-Yeop Rhoe, Sang-Hun Leef, Seung-min Parkg, Dong-Eun Kima,* and Bong-Hyun Juna,*

Fig. S1. Comparison of QY of SiO2@InP QDs@SiO2 NPs, CdSe/ZnS QDs, and InP/ZnS QDs. The QY of SiO2@InP QDs@SiO2 NPs, InP/ZnS QDs, and CdSe/ZnS QDs were 6.61%, 15.03%, and 86.65%, respectively.

Fig. S2. TEM images of SiO2@InP QDs@SiO2 NPs by amount of added QDs. The amount of added QDs were (a) 1.4 mg, (b) 2.8 mg and (c) 5.6 mg per 1mg of SiO2 NPs

Fig. S3. Cytotoxicity investigation of SiO2@InP QDs@SiO2 NPs and hydrophilic CdSe/ZnS QDs. Cell viability of A549 cells in DMEM after 24 hours incubation with SiO2@InP QDs@SiO2 NPs and hydrophilic CdSe/ZnS QDs