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Fig. S1. Comparison of QY of SiO2@InP QDs@SiO2 NPs, CdSe/ZnS QDs, and InP/ZnS QDs. The QY of SiO2@InP QDs@SiO2 NPs, InP/ZnS QDs, and CdSe/ZnS QDs were 6.61%, 15.03%, and 86.65%, respectively.
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Fig. S2. TEM images of SiO2@InP QDs@SiO2 NPs by amount of added QDs. The amount of added QDs were (a) 1.4 mg, (b) 2.8 mg and (c) 5.6 mg per 1mg of SiO2 NPs
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Fig. S3. Cytotoxicity investigation of SiO2@InP QDs@SiO2 NPs and hydrophilic CdSe/ZnS QDs. Cell viability of A549 cells in DMEM after 24 hours incubation with SiO2@InP QDs@SiO2 NPs and hydrophilic CdSe/ZnS QDs
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