Supporting Information for

Green tea catechin-grafted silk fibroin hydrogels with reactive oxygen species scavenging activity for wound healing applications

Gyeongwoo Leea, Young-Gwang Koa, Ki Hyun Baeb, Motoichi Kurisawab, Oh Kyoung Kwonc, Oh Hyeong Kwona,*

aDepartment of Polymer Science and Engineering, Kumoh National Institute of Technology, Gumi, Gyeongbuk 39177, Korea

bInstitute of Bioengineering and Bioimaging, 31 Biopolis Way, The Nanos, Singapore 138669, Singapore

cGastric Cancer Center, Kyungpook National University Chilgok Hospital, Daegu 41404, Korea

*Corresponding author: Professor Oh Hyeong Kwon

E-mail: ohkwon@kumoh.ac.kr

Tel: +82-54-478-7690

Fax: +82-54-478-7710

Table S1

Gel permeation chromatography (GPC) analysis of SF-WS

| Sample | Mn (Da) | Mw (Da) | Polydispersity index (PDI) |
| --- | --- | --- | --- |
| SF-WS | 3,922 | 15,599 | 3.98 |

* Note: Weight-average molecular weight (Mw) of native SF is up to 500 kDa.31

Fig. S1. The reaction mechanism for the SF-EGCG conjugates formation through autoxidation of EGCG at mild basic pH 7.4 and subsequent conjugation of EGCG quinone (ring B) with a lysine residue of SF-WS. SF-WS/EGCG-amine adduct (Michael addition) is considered the dominant final product as the minor formation of SF-WS/EGCG quinone imine adduct (Schiff base addition) is unfavorable due to rapid hydrolysis of the imine bond in aqueous solution.

Fig. S2. Mass spectrum of EGCG-L-lysine reaction product and EGCG-ethanolamine reaction product.

Fig. S3. (a) Synthetic scheme for SF-tyramine (SF-T) conjugate through EDC/NHS activation of carboxyl residue of SF-WS and subsequent amidation reaction with a primary amine group of tyramine. 1H NMR spectra of (b) SF-WS and (c) SF-T (DS = 1.37). The integrated intensity of the characteristic peaks of tyrosine and tyramine moieties (6.6~7.4 ppm, B1, B2) was compared with that of the peak of alanine residues (1.3~1.5 ppm, A) to determine DS of tyramine moieties.

Fig. S4. Storage modulus of (a) SF-T90/SF-EGCG10, (b) SF-T70/SF-EGCG30 and (c) SF-T50/SF-EGCG50 composite hydrogels as a function of H2O2 concentration. The dotted line indicates the desired level of storage modulus (1,000 Pa). Gelation time of (d) SF-T90/SF-EGCG10, (e) SF-T70/SF-EGCG30 and (f) SF-T50/SF-EGCG50 composite hydrogels as a function of HRP concentration. The dotted line indicates the desired threshold for gelation time (30 sec), (Mean ± SD, n = 5).

Fig. S5. Viability of NIH3T3 fibroblasts as a function of SF-WS and SF-EGCG concentrations for 24 hours (Mean ± SD, n = 4).