Experimental Methods

Methacrylated hyaluronic acid (MeHA) was synthesized by a substitution reaction between hyaluronic acid (HA) and methacrylic anhydride (MA) in water (Scheme 1a) [45, 46]. HA (1,500-2,000 kDa range, Xian DN biology, China) was dissolved at 0.5 % (w/v) in deionized water (20 g of HA in 4 L of deionized water), and a six-fold molar excess of methacrylic anhydride relative to HA repeat units, was added dropwise to the solution. The pH of reacting mixture was adjusted to 7.5-8.0 with 5 M NaOH solution, and the reaction was continuously stirred overnight at 5 °C with re-adjustment of pH. The reactant was precipitated with a five-fold volumetric excess of cold acetone. White MeHA was separated, rinsed three times with cold acetone, re-dissolved in deionized water, and lyophilized.

Carboxylated NDs and hydroxylated NDs were prepared as reported in previous studies [42, 43]. In brief, the commercial products of carboxylated ND-COOH were supplied by Nanoresource Co., Ltd. (Seoul, Korea). The carboxyl groups of ND-COOH were reduced by the addition of NaBH4 to generate hydroxyl end groups on the ND substrates. The ND-COOH (50 mg) was dispersed with sonication and mixed with NaBH4 (100 mg) in ethanol (100 mL) in an ice bath. The mixture was stirred for 24 h at 60 °C under reflux and then washed with ethanol (50 mL × 2) and distilled water (50 mL × 3). The final product of ND-OH dispersed in distilled water was lyophilized for further characterization.

Rheological flow properties of HA/ND hydrogel were investigated by a stress-controlled rheometer (Haake Mars IIM, Thermo Electron, Germany) at 25 °C. The parallel-plate fixture was set with a diameter of 25 mm and a 1 mm gap. Before each experimental run, the specimen was kept at the set temperature for 10 min to establish a homogeneous thermal state and eliminate residual thermal history. Viscosity was measured by a rotation ramp method with the shear rate from 0 to 100 (1/sec). Oscillation stress sweep tests were carried out at a frequency of 10 Hz in a stress range of 1–100 Pa. In addition, time stress tests were carried out using a constant shear stress and frequency (5.0 Pa and 10 Hz). Frequency sweep tests were carried out at a sheer stress of 5.0 Pa in a frequency range of 1–10 Hz. The results were analyzed using the Haake Rheowin Data Manager 3.6 software.

The HA/ND mixture was prepared at desired concentrations and processed for 3D printing under the following conditions. A micro-dispensing pump machine was used as the extrusion system (Rokit Invivo, Rokit Healthcare, Seoul, Korea)), and all printing was conducted at room temperature. During extrusion, a UV precuring system (6 W/cm2, 385 nm) near the nozzle was used to cure the extruded filament and construct 3D-layers. The dispensing nozzles were respectively 21 gauge (514 μm inner diameter), 23 gauge (337 μm inner diameter), and 26 gauge (260 μm inner diameter) to deposit precursor ﬁlaments. The distance between two adjacent ﬁlaments was approximately 1.0 mm and the vertical step of 0.2 mm. The nozzle printing speed was 2 mm/s and the standoﬀ distance was set as 2 mm. After printing, the 3D constructions were cured using UV light (18 W/cm2) for 15 min. Digital 3D design programmed in printing path code was performed using 3ds max 2018 (Autodesk Inc., Mill Valley, CA, USA). Printed 3D porous networks of crosslinked hyaluronic acid structure were imaged by scanning electron microscopy (SEM) using an EM-30 SEM (COXEM, Daejeon, Korea) at a 20.0 kV acceleration voltage. Crosslinked HA structures were lyophilized and then sputtered with gold under argon atmosphere using an SPT-20 ion coater (COXEM, Daejeon, Korea).

Compressive mechanical strength of the HA structures was determined by texture analyzer (TA.XT plus, Stable Micro Systems Ltd., UK). The indenter was equipped with a 5 N load cell (resolution of 0.1 mN) and 2 mm diameter flat-ended cylindrical stainless steel indentation probe. Compressive force was applied to the 3D-printed hydrogel vertically and the rate of force measurement was 20 μm/sec with a triggering force of 0.001 N as the initial depth of hydrogel.

Load-displacement data from indentation measurement were used to obtain compressive moduli using the mathematical model introduced by Oliver and Pharr [47]. Effective modulus, E*, was

1E*= 1- υs2Es+ 1-υi2Ei

where E and υ are Young’s modulus and Poisson’s ratio, respectively, and the subscripts s and i present specimen and indentor, respectively. Each term indicates elastic displacement resulted from a sample and indentor. However, since the indentor was very rigid compared to the soft specimen (stainless steel vs. soft hydrogel), contribution from the second term can be ignored.

The most widely used mathematical model of indentation for soft tissue can be expressed as following,

E*= 1β×dPdw×12×πA=S/2a

where β is a geometric constant such that β=1 for flat ended indentation probe and  dPdw is the stiffness (S) at instantaneous displacement (w) and load (P). Derivatives (dPdw) of incorporation with load and instantaneous displacement is used to account for the non-linearity of soft tissue. Measured stiffness at each measurement was calculated to obtain a calibrated effective modulus.