Figures and Tables Legends

Figure 1. The milky solution and pellet form of MLCNPs. The chitosan polymer, TPP powder and miltefosine solutions were mixed for formation of ionically cross-linked nanoparticles. H2O2 and D-Trehalose were added before centrifugation. The resulting milky solution (A) and pellet (B) MLCNPs, after centrifugation are shown.

Figure 2: Morphological examination of MLCNPs. The morphology and size of Miltefosine Loaded Chitosan Canoparticles was determined through scanning electron microscopy (SEM). The magnification used was between 20,000xs (A) to 45,000xs (B) with accelerating voltage of 20 kV. The MLCNPs displayed spherical shape with irregular surface morphology.

Figure 3. In vitro hemolysis assay for Mitefosine and MLCNPs. In vitro hemolysis assay was performed to check the toxicity of drug in human blood. The human blood was exposed to each drug and the remaining hemoglobin in supernatant was measured. Conventional miltefosine showed more hemolysis (B) with light pink color, than MLTNPs (A), the negative control PBS solution (C) is transparent (no hemolysis) and the positive control Triton-X 100 solution (D) showed dark red color due to erythrocytes lysis.

Table 1. Characteristic assessment of the MLCNPs Nanoparticles. The drug loading content and encapsulation efficacy were determined by colorimetric assay. The size and surface morphology of MLCNPs nanoparticles were determined using scanning electron microscopy. The zeta potential for MLCNPs was calculated.

Table 2: Anti-Leishmanial activities of Miltifosine, Chitosan and MLCNPs. The Leishmania tropica promastigotes and amastigotes were checked for drug sensitivity by MTT colorimetric method. The activity of Miltefosine Loaded Chitosan Nanoparticles was higher than the conventional Miltefosine, whereas Chitosan showed the lowest sensitivity.

Table 3. In human blood the in vitro Hemolysis assay for Mitefosine and MLCNPs. The hemolysis assay was performed for in vitro assessment of toxicity of mitefosine and MLCNPs in human blood. The human blood was exposed to each drug and the remaining hemoglobin in supernatant was measured. The negative control PBS solution did not showed any hemolysis, whereas the positive control Triton-X 100 solution showed 100 % hemolysis. The conventional Miltefosine showed almost twice heamolysis as compared to the MLTNPs.