Table 1. Substrate scope of electrocatalytic hydrogenation of quinolines and other N-heterocycles with H2O over the Co-F cathode.

aReaction conditions: substrates (0.2 mmol, 28.57 mmol L-1), Co-F electrode (working area: 1.0 cm2), a mixed solution of 1.0 M KOH/dioxane (6:1 v/v, 7 mL), −1.1 V, RT, 12 h. b a mixed solution of 1.0 M KOH/dioxane (5:2 v/v, 7 mL). c−1.2 V, 18 h. d3,4-Dihydroisoquinolines were used as substrates. Conv. of substrates and isolated yields of products are reported. Conv. was calculated by gas chromatography (GC) using dodecane as an internal standard. Isolated yields of products are given in round brackets.