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Polyethylene: PE; polypropylene: PP; polystyrene: PS; polyvinyl chloride: PVC; nitrile rubber: NBR; poly-methyl methacrylate: PMMA; poly vinyl alcohol: PVA; ethylene vinyl acetate: EVA; polyethylene glycol: PEG; polyurethane: PU; polyethylene terephthalates: PET; polyamide: PA; polyester: PES; polytetrafluoroethylene: PTFE.  rubber: TPE; acrylic polymers: AP; Nylon 6.6: Nylon; polystyrene-butadiene-styrene: SBS; thermoplastic polyurethane: TPU; ethylene-propylene rubber: EPR						
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Area Sample type Mean Measure unit Main polymers References
Ross Sea sea water 0.17 items·m-3 PE, PP, PES, PTFE, PMMA, PA Cincinnelli et al., 2017
Southern Ocean sea water 7.25* items·m-3 PE, PP Isobe et al., 2017



Ross Sea sediment na (5 -1705) N/m2 PE, PP, Nylon, SBS, PVC, PS, 
TPU, PVA, EPR Munari et al., 2017



Adelaide Island sediment 0.52*(1-10) items·m-3 Rayon* (semi-synthetic fibre) Reed et al., 2018
King George Islandsea water 2.4 items·100m-3 PEG, PU, PET, PA Absher et al., 2019
Antartic Peninsulasurface sea water 1794 items·km-2 PU, PA, PE, PS, PP Lacerda et al., 2019



sea water 353 items·km-2 PVC,  PP, PS, PVC, nylon Suaria et al., 2020



East-Antarctic sea ice 96 items·L-1 
PE, PP, PA (nylon), varnish (PU 
and polyacrylates), EVA, resins, 
NBR, PS, PVA, rayon*, PL, silicone. 



Kelly et al., 2020



Antarctic 
Peninsula sediment 1.3 items/g PEst, PP, PS, PU, PVC, TPE, AP Cunningham et al., 2020
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