Development of a smart pH-responsive nano-polymer drug, 2-methoxy-4-vinylphenol conjugate against the intestinal pathogen, Vibrio cholerae

Hema Bhagavathi Sarveswari1, Krishna Kant Gupta2, Ramya Devi3* and Adline Princy Solomon1*

1 Quorum Sensing Laboratory, Centre for Research in Infectious Diseases (CRID), School of Chemical and Biotechnology, SASTRA Deemed to be University, Thanjavur, 613401, India.

2 School of Chemical and Biotechnology, SASTRA Deemed to be University, Thanjavur, 613401, India.

3  Pharmaceutical Technology Laboratory, School of Chemical and Biotechnology, SASTRA Deemed to be University, Thanjavur, 613401, India.

Supplementary File

Figure S1  Particle size (A) and zeta potential (B) of polymeric (CAP) nanoformulation of 2M4VP.

Figure S2  Effect of CAP-2M4VP on the growth of V. cholerae MTCC 3905 and HYR14 after 24 hours at pH 6.

Figure S3 Effect of CAP-2M4VP on the growth of V. cholerae MTCC 3905 and HYR14 after 24 hours at pH 7.

Figure S4 Effect of CAP-2M4VP on the growth of V. cholerae MTCC 3905 and HYR14 after 24 hours at pH 8.

Figure S5 Effect of CAP-2M4VP on the growth of V. cholerae MTCC 3905 and HYR14 after 24 hours at pH 9.

Table S1 Release kinetics of CAP polymeric nano-formulation of 2M4VP.

| Kinetics Model | Parameters | pH 1.2 | pH 5.8 | pH 7 | pH 8 | pH 9 |
| --- | --- | --- | --- | --- | --- | --- |
| Zero order | R2 | -0.4503 | -1.2436 | -0.4118 | -0.4304 | -1.7858 |
|  | K0 | 1.719 | 1.900 | 3.148 | 1.922 | 1.934 |
|  | SS | 6237.5447 | 9447.6506 | 20041.2991 | 7435.7775 | 11611.2526 |
| First order | R2 | 0.0271 | -0.5434 | 0.6572 | 0.0768 | -0.9007 |
|  | K1 | 0.026 | 0.031 | 0.121 | 0.031 | 0.033 |
|  | SS | 4184.1863 | 6499.3417 | 4866.4044 | 4799.2933 | 7922.0191 |
| Higuchi | R2 | 0.7066 | 0.3813 | 0.7147 | 0.6958 | 0.1608 |
|  | KH | 9.457 | 10.531 | 17.267 | 10.531 | 10.831 |
|  | SS | 1261.7284 | 2605.5058 | 4050.4897 | 1581.5030 | 3497.7576 |
| Korsemeyer-Peppas | R2 | 0.9905 | 0.9767 | 0.9900 | 0.9808 | 0.9712 |
|  | KKP | 19.779 | 26.327 | 35.978 | 22.210 | 29.033 |
|  | n | 0.261 | 0.202 | 0.262 | 0.258 | 0.179 |
|  | SS | 40.7947 | 98.3140 | 142.5851 | 99.9653 | 120.2230 |
| Hixson-Crowell | R2 | -0.1172 | -0.7564 | 0.5100 | -0.0728 | -1.1741 |
|  | KHC | 0.008 | 0.009 | 0.032 | 0.009 | 0.009 |
|  | SS | 4804.8561 | 7396.2969 | 6955.8384 | 5577.0266 | 9061.8175 |
| Hopfenberg | R2 | 0.0268 | -0.5439 | 0.6571 | 0.0762 | -0.9011 |
|  | KHB | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
|  | SS | 4185.4535 | 6501.1905 | 4867.3656 | 4802.0359 | 7923.7080 |
| Baker-Lonsdale | R2 | 0.7990 | 0.5445 | 0.9086 | 0.7928 | 0.3837 |
|  | KBL | 0.002 | 0.003 | 0.010 | 0.003 | 0.003 |
|  | SS | 864.6038 | 1917.9818 | 1297.7094 | 1077.3329 | 2568.6804 |
| Weibull | R2 | 0.9943 | 0.9739 | 0.9707 | 0.9748 | 0.9944 |
|  | SS | 24.6371 | 110.0523 | 416.2617 | 131.1917 | 23.3906 |
| Gompertz | R2 | 0.9893 | 0.9656 | 0.9345 | 0.9583 | 0.9831 |
|  | SS | 45.8105 | 144.9309 | 930.3335 | 216.7893 | 70.5727 |