<Supporting Information>

Control of maleic acid-propylene diepoxide hydrogel for 3D printing application for flexible tissue engineering scaffold with high resolution by end capping and graft polymerization

Hao Nguyen Tran1, Ingul Kim2, Jong Heon Kim3, Eun-Jae Chung2, Insup Noh1,3

1 Department of Chemical and Biomolecular Engineering, Seoul National University of Science and Technology, Seoul 01811, Republic of Korea

2Department of Otorhinolaryngology, College of Medicine, Seoul National University Hospital, Seoul 03080, Republic of Korea

3 Convergence Institute of Biomedical Engineering and Biomaterials, Seoul National University of Science and Technology, Seoul 01811, Republic of Korea

Correspondence to Insup Noh (insup@seoultech.ac.kr)

(Submitted to Biomaterials Research, July 05, 2022)

Methods

Stretchability test: The stretchability of MPLE gel was evaluated by twisting the gel sample (2 mm x 8 mm x 40 mm) in air. Both sides of the samples were manually hold by using tweezers. Afterwards, the upper side was twisted and pulled upward gradually until breakage.

Self-healing test: The self-healing nature of both MPLE gels and LP-capped gel were evaluated by physical observation. The gel samples were cut into small pieces and thereafter brought into contact at 25℃. After self-healing for different intervals at 30 min, 4 hours, and 24 hours, the samples were manually extended to evaluate the self-healing property as well as fiber forming ability.

Gel fiber formation: The surface morphologies of the LP-capped gel fibres was investigated using scanning electron microscope (SEM; Tescan Vega 3, Czech Republic) with an accelerating voltage of 15 kV. For the gel fibre test, the LP-capped gel was manually stretched into very thin wire/fibres, then plunged in a liquid nitrogen slush for 20 min. Afterwards, the frozen samples were freeze-dried in a lyophilizer at -80 °C for 3 days.

Degree of conversion (DC) characterized by FTIR spectrometry: In this test, FTIR was utilized to examine the content of residual of C=C bonds in the MPLE gel (1:0.3) at different photo-crosslinking times (0, 1, 5, 10 mins). The degree of conversion (DC) was calculated based on the percentage of the remaining concentration of the aliphatic C=C double bonds (in 1642 cm−1) and the highly adsorbed C=O bands (1731 cm−1) as a reference peak before and after radical polymerization. All the experiments were performed in triplicate for each sample. The equation (1) was used by adopting previous publications [1-4]:

DC (%) = (1 - RcuredRuncured) x 100 (%)

Where Rcured is the absorbance ratio of polymerized aliphatic C=C double bonds and highly adsorbed C=O bands (C=Opolymer) after exposure to the UV light, while Runcured is the absorbance ratio of unpolymerized aliphatic C=C double bonds and highly adsorbed C=O bands (C=Ounpolymer) before exposure to the UV light.

Photorheology measurement: The photorheological study was conducted at room temperature (25°C) in parallel-plate mode with 25 mm diameter and 1 mm gap under the presence of UV light exposure. The unpolymerized inks were prepared in different ratios of LP-capped gel and PEGDA (1:0.1, 1:0.2, and 1:0.3 w/v) along with Irgacure 2959 (3% w/w) to obtain the photocurable inks, which were examined by shear rate of γ’ = 0.1 s-1. The irradiation started after 120 s and all samples were exposed to UV-light (365 nm, 30 mW/cm2) for a total of 480 seconds.

Results and discussion

Fig. S1: Step by step fabrication process of MPLE gel and its 3D printed sample.

Fig. S1: Stretchability of MPLE gels at initial stage (A-C) and after extension testing (D-F).

Both MPLE gels and LP-capped gel exhibited good flexible properties at early stage; however, the MPLE gels showed an obvious breakage when increasing the stretching force on the samples which indicates their limited stretchability when comparing to LP-capped gel.

Fig. S2: Self-healing test of LP-capped gel (A-D) with full heal-ability after 4 hours; and MPLE gel (1:0.3) (E-H) with partially recover after 24 hours.

The self-healability was tested for both LP-capped gel and MPLE gel (1:0.3) under ambient conditions. As displayed in Fig. S2, the hydrogel samples were cut into three small pieces, followed by dying in yellow, blue, and red colors (LP-capped gel) and yellow, orange, and pink colors [MPLE gel (1:0.3)]. After that, the cutting sections were attached together at the fresh surface. After 30min, the LP-capped gel started to adhere partially with the lines between the interfaces while the MPLE gel (1:0.3) was not adherent after 12 hours. Then the testing time was continued to 4 hours for LP-capped gel showing that the polymer matrix can be rearranged and repaired the damaged interfaces as fully recovery; however, the MPLE gel (1:0.3) exhibited limited healing property and stretchability.

Fig. S3: (A-a, A-b, A-c) Photographs of fibers formed by extension of LP-capped gel. (B) SEM images of the gel fiber at low and high magnification.

The optical Fig.s represent fiber formulation from LP-capped gel (Fig. S3A.a-c) where the fiber can be obtained by stretching manually. Fig. 3B reveals the fiber thicknesses ranging from 100-150 µm with rough surface. This is due to the shrinkage on the surface during the freeze-drying process. Furthermore, the outstanding elongation properties from LP-capped gel can be attributed to the combination between the hydrogen bonding and strong ionic interactions in the 3D crosslinked network.

Fig. S4. (A) FTIR spectra of MPLE (1:0.3) gel at different photo-crosslinking times and (B) their C=C bonds degree of conversion.

As shown in the Fig. S4-(A), the significant decrease of the C=C peak at 1642 cm-1 (yellow band) referring to C(=O) peaking was clearly observed over time (1, 5, and 10 mins) which confirmed the graft polymerization of PEGDA to the LP-capped copolymers under UV exposure. This result was consistent with the data presented in the Fig. S4-(B), where the degrees of conversions at 1, 5 and 10 mins were 23.47 ± 0.8%, 48.56 ± 5.4%, and 90.12 ± 4.5%, respectively.

3. References

[1]. Chen, H., Lee, S. Y., & Lin, Y. M. (2020). Synthesis and formulation of PCL-based urethane acrylates for DLP 3D printers. Polymers, 12(7), 1500.

[2]. Askari, F., Zandi, M., Shokrolahi, P., Tabatabaei, M. H., & Hajirasoliha, E. (2019). Reduction in protein absorption on ophthalmic lenses by PEGDA bulk modification of silicone acrylate-based formulation. Progress in Biomaterials, 8(3), 169-183.

[3]. Ashjari, H. R., Ahmadi, A., & Dorraji, M. S. S. (2018). Synthesis and employment of PEGDA for fabrication of superhydrophilic PVDF/PEGDA electrospun nanofibrous membranes by in-situ visible photopolymerization. Korean Journal of Chemical Engineering, 35(1), 289-297.

[4]. Belqat, M., Wu, X., Gomez, L. P. C., Malval, J. P., Dominici, S., Leuschel, B., ... & Mougin, K. (2021). Tuning nanomechanical properties of microstructures made by 3D direct laser writing. Additive Manufacturing, 47, 102232.