Supplementary Information

Atomic imaging and thermally induced dynamic structural evolution of two-dimensional non-layered Cr2S3

Chia-Ling Liu 1†, Yi-Tang Tseng 1, Chun-Wei Huang 2, Hung-Yang-Lo1, An-Yuan-Hou1, Che-Hung-Wang 1, AkiraYasuhara3, Wen-Wei Wu 1,4*

1 Department of Materials Science and Engineering, National Yang Ming Chiao Tung University, Hsinchu 300, Taiwan

2 Department of Materials Science and Engineering, Feng Chia University, Taichung 407, Taiwan

3 EM Application Department of EM Business Unit, JEOL Ltd, 3-1-2 Musashino, Akishima, Tokyo 196-8558, Japan

4 Center for the Intelligent Semiconductor Nano-system Technology Research, National Yang Ming Chiao Tung University, Hsinchu 300, Taiwan

*Correspondence and requests for materials should be addressed to W.W.W (email:

: wwwu@mail.nctu.edu.tw

List of contents

Figure S1｜Schematic diagram of the experimental setup.Figure S2｜XPS result of CVD-grown Cr2S3.

Figure S3｜EDS elemental mapping showing the distribution of Cr and S.

Figure S4｜Multislice simulated ADF-STEM image and atomic models of Cr-S compounds.Figure S5｜Simulated diffraction pattern of cross-sectional Cr-S compounds.

Figure S6｜Simulated diffraction pattern of plane-view Cr-S compounds.

Figure S7｜TEM images showing the phase transformation of Cr2S3 along [001].

Figure S8｜STEM images and EELS showing the morphologic information of FIB-fabricated Cr2S3 specimen.

Figure S9｜Line graph of theoretical distance between Cr atoms.

Figure S10｜Free energy curves at 600 °C.

Figure S11｜EDS result showing the variation of atomic ratio of Cr and S element.

Figure S12｜The schematic diagram of 2D and quasi-1D specimens shows the morphologic information and plane surface ratio.

Figure S1. The Schematic diagram of e experimental setup.

Figure S2. The XPS result of CVD-grown Cr2S3. (a) Survey scan spectrum for obtained Cr2S3 nanosheets and the corresponding atomic percentage of Cr and S elements are shown in the (b).

Figure S3. EDS elemental mapping showing the distribution of Cr and S.  (a) Low-magnification STEM image (b,c) EDX spectrum of the Cr2S3 nanoflake. (d) Cr and S elemental atomic percentage of the plots shown in (a).

Figure S4. Multislice simulated ADF-STEM image and atomic models of Cr-S compounds. (a) STEM image of R-Cr2S3. (b) STEM image of T-Cr2S3.  (c) STEM image of M-Cr3S4. (d) STEM image of T-Cr5S6. (f) Atomic model of R-Cr2S3. (g) Atomic model of T-Cr2S3.  (h) Atomic model of M-Cr3S4. (i) Atomic model of T-Cr5S6.

Figure S5. Simulated diffraction pattern of cross-sectional Cr-S compounds. (a) Simulated diffraction pattern of R-Cr2S3. (b) Simulated diffraction pattern of T-Cr2S3. (c) Simulated diffraction pattern M-Cr3S4. (d) Simulated diffraction pattern T-Cr5S6. (e) The d-spacing corresponds to Cr-S crystals.

Figure S6. Simulated diffraction pattern of plan-view Cr-S compounds. (a) Simulated diffraction pattern of R-Cr2S3. (b) Simulated diffraction pattern of T-Cr2S3. (c) Simulated diffraction pattern of M-Cr3S4. (d) The d-spacing corresponds to Cr-S crystals.

Figure S7. TEM images showing the phase transformation of Cr2S3 along [001].

(a) HRTEM image were held at 600 °C for three minutes. (b) Correspond FFT pattern under 600°C.

Figure S8. STEM images and EELS showing the morphologic information of FIB-fabricated Cr2S3 specimen. (a) Low-magnification ADF-STEM image shows the length of FIB-fabricated Cr2S3 is 4.56 µm. (b) High-magnification ADF-STEM image shows the width of FIB-fabricated Cr2S3 is 124 nm. (c) Electron energy loss spectroscopy determined the height of FIB-fabricated Cr2S3 is 117.5 nm.

Figure S9. Line graph of theoretical distance between Cr atoms. (a) Horizontal distance between Cr atoms for R-Cr2S3, Cr2S3(Trigonal), M-Cr3S4, and T-Cr5S6 crystals. (b) Vertical distance between Cr atoms for R-Cr2S3, T-Cr2S3, M-Cr3S4, and T-Cr5S6 crystals.

Figure S10. Free energy curves at 600 °C.35

Figure S11. EDS result showing the variation of atomic ratio of Cr and S element. (a) Atomic ratio of Cr and S under 25°C. (b)Atomic ratio of Cr and S under 400°C. (c)Atomic ratio of Cr and S under 600°C.

Figure S12. The schematic diagram of 2D and quasi-1D specimens shows the morphologic information and plane surface ratio.