Reusable titania-SBA-15 photocatalyst synthesized by different silica/titania ratios for enhancing methylene blue photodegradation

Sevgi Can Göl, Elif AKBAYa

Eskişehir Technical University, Dept. of Chemical Engineering, Eskişehir, 26470, Turkey

aCorresponding Authors: eodes@eskisehir.edu.tr

Supplementary data

Table S1. The naming of TiO2/SBA-15 (R=Si/Ti) catalysts synthesized containing of TiO2

| Name of catalyst | Containing TiO2 amount (g) |
| --- | --- |
| TiO2/SBA-15 (64) | 0.05 |
| TiO2/SBA-15 (32) | 0.1 |
| TiO2/SBA-15 (16) | 0.2 |
| TiO2/SBA-15 (11) | 0.3 |
| TiO2/SBA-15 (8) | 0.4 |
| TiO2/SBA-15 (6) | 0.5 |

Tablo S2. Amounts of catalyst used in the photocatalytic reaction for each catalyst

| Catalyst | TiO2 Content (mg) | Amount of Catalyst (mg) |
| --- | --- | --- |
| TiO2 | 6 | 6 |
| TiO2/SBA15 (R=64) | 6 | 311 |
| TiO2/SBA15 (R=32) | 6 | 162 |
| TiO2/SBA15 (R=16) | 6 | 75 |
| TiO2/SBA15 (R=11) | 6 | 65 |
| TiO2/SBA15 (R=8) | 6 | 50 |
| TiO2/SBA15 (R=6) | 6 | 39 |

Table S3. Textural properties of reused TiO2/SBA-15 (16) catalysts

| TiO2/SBA-15 (R=16) | Surface Area BET (m2/g) | Pore Volume (cm3/g) | Pore Diameter (nm) |
| --- | --- | --- | --- |
| Fresh catalyst | 609 | 0,76 | 5,45 |
| Reused Catalyst without calcination | 503 | 0,47 | 4,26 |
| Reused Catalyst with calcination | 670 | 0,67 | 4,75 |

Figures

b)

a)

d)

c)

f)

e)

Figure S1. The bandgap energy (Eg) by using the modified plot of the Kubelka–Munk function, a) TiO2/SBA-15(R=64), b) TiO2/SBA-15(R=32), c) TiO2/SBA-15(R=16), d) TiO2/SBA-15(R=11), e) TiO2/SBA-15(R=8), f) TiO2/SBA-15(R=6)

Figure S2. Wide-angle (a) and small-angle (b) XRD patterns of reused TiO2/SBA-15 (16) catalysts

c)

b)

a)

Figure S3. SEM of reused TiO2/SBA-15 (16) catalysts; a) fresh B) reused, c) reused with calcination

Figure S4. (a) N2 adsorption-desorption isotherms and (b) pore distributions of reused TiO2/SBA-15 (16) catalysts